SUPPORTING INFORMATION

Perovskite detectors for X-ray detection

| Material | Sensitivity (μC Gy–1 cm–2) | LoD (nGyair s−1) | Electric field (V μm-1) | Flexibility | Ref |
| --- | --- | --- | --- | --- | --- |
| CsPbBr3 Quasi‐Monocrystalline Film | 55684 | - | 4200 | No | 1 |
| MA3Bi2I9 polycrystalline wafer | 563 | 9.3 | 0.2 | No | 2 |
| CH3NH3PbI3 wafer | 122000 |  | 0.013 | No | 3 |
| Cs2AgBiBr6 in a polymer matrix | 40 | - | 4 | 10 mm | 4 |
| MAPb(I0.9Cl0.1)3-filled membranes | 8696 ± 228 | - | 0.05 | 45 mm x 10 cycles | 5 |
| MAPbI3 filled PET | 6722 | 1.87 | 8.7 | 0.5 mm x 3000 cycles | 6 |
| Layered polymer-perovskite (CsPbBr3 , MAPBr3; Cs2AgBiBr6, FAPbI3) | 8380 | 26 | 1 (LoD: 0.5) | 1.5 mm x 30000 cycles | 7 |
| CsBi3I10 | 1622.53 | 220 |  | Yes, radius n/a | 8 |
| CsPbBr3-PBMA composite | 106 ± 1 | 37.2 ±1.1 | 0.43 | 0.5 mm max 5 mm x 1500 cycles | This work |

Table S1: Comparison of the detection performance of flexible and rigid perovskite X-ray detectors.

Perovskite detectors for proton detection

| Material | Proton energy (MeV) | Electric field (V μm-1) | Sensitivity (C H+ -1) | Ref. |
| --- | --- | --- | --- | --- |
| CsPbCl3 film | 100-228 | 2 | 4·10-20 | 9 |
| MAPbBr3-(PEA)2PbBr4 film | 5 | 0.2 | (1.12 ± 0.01)·10-18 | 10 |
| MAPbBr3 single crystal | 3 | 0.01 | (2.19 ± 0.03)·10-18 | 11 |
| (PEA)2PbBr4 film | 5 | 0.5 0.5 | (1.0 ± 0.2) × 10−17 (2 μm film) (5.7 ± 0.1) × 10−18 (10 μm film) | 12 |
| CsPbBr3 – PBMA composite | 5 | 2 0.1 0.1 | (9.3 ± 0.2)∙10-18 (100 μm) (1.1 ± 0.1)∙10-19 (100 μm) (6.3 ± 0.3)∙10-19 (470 μm) | This work |

Table S2: Comparison of the detection performance perovskite proton detectors.

Polymer-perovskite composites

Figure S1: XRD spectrum of the composite pellet and of the powder before pressing compared with reference orthorhombic CsPbBr3 spectrum.

Photoconducting properties

Figure S2: : (a) Bias study of the 100 µm sample to maximize the photocurrent, three peaks for each applied bias are acquired shining an X-ray beam at 40 kVp with dose rate 410 µGy/s. (b) Photocurrent values extracted from the dynamics acquired in (a)

Figure S3: Photocurrent as a function of dose rate over an extended dose rate range showing an exponential trend y=xα with α = 0.79.

Figure S4: Irradiations performed at 58 nGy/s of the 470 µm pellet biased at 0.426 V/µm

Figure S5: dark current of 100 µm pellet operated at 1.6 V µm-1 for 14 hours and 41 minutes. The insert shows the typical initial bias relaxation trend.

Flexible photoconductors

Figure S6:  IV characteristic of 100 µm pellet on PET in dark conditions and under 1 sun illumination.

Figure S7: (a) dynamic response of one pixel in the 100 μm sample on PET biased at 0.426 V/µm. (b) Average sensitivity of 4 pixel in the 100 μm sample biased at 0.426 V/µm from which the sensitivity is extracted though a linear fit.

Figure S8: (top) cross-section SEM image of the bent portion of the device. (bottom) Cross-section SEM image a portion of the composite where no bending has occurred. Both images refer to a part of the sample not delaminated form the plastic substrate.

Proton detection

Figure S9: the SRIM simulations of the linear energy transfer of a proton beam of 4.4 MeV protons with only CsPbBr3 (ρ = 4.55 g cm⁻³), and only PBMA (ρ = 0.89 g cm⁻³).