Supplementary materials

Algal cultivation

Each strain was grown in 200 mL Erlenmeyer glass flasks, at 20±2 °C, light intensity 90-110 µmol m-2 s-1, and with light:dark photoperiod 16:8 h. A. platensis was maintained in 1 L bottle supplied with air at a low flow rate (1-2 L min-1) at 25±2 °C and with light intensity of 250-300 µmol m-2 s-1. Before the exposure to SWCNTs, algal cultures at the exponential growth phase were diluted with the respective growth medium to obtain the specific optical density chosen for the tests, which was measured at 750 nm (OD750) using a JASCO spectrophotometer (UV/VIS, JASCO V-650, Tokyo, Japan). Aliquots of algal culture (1 mL) were diluted with the respective growth medium at an OD₇₅₀ of 0.1. The ζ-potential was then measured in triplicate at the spontaneous pH and 25 °C using a Zetasizer Nano ZSP analyser (Malvern, UK) with DTS1061 cells.

Characterisation of algal biomass and growth media analysis

After 7 and 14 days of growth in the presence of 1 mg L-1 of LSZ@SWCNT, Thalassiosira sp. and A. platensis biomass were collected through centrifugation (Thalassiosira sp.) or by filtration on nylon filters with a porosity of 11 µm (A. platensis).

The obtained filtrates were maintained at -20°C to determine the main physicochemical parameters (pH and conductivity) and the residual inorganic nutrient content (N-NO3 and P-PO4). The pH was measured with a pH meter, while conductivity was determined using a HACH water probe (HQ4300). For A. platensis, both N-NO3 and P-PO4 contents were determined by ionic chromatography (883 Basic IC plus, METROHM, Switzerland), while due to the salinity of the growth medium, residual N-NO3 and P-PO4 of Thalassiosira sp. cultures were determined spectrophotometrically by the cadmium-copper reduction to nitrite and the molybdate blue method, respectively.

The collected biomass was analysed as follows:

- Proteins were extracted from freeze-dried algal biomass (10-15 mg) with 3 mL NaOH (0.5 M), incubated at 90°C for 8 min under magnetic stirring, transferred to ice for 2 min, and subsequently centrifuged (2550 × g, 10 min). The resulting supernatant was collected, and the extraction procedure was repeated 3 times. Protein content was determined in the collected supernatant with the Folin phenol reagent.1

- Intracellular polysaccharides were extracted from freeze-dried samples (5-10 mg) and quantified spectrophotometrically through the phenol‑sulfuric acid colourimetric reaction.2,3

- Lipids were extracted from freeze-dried samples (50 mg) with 2 mL of a dichloromethane/methanol 2:1 mixture. The samples were stirred at 60°C for 1 h and then centrifuged (3000 × g, 10 min) to separate the supernatant from the residual biomass. The procedure was repeated twice, and after complete solvent evaporation, total lipids were measured gravimetrically, while fatty acids were analysed by GC-MS.4

- Chlorophyll a and carotenoids were extracted from freeze-dried biomass (5 mg) by a modified bead-beating protocol.5 The extraction solvent, i.e., acetone, was saturated with CaCO3 to avoid phaeophytinisation. Afterwards, algal biomass was weighed in a 1.5 mL Eppendorf tube with glass beads (size 0.5 mm), and then 1 mL of CaCO3-saturated acetone was added. The mixture was first vortexed for 1 min, then transferred into an ultrasonic bath for 20 min, and this sequence was repeated twice. The supernatant was collected and diluted 10 times, and then chlorophyll a and total carotenoids were determined spectrophotometrically by measuring the absorbance at 750, 662, 645, and 470 nm. Pigment degradation was minimised by analysing all the extracts immediately after the extraction step and performing the analysis in semi-dark conditions. The concentration of chlorophyll a and total carotenoid was measured according to the following equations modified from the literature:

(1)				Chla=11.24×A662-2.04×A645

(2)				Cartot=1000 × A470 -1.90×Chla/214

Where:

Chla = concentration of chlorophyll a

Cartot = concentration of total carotenoids

A662, A645 and A470 = absorbance at 662, 645, and 470 nm

Chlorophyll a and total carotenoid contents were expressed as a percentage of dry weight (%dw).

- C-phycocyanin (C-PC) was determined on freeze-dried samples of A. platensis (5 mg) according to the literature.6 The samples were extracted with 1 mL of phosphate buffer 0.1 M (pH 7) and then kept for 24 h at 25°C under constant magnetic stirring. Samples were centrifuged (2550 × g, 10 min), and the supernatant was diluted 20 times with 0.1 M phosphate buffer. C-PC content was derived spectrophotometrically by measuring the absorbance at fixed wavelengths of 615 and 652 nm, using the following equation:

(3)				C-PC =A615-0.474×A652 / 5.43

Where:

C-PC = concentration of C-phycocyanin

A615 and A652 = absorbance at 615 and 652 nm

Data were expressed as a percentage of dry weight (%dw).

- Micro-Raman spectroscopy. Algal samples were centrifuged and washed twice with distilled H2O. The samples were drop-cast on microscope slides, and the Raman spectra were recorded with a Renishaw micro-Raman 1000 system, exciting at 514 nm (Argon green laser) at RT. 20x objectives were used to reach different degrees of magnification. To reduce the pigments’ autofluorescence background, samples underwent a photobleaching process, i.e., pre-illuminating the photosynthetic sample with defocused intense light to saturate and vanish (photo bleach) fluorescence from the fluorophores.

- ESEM and TEM analysis. Algal samples were centrifuged, washed twice with distilled H2O, fixed using 2.5% glutaraldehyde in 0.1 M phosphate buffer, and kept overnight at 4 °C. After that, the samples were washed 4 times with 0.1 M phosphate buffer, then dehydrated with increasing gradients of ethanol (from 50 to 100%). Finally, the dehydrated samples were dried in air, mounted on stubs covered with carbon foil, coated with gold using a BIO-RAD Sem Coating System SC502 working at 12 mA for 1 min, and then images were acquired by an ESEM-FEG QUATTRO S (Thermofisher). For TEM analysis, algal samples were centrifuged and processed for ultrastructural study using the following protocol: the pellets were fixed by immersion in 2.5% glutaraldehyde (DDK, Italia) in cacodylate buffer 0.1 M and post-fixed in 1% OsO4 (EMS, Hatfield, PA) in 0.1 M cacodylate buffer. Specimens were dehydrated in ascending ethanol and embedded in Araldite (Serva, Heidelberg, Germany). Thin sections, stained with uranyl acetate and lead citrate, were studied using a TEM Philips CM100 (Philips/FEI Corporation, Eindhoven, The Netherlands), and images of the samples were acquired by ITEM (FEI FIVE) image acquisition software.

1 Lowry, O.H., Rosebrough, N.J., Farr, A.L., Randall, R.J., 1951. Protein measurement with the Folin phenol reagent. J. Biol. Chem. 193, 265–275. https://doi.org/10.1016/0304-3894(92)87011-4.

2 Dubois, M., Gilles, K.A., Hamilton, J.K., Rebers, P.A., Smith, F., 1956. Colorimetric method for determination of sugars and related substances. Anal. Chem. 28, 350–356. https://doi.org/10.1021/ac60111a017

3 Myklestad, S., Haug, A., 1972. Production of carbohydrates by the marine diatom Chaetoceros affinis var. willei (Gran) Hustedt. I. Effect of the concentration of nutrients in the culture medium. J. Exp. Mar. Bio. Ecol. 9, 125–136. https://doi.org/10.1016/0022-0981(72)90041-X

4 Samorì, C., Torri, C., Fabbri, D., Falini, G., Faraloni, C., Galletti, P., Spera, S., Tagliavini, E., Torzillo, G., 2012. Unusual Catalysts from Molasses: Synthesis, Properties and Application in Obtaining Biofuels from Algae. ChemSusChem 5, 1501–1512. https://doi.org/10.1002/cssc.201100822

5 Hynstova, V., Sterbova, D., Klejdus, B., Hedbavny, J., Huska, D., Adam, V., 2018. Separation, identification and quantification of carotenoids and chlorophylls in dietary supplements containing Chlorella vulgaris and Spirulina platensis using High Performance Thin Layer Chromatography. J. Pharm. Biomed. Anal. 148, 108–118. https://doi.org/10.1016/j.jpba.2017.09.018

6 Pan-utai, W., Kahapana, W., Iamtham, S., 2018. Extraction of C-phycocyanin from Arthrospira (Spirulina) and its thermal stability with citric acid. J. Appl. Phycol. 30, 231–242. https://doi.org/10.1007/s10811-017-1155-x

Table S1. Microalgae and cyanobacteria used in the present study. Suppliers: SAG = Culture Collection of Algae of Göttingen University; CCAP = Culture Collection of Algae and Protozoa; CCMP = Provasoli-Guillard National Center for Marine Algae and Microbiota (NCMA), formerly known as Culture Collection of Marine Phytoplankton.

| Strain | Class | Strain details | Growth medium | Source, strain num. |
| --- | --- | --- | --- | --- |
| Euglena gracilis | Euglenophyceae | Freshwater, unicellular, motile, ~ 10x10x45 µm | Cramer-Myers (CM) 1 | SAG 1224-5/25 |
| Scrippsiella sp. | Dinophyceae | Seawater, unicellular, motile, thecate, ~ 15x15x20 µm | f/2 with 5-fold diluted N and P, salinity 30‰ (fN/10 P/10 30) 2 | Northern Adriatic Sea (Emilia-Romagna, Italy) |
| Thalassiosira sp. | Mediophyceae | Seawater, colonial, 2 - 20 cells bound by a chitin fibril, single cylindrical cells, ~ 24x23 µm | f/2 + Na2SiO3, salinity 30‰ (f/2+Si 30) 2 | Northern Adriatic Sea (Marche, Italy) |
| Stephanodiscus hantzschii | Mediophyceae | Freshwater, unicellular, spherical, diameter ~ 5 µm | Diatom’s medium (DM) 3 | CCAP 1079/4 |
| Arthrospira platensis | Cyanophyceae | Freshwater, alkaline (pH > 9), filamentous (100 µm long spiral-like shape), ~ 2x2x6 µm | Zarrouk’s medium (ZM) 4 | Alkaline freshwater pond (Emilia-Romagna, Italy) |

1 Cramer M., Myers J., Arch. Mikrobiol., 1952, 17, 384–402.

2 Guillard R.R.L., Culture of Phytoplankton for Feeding Marine Invertebrates. In: Smith, M.L. and Chanley, M.H., Eds., Culture of Marine Invertebrates Animals, Plenum Press, New York, 1975, 29-60.

3 Beakes G.W., Canter H.M., Jaworski G.H.M., Can. J. Bot., 1988, 66(6), 1054-1067.

4 Zarrouk C., Ph.D. thesis, Univ. Paris, France,1966.

Table S2. The main properties of the different proteins tested here to disperse SWCNTs.1,2,3,4

| Protein | MW (kDa) | Isoelectric point | Primary structure | Secondary structure | Sigma-Aldrich code |
| --- | --- | --- | --- | --- | --- |
| Lysozyme, LSZ | 14.4 | 10.7 | Single polypeptide chain; 129 AA residues; 4.6% lysine, 8.5% arginine | 42% α- helix; 6% β-sheet; globular protein | L6876 |
| Bovine Serum Albumin, BSA | 66.4 | 4.5 | Single polypeptide chain; 583 AA residues; high percentage of acidic and polar residues | 69% α- helix organised in three domains; globular protein | A2153 |
| Histone, HST | 15.3 | 11.7 | High content of lysine and arginine | Octamer; three α- helixes | H9250 |
| Myoglobin, MGB | 16.9 | 7.2 | Single polypeptide chain; 154 AA residues | 75% α-helix; one heme group into a hydrophobic cleft; globular protein | M1882 |
| Protamine, PRT | 4.3 | 13 | Single short polypeptide chain; 31 AA residues; 50% arginine | α- helix | P4005 |

1 Nepal D., Geckeler K.E., Small, 2006, 2(3), 406-412.

2 Matsuura K., Saito T., Okazaki T., Ohshima S., Yumura M., Iijima S., Chem. Phys. Lett., 2006, 429, 497-502.

3 Gangloff Y. G., Romier C., Thuault S., Werten S., Davidson I., Trends Biochem. Sci., 2001, 26(4), 250-257.

4 Lewis J. D., Saperas N., Song Y., Zamora M. J., Chiva M., Ausiò J., PNAS, 2004, 101(12), 4148-4152.

5 Eslami-Farsani R., Farhadian S., Shareghi B., Asgharzadeh S., J. Mol. Liq., 2022, 352, 118691.

Table S3. ζ-Potential (mV) of the tested microalgae and cyanobacteria. Data are reported as the mean of three replicates ± standard deviation.

| Species | ζ-Potential (mV) |
| --- | --- |
| E. gracilis | -22.0±1.7 |
| Scrippsiella sp. | n.d. |
| Thalassiosira sp. | -6.0±1.3 |
| S. hantzschii | -18.7±1.7 |
| A. platensis | -19.3±1.0 |

Table S4. Physicochemical parameters (pH and conductivity) and residual inorganic nutrients (N-NO3 and P-PO4) measured in A. platensis and Thalassiosira sp. cultures after 7 and 14 days.

|  |  |  | pH | Conductivity (mS cm⁻¹) | N-NO₃ (mg L⁻¹) | P-PO₄ (mg L⁻¹) |
| --- | --- | --- | --- | --- | --- | --- |
| A. platensis | day 7 | CTRL | 10.16 | 19.78 | 245.4 | 43.2 |
|  |  | LSZ@SWCNT | 10.19 | 19.91 | 233.4 | 43.4 |
|  | day 14 | CTRL | 10.36 | 20.84 | 229.4 | 45.0 |
|  |  | LSZ@SWCNT | 10.26 | 22.02 | 235.6 | 43.1 |
| Thalassiosira sp. | day 7 | CTRL | 8.62 | 40.70 | 5.6 | 0.12 |
|  |  | LSZ@SWCNT | 8.76 | 43.13 | 4.8 | 0.10 |
|  | day 14 | CTRL | 8.67 | 50.00 | 5.4 | 0.07 |
|  |  | LSZ@SWCNT | 8.73 | 49.37 | 4.8 | 0.07 |

Table S5. Lipophilic pigments content, and the ratio between chlorophyll a and total carotenoids of A. platensis and Thalassiosira sp. after 7 and 14 days (d) of exposure to LSZ@SWCNT at the concentration of 1 mg L-1 compared to the control. (Chla = chlorophyll a, expressed as a percentage on a dry weight basis, %; Cartot = total carotenoids, expressed as a percentage on a dry weight basis, %; Chla/Cartot = ratio between Chla and Cartot).

|  | Time (d) | Chla (%) |  | Cartot (%) |  | Chla/Cartot |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | A. platensis | Thalassiosira sp. | A. platensis | Thalassiosira sp. | A. platensis | Thalassiosira sp. |
| Control | 7 | 2.25 | 1.03 | 0.52 | 0.65 | 4.34 | 1.59 |
|  | 14 | 2.65 | 0.82 | 0.62 | 0.59 | 4.30 | 1.38 |
| LSZ@SWCNT | 7 | 2.64 | 0.88 | 0.53 | 0.50 | 4.97 | 1.75 |
|  | 14 | 2.73 | 1.17 | 0.59 | 0.70 | 4.62 | 1.69 |

Table S6. The ratio between saturated and unsaturated fatty acids (i.e. SFA/UFA) of A. platensis and Thalassiosira sp. measured after 7 and 14 days (d) of exposure to LSZ@SWCNT at the concentration of 1 mg L-1 compared to the control.

|  | Time (d) | SFA/UFA ratio |  |
| --- | --- | --- | --- |
|  |  | A. platensis | Thalassiosira sp. |
| Control | 7 | 1.0 | 0.9 |
|  | 14 | 0.8 | 0.6 |
| LSZ@SWCNT | 7 | 0.9 | 0.6 |
|  | 14 | 1.0 | 0.5 |

Figure S1. UV-Vis absorption spectra of a) LSZ@SWCNT, b) BSA@SWCNT, c) HST@SWCNT, and d) SWCNT-COOH in the algal growth media. (CM: Cramer’s medium for euglenoids; DM: Diatom’s medium for freshwater diatoms; f/2+Si 30: f/2 medium plus silica at salinity 30‰ for marine diatoms; f N/10 P/10 30: f/2 with five-fold diluted macronutrients N and P, at salinity 30‰ for marine dinoflagellates; ZM: Zarrouk’s medium for alkaline cyanobacteria).

Figure S2. Optical density measured at 750 nm (%/ctrl) of E. gracilis, Scrippssiella sp., A. platensis, S. hantzschii and Thalassiosira sp. exposed for 72 h to LSZ@SWCNT at the concentrations of 0.1 and 1 mg L-1.

Figure S3. Microscope images of the diatoms S. hantzschii (a and b) and Thalassiosira sp (c and d) exposed for 72 h to LSZ@SWCNT at the concentrations of 1 (a and c) and 10 mg L-1 (b and d) (320x magnification, Zeiss Axiovert 100).

Figure S4. Photosynthetic activity (maximum quantum yield, Ymax, %/ctrl) of E. gracilis, S. hantzschii, and Thalassiosira sp. exposed for 72 h to LSZ@SWCNT at the concentration of 10 mg L-1.

Figure S5. Optical density measured at 750 nm (%/ctrl) of A. platensis and Thalassiosira sp. measured after 1, 3 and 7 days of exposure to SWCNT-COOH, HST@SWCNT, and LSZ@SWCNT at a concentration of 1 mg L-1.

Figure S6. Performances of A. platensis and Thalassiosira sp. evaluated after 7 and 14 days of exposure to LSZ@SWCNT at a concentration of 1 mg L-1 in 0.5-L experiments: a) maximum quantum yield, Ymax, and effective quantum yield, Yeff (%/ctrl); b) optical density measured at 750 nm (%/ctrl).

Figure S7. Fatty acid profile (relative distribution, %) of a) A. platensis and b) Thalassiosira sp. exposed for 7 and 14 days to LSZ@SWCNT at a concentration of 1 mg L-1 compared to the control. Myristic acid (14:0), pentadecanoic acid (15:0), palmitoleic acid (16:1), palmitic acid (16:0), γ-linolenic acid (γ-18:3), linoleic acid (18:2), oleic acid (18:1), stearic acid (18:0), eicosapentaenoic acid (20:5) and docosahexaenoic acid (C22:6).

Figure S8. Raman spectra (λexc = 514 nm) at RT of a) A. platensis (dark line) exposed to LSZ@SWCNT at a concentration of 1 mg L-1 and the corresponding control (blue line) from 1742 to 1143 cm-1 and b) LSZ@SWCNT from 100 to 3200 cm-1.

Figure S9. ESEM images of A. platensis samples after 14 days, untreated (a, c, e) and treated with LSZ@SWCNT at the concentration of 1 mg L-1 (b, d, f) Images were taken at different magnification values: 10000x (a, b), 20000x (c, d) and 50000x (e, f).

Figure S10. ESEM images of Thalassiosira sp. samples after 14 days, untreated (a, c, e) and treated with LSZ@SWCNT (b, d, f) at the concentration of 1 mg L-1 (b, d, f). Images were taken at different magnification values: 10000x (a, b), 20000x (c, d) and 50000x (e, f).

Figure S11. TEM images of A. platensis and Thalassiosira sp. without treatment (a, c) and exposed to SWCNT@LSZ at a concentration of 1 mg L-1 for 14 days (b, d). White letters indicate observed effects on some cellular structures upon exposure (md = membrane detachment; v = vacuolization; ch = chloroplasts; sg = starch grain-like structures; cc = compromised cytoplasmic compartment with empty spaces). Images were acquired at magnifications of 13500 and 19000x.