SUPPORTING INFORMATION

Unique Performance Considerations for Printable Organic Semiconductor and Perovskite Radiation Detectors: Towards Consensus on Best Practice Evaluation

Jessie A. Posar,1,2,* Matthew Large,3 Andrea Ciavatti,4 Laura Basiricò,4 Beatrice Fraboni,4 Paul J. Sellin,5 Attila J. Mozer,6 Marco Petasecca,3 and Matthew J. Griffith 2,7,*

J. A. Posar

1. Centre for Medical Radiation Physics, University of Wollongong, Wollongong, NSW, 2522, Australia

2. School of Aeronautical, Mechanical and Mechatronic Engineering, University of Sydney, Camperdown, NSW, 2506, Australia.

E-mail: j.posar@uow.edu.au

M. Large, M. Petasecca

3. Centre for Medical Radiation Physics, University of Wollongong, Wollongong, NSW, 2522, Australia.

A. Ciavatti, L. Basiricò, B. Fraboni

4. Department of Physics and Astronomy, University of Bologna, Viale Berti Pichat 6/2, Bologna, 40127, Italy.

P. Sellin

5. Department of Physics, University of Surrey, Guildford, Surrey, GU2 7XH, United Kingdom.

A. J. Mozer

6. Intelligent Polymer Research Institute, Innovation Campus, Squires Way, North Wollongong, NSW 2500, Australia.

M. J. Griffith

2. School of Aeronautical, Mechanical and Mechatronic Engineering, University of Sydney, Camperdown, NSW, 2506, Australia

7. Future Industries Institute, University of South Australia, Mawson Lakes, SA, 5095, Australia.

Email: matthew.griffith@unisa.edu.au

Measurement of Mobility Using Space Charge Limited Current

Charge mobility can be derived from the current – voltage behavior of diodes and transistors under specific operational regimes. The derivation of mobility values from these characterizations is convenient as they can be performed on the same device used for sensitivity measurements with the same instrumentation, without a need for dedicated mobility measurement systems. According to the Mott-Gurney law, the space charge limited current density (J) of a single charge carrier device can be described as:[138]

(Eq. 7)

(Eq. 7)

J=98εμV2d3

where ɛ is the dielectric constant of the semiconductor, V is the applied voltage and d is film thickness. The space charge limited condition may be achieved at sufficiently high voltages when the amount of injected charge in the device reaches the amount of the charge stored on the electrodes (capacitive charge). Typically, the logarithm of the current output of the diode is plotted versus the logarithm of the applied voltage, and the mobility is calculated from the section of the curve where the slope equals 2.

Measurement of Mobility Using Time of Flight (TOF)

The TOF mobility is measured from the carrier drift velocity vdr, assuming that the drift velocity is not saturated, from the expression:

(Eq. 10)

(Eq. 10)

The carrier drift velocity is deduced from the measured carrier transit time tr, and the thickness d of the sample. For an applied bias voltage V, the mobility becomes:

(Eq. 11)

(Eq. 11)

μ=d2Vτtr

(Eq. 12)

(Eq. 12)

Hence a plot of 1/tr vs V is often used to extract mobility from the gradient, which has a value of /d2. As previously discussed, this basic parameterization of mobility assumes that there is no field dependence, which will tend to make single-point mobility measurement less reliable. Under the influence of the applied electric field, the generated carriers drift towards the contacts and induce a current pulse in the external circuit. The induced current is proportional to the drift velocity of the carrier, by Ramo's theorem, giving:

I(t)=vdr(t) qd

where q is the total charge created by the event, and d is the active width of the device. For very fast drift velocities bandwidths of >1GHz are necessary, which require careful shielding and earthing to prevent pickup of RF noise. Alternatively, where drift times are not too short (eg. > 50 ns), an integrating charge preamplifier can be used which generally provides a better signal/noise ratio than a current amplifier.

Measurement of Mobility Using the Hecht Equation

(Eq. 14)

(Eq. 14)

The total charge induced at the device contacts is fundamentally defined in terms of electron and hole drift lengths, and the generalised carrier population N(x) at a distance x from the point of origin is given by:

Nx=N0exp-xλ=N0exp-xμτE

(Eq. 15)

(Eq. 15)

In the most general form, the expression for the depth-dependent charge collection efficiency CCE(x), where x is the distance of the interaction position from the cathode, can be expressed in terms of the separate electron and hole drift lengths. This is given by

CCE(x)=Q(x)N0q=λhd1-exp-xλh+λed1-expx-dλe

where e, h are the electron-only and hole-only mean drift lengths, and d is the detector thickness. This expression is the generalised form of the Hecht Equation, first published in 1932,[149] describing the variation in induced charge as a function of the interaction depth in the detector.

(Eq. 16)

(Eq. 16)

The Hecht method measures the mean charge amplitude of each pulse as a function of increasing bias, using the Hecht equation to extract the mobility-lifetime product as a direct measure of the charge transport performance of the device. Alpha particle irradiation is typically used for this measurement, particularly if the detector devices are relatively thick (eg. >100 m). In this case the alpha particle is stopped at a shallow depth ~20µm under the irradiated contact, and the induced signal is predominantly due to charge drift to the far electrode. Therefore, for alpha irradiation of the anode contact the resulting signal measures hole transport, and vice versa for cathode irradiation. In this limiting case where x << d, the general form of the Hecht equation can be simplified to the ‘single carrier’ Hecht equation:

CCE=λd1-exp-dλ

By fitting the single carrier Hecht equation, the mobility-lifetime product can be separately extracted for either electrons or holes.

Measurement of Mobility Using photoCELIV

CELIV was originally developed as an alternative to TOF to measure charge mobility in microcrystalline silicon exhibiting a large intrinsic charge carrier concentration.[151] In such high intrinsic conductivity cases, TOF is problematic as the externally applied electric field rapidly rearranges (within the dielectric relaxation time) and the charge carriers drift under a time-dependent, non-uniform electric field, giving erroneous TOF mobility values as discussed in Section 4.3. Juska et al realized that in such cases charge mobilities can instead be determined from the dielectric relaxation process by applying a linearly increasing voltage sweep (Figure 9a). For the case of materials with low intrinsic conductivity, the current response over a low impedance (differential mode) is a step-like current pulse, where the constant current density, j(0) corresponds to the constant charging of the capacitor.[141] From j(0), either the film thickness or the dielectric constant of the sample can be calculated if the other parameter is already known. CELIV requires a blocking contact, i.e. no charge injection at least on the timescale of the voltage ramp. Typically, at least one good blocking contact of a diode can fulfill this requirement. If intrinsic charge carriers are present, for example through doping, a current peak additional to the capacitive current pulse is detected. From the time to reach extraction current maximum (tmax), the charge mobility can be calculated (Figure 9b). Additional charge carriers can also be photogenerated by a steady state illumination or by a laser pulse preceding the voltage extraction pulse, a technique known as photoCELIV.[152] In the latter case, an additional measurement parameter, a delay time, can be introduced. Such delay time-dependent photo-CELIV measurements proved to be particularly useful to simultaneously measure charge carrier lifetime (from the extracted charge carrier density versus delay time) and charge mobility (obtained from tmax) versus charge density, delay time or mean applied electric field strength (A’× tmax).[133]