SUPPLEMENTARY MATERIALS

Molecular characterisation

Figure S1: 1H-NMR spectrum of P(BS-HDG)5 copolymer with signals’ assignment.

Figure S2: 13C-NMR spectra of all the materials under study with signals’ assignment

Table S1: Values of integrals of the 13C-NMR signals and the probability values used to calculate the degree of randomness and the block length for P(BS-HDG)5, P(BS-HDG)20 and P(BS-HDG)120 copolymers.

|  | P(BS-HDG)5 | P(BS-HDG)20 | P(BS-HDG)120 |
| --- | --- | --- | --- |
| IS-B-S | 1 | 1 | 1 |
| IS-B-DG and IDG-B-S | 0.03 and 0.07 | 0.14 and 0.24 | 0.55 and 0.54 |
| IDG-B-DG | - | - | 0.35 |
| IDG-H-DG | 0.58 | 0.66 | 0.56 |
| IDG-H-S and IS-H-DG | 0.05 and 0.05 | 0.16 and 0.11 | 0.50 and 0.43 |
| IS-H-S | - | - | 0.38 |
| PB-S | 0.043 | 0.160 | 0.353 |
| PB-DG | - | - | 0.609 |
| PH-DG | 0.079 | 0.170 | 0.454 |
| PH-S | - | - | 0.550 |

Thermal characterisation

Figure S3: DSC scans of all the polymers under study: crystallization from the melt (10 °C/min).

Table S2: Crystallization temperature (Tc) and enthalpy (ΔHc) obtained from cooling DSC scans (10 °C/min)  of all the polymers under study

| Sample | Tc (°C) | ΔHc (J/g) |
| --- | --- | --- |
| PBS | 74 | 66 |
| PBS/PHDG | 65 | 39 |
| P(BS-HDG)5 | 59 | 43 |
| P(BS-HDG)20 | 33 | 39 |
| P(BS-HDG)120 | - | - |
| PHDG | - | - |

Mechanical cyclic tests

Table S3: Cyclic test data of PBS/PHDG and P(BS-HDG)5 after 21 cycles. Experiment 1: maximum elongation of 8% and 10% for PBS/PHDG and P(BS-HDG)5; Experiment 2: maximum elongation of 18% and 20% for PBS/PHDG and P(BS-HDG)5.

| Polymer | Experiment 1 |  | Experiment 2 |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Shape recovery (%) | Hysteresis (mJ/mm3) |  | Shape recovery (%) | Hysteresis (mJ/mm3) |
| PBS/PHDG | 63.37 | 3.40 |  | 56.30 | 5.39 |
| P(BS-HDG)5 | 71.20 | 1.70 |  | 62.95 | 5.88 |

Qualitative memory shape evaluation

Hydrolytic degradation tests

Figure S4: chromatograms of neat PBS/PHDG blend (T0) and partially degraded samples after 2, 4 and 6 months of incubation.

Figure S5: First DSC scan of A) PBS, B) PBS/PHDG and C) P(BS-HDG)5 after 1, 3 and 6 months of incubation in hydrolytic conditions, compared of those of the neat (t0) and blank samples after 1 and 6 months.

Table S4: Thermal characterisation data of the partially hydrolysed PBS, PBS/PHDG, P(BS-HDG)5 samples compared with those of the neat samples (t0) and the corresponding blanks.

|  | Tg (°C) | ΔCp (J/g*°C) | Tm (°C) | ΔHm (J/g) | Tg (°C) | ΔCp (J/g*°C) | Tm (°C) | ΔHm (J/g) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | PBS blank |  |  |  | PBS partially degraded |  |  |  |
| 0m | -32 | 0.135 | 113 | 54 | -32 | 0.135 | 113 | 54 |
| 1m | -32 | 0.175 | 115 | 56 | -30 | 0.192 | 114 | 55 |
| 2m | -30 | 0.163 | 114 | 55 | -30 | 0.184 | 114 | 58 |
| 3m | -32 | 0.230 | 114 | 56 | -32 | 0.241 | 114 | 63 |
| 4m | -30 | 0.203 | 114 | 58 | -31 | 0.188 | 115 | 63 |
| 5m | -30 | 0.073 | 114 | 58 | -31 | 0.178 | 115 | 63 |
| 6m | -30 | 0.163 | 114 | 55 | -32 | 0.157 | 115 | 62 |
|  | PBS/PHDG blank |  |  |  | PBS/PHDG partially degraded |  |  |  |
| 0m | -39 | 0.324 | 38 113 | 3 39 | -39 | 0.324 | 38 113 | 3 39 |
| 1m | -39 | 0.318 | 46 112 | 11 39 | -38 | 0.316 | 40 50 113 | 6.7 1.8 47 |
| 2m | -42 | 0.288 | 45 111 | 15 38 | -39 | 0.389 | 38 48 111 | 6.5 6.3 42 |
| 3m | -43 | 0.174 | 45 111 | 15 42 | -39 | 0.428 | 39 49 112 | 3.6 8.9 48 |
| 4m | -44 | 0.305 | 44 110 | 13 43 | -40 | 0.266 | 48 111 | 12 47 |
| 5m | -44 | 0.141 | 45 110 | 15 43 | -39 | 0.266 | 39 50 113 | 4.8 7.9 47 |
| 6m | -46 | 0.227 | 45 110 | 17 52 | -41 | 0.268 | 50 111 | 11 49 |
|  | P(BS-HDG)5 blank |  |  |  | P(BS-HDG)5 partially degraded |  |  |  |
| 0m | -38 | 0.409 | 42 110 | 3 36 | -38 | 0.409 | 42 110 | 3 36 |
| 1m | -39 | 0.426 | 45 110 | 3.3 43 | -39 | 0.368 | 51 111 | 1.6 47 |
| 2m | -42 | 0.447 | 43 109 | 3.3 42 | -40 | 0.400 | 50 112 | 5.7 49 |
| 3m | -43 | 0.378 | 44 108 | 3.3 46 | -41 | 0.294 | 49 112 | 4.0 51 |
| 4m | -44 | 0.393 | 49 108 | 3.0 45 | -41 | 0.347 | 48 110 | 6.2 53 |
| 5m | -44 | 0.328 | 50 107 | 4.8 45 | -41 | 0.216 | 50 111 | 7.4 51 |
| 6m | -46 | 0.379 | 49 106 | 4.8 49 | -45 | 0.202 | 111 | 72 |