Table S1. This table synthesizes both the physical attributes and the environmental/operational context of the waste dump in Skien as detailed in Hale et al., 2022.

| Parameter | Landfill |
| --- | --- |
| Usage Period | 1975–1993 |
| Depth | 13 m |
| Top Cover Thickness | 0.3-1.5 m (material type and quality unknown; Norwegian Environmental Agency, 2019) |
| Waste Composition | Household waste, waste oil, and a mixture of special waste |
| Leachate Contamination | Similar contamination trends noted, with soil and water samples indicating potential leachate issues due to legacy waste components |
| Hydrological Impact | Situated in farmland/industrial area, contributing to potential leachate mixing with surface runoff |

Table S2.  Full width at half maximum (FWHM) of IR bands of LDPE samples

| Sample | FWHM₇₂₀ | FWHM₁₄₇₅ | FWHM₂₉₀₀ α | FWHM₂₉₀₀ β |
| --- | --- | --- | --- | --- |
| Control | 10 ±2 | 13 ±2 | 19 ±2 | 13 ±2 |
| Exposed to Pn | 12 ±2 | 17 ±2 | 18 ±2 | 12 ±2 |
| Exposed to Re | 12 ±2 | 16 ±2 | 19 ±2 | 13 ±2 |