Supplemental material

Probing the DOS Band Tail in Amorphous Thin-Film Transistors via Capacitance–Voltage Analysis

by Nikolas Franke1, Luca Fabbri1, Lorenzo Margotti1, Jinhui Cho2, Kristofer Paetow2, Yang-Wen Chen2, Agus Widjaja2, Beatrice Fraboni1, Tobias Cramer1

1 Department of Physics and Astronomy, University of Bologna, Viale Berti Pichat 6/2, 40127 Bologna (Italy)

2 InnovaFlex® Foundry, 1635 Aeroplaza Dr, Colorado Springs, CO 80916, USA

Full derivation of MIS junction model with exponential DOS

Figure 1 illustrates the energy level diagram relevant for the MIS junction. The left side depicts the energy levels at the flat band potential, while the right side displays depletion condition. This visualization encompasses all parameters crucial to our model. Our derivation is divided into two parts: first, we delve into the semiconductor's band-bending phenomenon; second, we establish a connection between band bending and experimental observables, namely the gate voltage UG and the total specific capacitance c. The model is derived for a n-type semiconductor, but the same argumentation is valid for a p-type semiconductor.  As a final part, we describe the LinFit and FullFit procedure used to derive the model parameters. Here we include the prove of equivalence of our model to the Mott-Schottky equation under the assumption of depletion condition of the channel.

Semiconductor capacitance with exponential DOS

The degree of band bending in the semiconductor is quantified by the function ϕx, which determines the vacuum level shift in the semiconductor as a function of the distance from the semiconductor-dielectric interface (defined to be at x=0).

In the initial step, we derive the differential equation of ϕx, and its correlation to the semiconductor's DOS. Alterations in the vacuum level are attributed to the accumulation of space charge ρ in the semiconductor, as defined by the Poisson equation:

d2ϕxdx2=-ρxεε0#S1

where ε denotes the specific permittivity of the semiconductor.

The space charge originates from the Fermi-Dirac integral

ρEF= q0ND- q0-∞∞gEfE,EFdE #S2

where gE=N0expEEt represents the exponential density of states of the conduction band tail, fE,EF is the Fermi-Dirac distribution and ND denotes the doping density of oxygen vacancies. For an IGZO semiconductor, the DOS is shown in Figure 2 where the red area corresponds to gE while the green area corresponds to the density of occupied state that is the product of gE*fE,EF. The signs in the derivation are set for a n-doped semiconductor with an exponential tail of the conduction band.

For the case of Et>kBT a solution to the Fermi-Dirac integral can be found in the literature:

DOOS(EF)=N0πkBTsinπkBTEtexpEFEt

Next, we introduce, that in the bulk, far from interfaces, there's no space charge ρEF=0 to obtain

N0=NDsinπkTEtπkTexp-EF,bulkEt#S3

We note that EF,bulk is dependent on temperature and this will lead to a temperature dependence of the flatband voltage. Instead the analytical shape of the local charge density function ρEF is independent of temperature for the condition of Et>kBT. It explicit form is obtained by introducing (S3) into eqn. (1) of the manuscript

ρEF=q0ND1-expEF,bulk-EFxEt#S4

Equation (4) explains how local Fermi level variations relate to the accumulation of space charge in the semiconductor. Finite temperatures are accounted for by a temperature induced shift in the flat band voltage, as seen in Figure 3. These Fermi level variations are directly linked to the vacuum level shift, where the electrostatic potential ϕx is defined as:

ϕx=EF,bulk-EFx#S5

By substituting equations (3) and (4) into (1), we obtain the complete nonlinear Poisson equation containing DOS parameters Et, ND and indirectly N0:

d2ϕxdx2=q0NDεε01-expϕEt#S6

Equation (5) represents a nonlinear, second-order differential equation that cannot be solved analytically so far. However, we can solve some important parts of the differential equation. In particular one can obtain an analytic expression for the first derivative of the potential dϕxdx. It is also important to realize that two boundary conditions are necessary to determine the potential with the differential equation. In our case we will start with a simple scenario in the CV measurements, that is an infinitely thick semiconductor. For such a case we can define boundary conditions

ϕx=∞=0dϕx=∞dx=0#S7

We introduce new variables α=q0NDεε0 and β=q0Et to obtain:

d2ϕdx2=αexpβϕ-1#S8

We can then further simplify βϕ=y and introduce a new variable κ= βα to get

d2ydx2=κ2expy-1#S9

For this differential equation we can do a first integration step

dydx2=2κ2expy-1dy=2κ2expy-y+C1#S10

Now we use the boundary conditions from (7), which allows to determine the integration constant C1=-2κ2. It follows:

dydx=±κ2expy-y-2#S11

A further integration step of this equation to obtain yx is not possible. However, for CV measurements the knowledge of  dydxx is already sufficient. We resubstitute:

dϕdx=±κβ2expβϕ-βϕ-2#S12

From Gauss law on electrostatic charges, we know:

σ=εε0d2ϕdx2dx =-εε0dϕdxx = 0#S13

This effectively removes any screening-induced shift of ϕ, thus justifying our assumption of infinite semiconductor thickness. Figure 4 shows thickness dependent CV measurements in linear and log scale, proving this point.

Therefore, our solution provides the surface charge present in the semiconductor

σ=±εε0αββ2expβϕ0-βϕ0-2#S14

Here ϕ0 denotes the value of the potential ϕ at x=0. This value is also called the surface potential. It is the value of the electrostatic potential at the interface between semiconductor and gate dielectric. In Figure 5a and b the influence of Et and ND on the σ are shown. As seen, by increasing Et, the slope of the surface charge function for accumulation is decreasing while for the depletion region no effect can be seen. Increasing ND on the other side, corresponds to a constant offset of the whole function affecting both the depletion and accumulation regime.

Since we are interested in calculating the capacitance, we need

cs = dσdϕ0 = εε0αβexpβϕ0-12expβϕ0-βϕ0-2#S15

Relation of band bending to experimental parameters

The remaining step is now to correlate the calculated capacitance cs(ϕ0), to the measured capacitance c(UG). Therefore, the transistor consists of the following layers: the electrodes, the dielectric with its oxide capacitance cox and the semiconductor with its capacitance cs. This results in the following equation

c= cscoxcs+cox#S16

So far, our expression describes cs in dependence of ϕ0 but to compare with experimental measurements we need the gate potential UG. The correlation between the two potentials is given by the energy diagram shown in Figure 1. On the left side the flat band condition is displayed while the right side shows the energy diagram in depletion condition for an applied potential UG < UFB. Thereby, UFB is the flat band potential and EF,bulk is the fermi level of the bulk as calculated above.

According to the energy diagram, the applied gate voltage is the serial combination of UFB, the potential drop over the dielectric UOx and the actual surface potential ϕ0. We can write the correlation as

UG=UFB+UOx+ϕ0#S17

Here UOx=σcox is the potential drop across the dielectric determined by cox, the capacitance per unit area of the dielectric. In differential notation this simplifies to

d ϕ0dUG=1-ddUGσcox=1-ccox#S18

Now we can rewrite the differential notation in integral notation

ϕ0=1-cUGcoxdUG +const#S19

The constant is determined so that ϕ0UG-UFB=0. We note that when UG=UFB (flatband condition) then also σ=0 applies.

Procedure to obtain parameters  ND, UFBand Et based on linear fitting (LinFit)

In order to perform the linear fitting procedure (LinFit), we first calculate cs according to equation (S16). To do so, we assume cox to be the mean value of c in accumulation at UG=9V. This assumption is justified as in strong accumulation, cs can be neglected and the measured capacitance is fully dominated by cox.

For the depletion condition we can simplify our derived model to obtain the Mott-Schottky equation and obtain ND and UFB therefrom. Using equation S15 for cs, for depletion region: βϕ0≪0 the equation simplifies to

cs = εε0α2-1-ϕ0-1β#S20

Resubstituting α=q0NDεε0, β=q0Et and taking the square of the capacitance we obtain

1cs2 =  2εε0q0NDϕ0-Etq0#S21

Using equation (S17), the potential is given as ϕ0= UG-UFB-UOx. For UOx, since cOx≫cs we can assume that UOx~0. Reason being that due to the low concentration of charge carriers the tail in the IGZO being long and thus in comparison the potential drop over the oxide can be neglected. Assuming further that Etq0~0, we obtain the Mott-Schottky equation given by

1cs2 =  2εε0q0NDUG-UFB#S22

Remember that finite temperature is accounted for by a shift in flat band potential UFB. Thus, for depletion condition, our model is in accordance with the theory of Mott-Schottky, allowing us to derive the parameters ND and UFB.

The determined parameters ND and UFB are now used to evaluate the missing parameter Et by performing a liner fit of equation (13). We therefore compute σ from the measured capacitance c according to the equation for total accumulated charge

σ(UG)=UFBUGcUdU#S23

We then convert UG into ϕ0 using equation (S17). The fitting of equation (S14) to our data is now performed in the accumulation regime only (ϕ0>0), with the sole parameter evaluated being Et. The remaining parameters are adopted from the Mott-Schottky analysis and remain unchanged.

Procedure to obtain parameters  ND, UFBand Et based on non-linear numerical optimization (FullFit)

In order to perform the non-linear optimization a good initial guess of parameters ND, UFB, Et and cox is needed. To obtain the guess, we first calculate ϕ0 from the measured data using equation (S19). The initial guess for the flatband potential UFB is determined by ϕ0UG-UFB=0.  Starting values for ND, Et and cox are then obtained following the LinFit procedure described above. Then we calculate a first value for cs from equation (S15) and for csim according to equation (S16). Now we calculate the mean absolute error between measured capacitance c and the calculated csim:

err=ici-csim,i2#S24

Using  matlab “fmin” function to minimize the mean absolute error by iterating over the whole process (equations S19, S15 and S16) using ND, UFB, Et and cox as optimization parameters.

Figure 1: Schematic band diagram of the MIS junction in a transistor with IGZO. Depletion condition is shown on the left while flat band condition is shown on the right.

Figure 2: Schematic diagram of the band edge in an IGZO semiconductor. The DOS is shown in red while the DOS with respect to the Fermi Dirac Distribution is shown in green. For this plot EF = EF,bulk was calculated using ND = 1e12 cm-3 and Et = 0.04 eV based on evaluation results and N0 = 1.55e20 cm-3 from literature. A temperature of 300 K was assumed. EC and EV were taken from literature.

Figure 3: Thickness dependence of CV measurements in lin and log scale. No dependence of the measured capacitance on the thickness could be observed.

Figure 4: Surface potential – surface charge plots in dependence of Et (a) and ND (b)