Supplementary Information

Development of novel organic/inorganic osteomimetic inks for 3D bioprinted in vitro bone models

Tiziana Fischettia,1, Gabriela Graziania,2, Giorgia Borciania,3, Matteo Pittonb, Elisa Boaninic, Nicola Baldinia,d, Silvia Farèb,§

T.Fischetti, G.Graziani, G. Borciani, N. Baldini

tiziana.fischetti@ior.it; gabriela.graziani@uniroma5.it; giorgia.borciani@ior.it; nicola.baldini@ior.it

a BST Laboratory, Rizzoli RIT-Research, Innovation & Technology Department, Istituto di Ricerca Codivilla Putti, IRCCS Istituto Ortopedico Rizzoli, via di Barbiano 1/10, 40136, Bologna, Italy

1 present address: Department for Functional Materials in Medicine and Dentistry, Institute of Biofabrication and Functional Materials, University of Würzburg and KeyLab Polymers for Medicine of the Bavarian Polymer Institute (BPI), Pleicherwall 2, D-97070, Würzburg, Germany

2 present address: Department of promotion of Human sciences and quality of life, San Raffaele Rome University, via val di Canutta 247, 00166, Roma, Italy

3 present address: RAMSES Laboratory, Rizzoli RIT-Research, Innovation & Technology Department, Istituto di Ricerca Codivilla Putti, IRCCS Istituto Ortopedico Rizzoli, via di Barbiano 1/10, 40136, Bologna, Italy

M.Pitton, S. Farè,§

matteo.pitton@polimi.it; silvia.fare@polimi.it

b Department of Chemistry, Materials and Chemical Engineering “Giulio Natta”, Politecnico di Milano, Via Mancinelli 7, 20131, Milan, Italy

E.Boanini

elisa.boanini@unibo.it

c Department of Chemistry “Giacomo Ciamician”, University of Bologna, Via Francesco Selmi, 2, 40126, Bologna, Italy

N. Baldini

d Department of Biomedical and Neuromotor Sciences, University of Bologna, via Massarenti 9, 40138, Bologna, Italy

§ Corresponding author: Silvia Farè

Figure SM1. Saos-2 cell metabolic activity under UV lamp exposure at 1d, 2d and 3d (* p ≤ 0.05, *** p ≤ 0.001).

Figure SM2. Viscosity versus shear rate for GelMA 7.5%/0 nHA and loaded with 0.1, 0.2, 0.5 and 1 nHA, measured at 24 °C.

Table SM1. Values of p-index for a) GelMA 7.5%/0, 0.1, 0.2, 0.5, 1 nHA, and b) GelMA 10%/0, 0.1, 0.2, 0.5, 1 nHA, measured at 22 and 24 °C.

a

| p index | T = 22 °C | T = 24 °C |
| --- | --- | --- |
| GelMA 7.5%/0 nHA | 0.29 | 0.90 |
| GelMA 7.5%/0.1 nHA | 0.15 | 0.97 |
| GelMA 7.5%/0.2 nHA | 0.25 | 0.84 |
| GelMA 7.5%/0.5 nHA | 0.10 | 0.35 |
| GelMA 7.5%/1 nHA | 0.16 | 0.73 |

b

| p index | T = 22 °C | T = 24 °C |
| --- | --- | --- |
| GelMA 10%/0 nHA | 0.10 | 0.35 |
| GelMA 10%/0.1 nHA | 0.06 | 0.11 |
| GelMA 10%/0.2 nHA | 0.04 | 0.42 |
| GelMA 10%/0.5 nHA | 0.06 | 0.12 |
| GelMA 10%/1 nHA | 0.08 | 0.22 |

Figure SM3. Viscosity versus shear rate for GelMA 10%/0 nHA and loaded with 0.1, 0.2, 0.5 and 1 nHA, measured at a) 22 °C, and b) 24 °C.

Figure SM4. Inks preliminary biological evaluation: Saos-2 cells viability cultured for 1d in contact with the conditioned medium (CM) derived from the incubation of GelMA w/wo nHA in culture medium for 1d (*** p ≤ 0.001).

Figure SM5. Bioinks preliminary biological evaluation: Saos-2 cells viability embedded in bulk samples of GelMA w/wo nHA at 1d, 3d, 7d and 14d (* p ≤ 0.05, ** p ≤ 0.01, *** p ≤ 0.001).

.