Poly(butylene isophthalate-co-2,5-furandicarboxylate): Toward Sustainable and Moisture-Resistant Monolayer Food Packaging

- Supplementary information -

Matteo Venturi a, Valentina Siracusa b, Elisa Boanini c, Elisabetta Salatelli d, Maurizio Fiorini a, Michelina Soccio a,e,f, Nadia Lotti a,e,g

a Department of Civil, Chemical, Environmental and Materials Engineering, University of Bologna, Via Terracini 28, Bologna, 40131, Italy.

b Department of Chemical Science, University of Catania, Viale A, Doria 6, Catania 95125, Italy

c Department of Chemistry “G. Ciamician”, University of Bologna, Via Gobetti 85, Bologna, 40129, Italy

d Department of Industrial Chemistry “Toso Montanari”, Via Gobetti 85, Bologna, 40129, Italy

e Interdepartmental Center for Industrial Research on Advanced Applications in Mechanical Engineering and Materials Technology, CIRI-MAM, Viale del Risorgimento 2, 40136, Bologna, Italy.

f Interdepartmental Center for Industrial Research on Buildings and Construction CIRI-EC, Via del Lazzaretto 15/5, 40131, Bologna, Italy.

g Interdepartmental Center for Industrial Agro-Food Research, CIRI-AGRO, Via Quinto Bucci 336, 47521, Cesena, Italy.

List of figures

Figure S1. 1H-NMR spectra (400MHz) in CDCl3 of the synthesized polymers.	3

Figure S2. 13C-NMR spectra (400MHz) in CDCl3 of the synthesized polymers.	4

Figure S3. Fitting of glass transition temperature to Fox equation for the different synthesized copolymers revealed by DSC on the as-molded films.	5

Figure S4. Stress strain curves of the compression molded films prepared from the synthesized polymers stretched at a strain rate of 10 mm/min.	6

Figure S5. DSC thermograms (a) and XRD diffraction patterns (b) of semicrystalline and amorphous films employed for the comparison of permeabilities reported in Figure 7 and Table 5.	7

List of tables

Table S1. Thermal data retrieved from the DSC analysis of the polymer films immediately after compression molding.	5

Table S2. Thermal data for the semicrystalline (SC) and amorphous (A) films used for investigating the effect of crystallinity on the GTR reported in Figure 7 and Table 5.	7

Figure S1. 1H-NMR spectra (400MHz) in CDCl3 of the synthesized polymers.

Figure S2. 13C-NMR spectra (400MHz) in CDCl3 of the synthesized polymers.

Table S1. Thermal data retrieved from the DSC analysis of the polymer films immediately after compression molding.

| Sample | Tg (°C) | ∆Cp (°C) | Tcc (°C) | Tm (°C) | ∆Hmneat (J/g) |
| --- | --- | --- | --- | --- | --- |
| PBI | 20.7 | 0.45 | 105.3 | 138.1 | -1.6 |
| P(BI90BF10) | 21.0 | 0.52 |  |  |  |
| P(BI80BF20) | 22.6 | 0.51 |  |  |  |
| P(BI70BF30) | 24.2 | 0.42 |  |  |  |
| P(BI60BF40) | 26.1 | 0.39 |  |  |  |
| P(BI50BF50) | 26.9 | 0.40 |  |  |  |
| P(BI40BF60) | 27.5 | 0.45 |  |  |  |
| P(BI30BF70) | 30.0 | 0.43 |  |  |  |
| P(BI20BF80) | 30.9 | 0.53 |  |  |  |
| P(BI10BF90) | 30.5 | 0.51 | 109.3 | 159.2 | -1.6 |
| PBF | 36.6 | 0.47 | 96.8 | 169.2 | -0.3 |

Figure S3. Fitting of glass transition temperature to Fox equation for the different synthesized copolymers revealed by DSC on the as-molded films.

Figure S4. Stress strain curves of the compression molded films prepared from the synthesized polymers stretched at a strain rate of 10 mm/min.

Figure S5. DSC thermograms (a) and XRD diffraction patterns (b) of semicrystalline and amorphous films employed for the comparison of permeabilities reported in Figure 7 and Table 5.

Table S2. Thermal data for the semicrystalline (SC) and amorphous (A) films used for investigating the effect of crystallinity on the GTR reported in Figure 7 and Table 5.

|  |  | DSC |  |  |  |  |  | XRD |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Tg (°C) | ∆Cp (°C) | Tm (°C) | Tcc (°C) | ∆Hmneat (J/g) | Xc (%) | Xc (%) |
| P(BI30BF70) | A | 28.8 | 0.33 | 132.0 | - | 1.1 | 1 | 0 |
|  | SC | 26.4 | 0.12 | 58.8 129.5 | 67.3 | 28.6 | 22 | 18 |
| P(BI90BF10) | A | 21.3 | 0.36 | 124.1 | 75.4 | 2.4 | 2 | 4 |
|  | SC | 14.6 | 0.06 | 57.8 125.0 | 79.6 | 34.8 | 31 | 30 |