Supplementary Material for

Magnetic properties of Ge, Re and Cr substituted Fe5SiB2

M. Casadeia,b, M.M. Isaha, R. Cabassib, G. Trevisib, S. Fabbricib, M. Bellib, C.De Julián Fernándezb, G. Allodic, V. Fournéed, S. Sannaa,*, F. Albertinib

a Department of Physics, University of Bologna, viale Berti Pichat 6/2, Bologna, Italy

b IMEM-CNR, Via delle Scienze 37, Parma, Italy

c Department of Mathematical, Physical and Computer Science, University of Parma, Parco Area delle Scienze 7/A, Parma, Italy

d Institut Jean Lamour, Campus Artem, 2 allée André Guinier, 54011 Nancy, France

Rietveld refinement results

| Fe5SiB2 Rwp=18.9 | Wyckoff position | x | y | z |
| --- | --- | --- | --- | --- |
| Fe1 | 4c | 0.0 | 0.0 | 0.0 |
| Fe2 | 16l | 0.1689(9) | 0.6688(9) | 0.1367(7) |
| Si | 4a | 0.0 | 0.0 | 0.25 |
| B | 8h | 0.6205(9) | 0.1197(9) | 0.0 |

| Fe5Si0.75Ge0.25B2 Rwp=19.7 | Wyckoff position | x | y | z |
| --- | --- | --- | --- | --- |
| Fe1 | 4c | 0.0 | 0.0 | 0.0 |
| Fe2 | 16l | 0.1697(7) | 0.6697(7) | 0.1391(5) |
| Si | 4a | 0.0 | 0.0 | 0.25 |
| Ge | 4a | 0.0 | 0.0 | 0.25 |
| B | 8h | 0.6197(9) | 0.1197(9) | 0.0 |

| Fe4.75Re0.25SiB2 Rwp= 10.8 | Wyckoff position | x | y | z |
| --- | --- | --- | --- | --- |
| Fe1 | 4c | 0.0 | 0.0 | 0.0 |
| Fe2 | 16l | 0.1688(1) | 0.6688(1) | 0.1386(2) |
| Re1 | 4c | 0.0 | 0.0 | 0.0 |
| Re2 | 16l | 0.1688 | 0.6688 | 0.1386(2) |
| Si | 4a | 0.0 | 0.0 | 0.25 |
| B | 8h | 0.6073(7) | 0.1073(7) | 0.0 |

| Fe4.75Cr0.25SiB2 Rwp=13.1 | Wyckoff position | x | y | z |
| --- | --- | --- | --- | --- |
| Fe1 | 4c | 0.0 | 0.0 | 0.0 |
| Fe2 | 16l | 0.1682(1) | 0.6682(1) | 0.1394(1) |
| Cr1 | 4c | 0.0 | 0.0 | 0.0 |
| Cr2 | 16l | 0.1682(1) | 0.6682(1) | 0.1394(1) |
| Si | 4a | 0.0 | 0.0 | 0.25 |
| B | 8h | 0.6300(8) | 0.1300(8) | 0.0 |

Table S1: Rietveld refinement results.

Fig S1: SPD curves of d2M/dH2 as a function of applied field for Fe5SiB2 and Ge, Re and Cr substituted samples at room temperature. The position of peak corresponds to the anisotropy field of the material.

Fig S2: Low field (100 Oe) magnetization curves for Fe5SiB2 and Ge, Re and Cr substituted samples as a function of temperature. Notice how the undoped and Ge doped samples show peaks at different temperatures, corresponding to the spin reorientation temperature, while Re and Cr doped samples have a monotonous behavior.

Fig S3: c/a ratio and cell volume as a function of elemental substitution.

Fig S4: Frequencies of the Gaussian components needed to fit the spectra at different temperatures for a) undoped, b) Ge doped, c) Re doped and d) Cr doped samples with the maximum content of substituting elements.

Evidence for 11B NMR

Figure S5: a) Zero-field NMR frequency spectrum of 10B (bullets) and 11B stars of undoped Fe5SiB2 at 77 K. b) The two spectra overlaid, with the 11B spectrum unscaled, and frequencies of the 10B spectral points multiplied by γ11/γ10 = 2.986, where γ10, γ11  are the gyromagnetic ratios of the 10B and 11B boron isotopes, respectively. In both panels, the dashed vertical lines mark the 57Fe resonance frequencies predicted from the 57Fe Moessbauer spectra of Wäppling et al. [7].

a)

b)

The experimental proof that the reported MNR signals are due to the 11B resonance is provided by the occurrence of replica spectra for the 10B isotope. As both isotopes experience the same hyperfine field, their resonance frequency are scaled by their gyromagnetic ratio, γ11/2π = 13.66 MHz/T and γ10/2π =  4.5743 MHz/T for 11B and 10B, respectively.

Model for the NMR spectral shape

Here we outline a simple model for the shapes of the 11B NMR spectra. The model assumes an anisotropic hyperfine interaction

ν=Ax2cos2ϕ+Ax2sin2ϕsin2θ+Ax2cos2θ

where θ, φ are the polar angles of the spin relative to the crystal axes, and a random orientation of the spin inside a domain wall, whereby the solid angle is spanned with uniform probability. The spectral weight g(ν) thus coincides with the solid angle portion corresponding to a resonance frequency ν . In the presence of a cylindrical hyperfine tensor (Ax = Ay) the spectral density can be calculated analytically as

gν=1|dνd cosθ|= ν(ν2-Ax2)(Az2-Ax2)

showing a powder singularity at ν = Ax . The latter, however, is smeared out in practice by any source of  inhomogeneity in the hyperfine coupling. In the general case, a numerical integration is needed to calculate g(ν) and a powder singularity does not show up for non degenerate hyperfine tensor components Ax ≠ Ay ≠ Az.

In Fig. S6 we show a fit of the spectrum of the undoped compound well above the spin reorientation (T = 280K) to the model sketched above, where the inhomogeneity of the hyperfine coupling is accounted for by an incoherent Gaussian broadening (i.e. the convolution of the calculated spectrum with a Gaussian distribution). The fit reproduces the skew lineshape of the spectrum with reasonable accuracy, yielding best fit parameters Ax = Ay =29.27(5) MHz, Az  =25.19(2) MHz and Gaussian broadening σ =0.93(3) MHz at this particular temperature in this sample. Fits of similar quality are obtained for the Ge sample above the reorientation transition and for the other samples not showing it.

Figure S6: Zero-field NMR spectrum of the undoped sample at 280K, and its best fit to an isotropic angular spin spin distribution in the presence of an anistropic hyperfine coupling, as discussed in the text.