Supplementary Material

Sustainable Recovery of Rare Earth Elements from Aqueous Media Using Fruit Pomaces: Adsorption Performance, Thermodynamics, and Environmental Assessment

Salvatore Giovanni Michele Raccuia1, Emanuele Zanda1, Clemente Bretti1, Mauro Formica2, Eleonora Macedi2, Andrea Melchior3, Marilena Tolazzi3, Alberto Pettignano4, Nicola Muratore4, Davide Lascari4, Edoardo Teresi 5, Cristian Chiavetta 6, Giovanna De Luca1, Anna Irto1, Concetta De Stefano1, Paola Cardiano1, Gabriele Lando1

1Dipartimento di Scienze Chimiche, Biologiche, Farmaceutiche e Ambientali, Università degli Studi di Messina, 98168, Messina, Italy;

2Dipartimento di Scienze Pure e Applicate, Università degli Studi di Urbino “Carlo Bo”, 61029, Urbino, Italy;

3Dipartimento Politecnico di Ingegneria e Architettura, Laboratorio di Tecnologie Chimiche, Università di Udine, 33100, Udine, Italy;

4Dipartimento di Fisica e Chimica– Emilio Segré, Università di Palermo, I-90128 Palermo, Italy;

5Dipartimento di Ingegneria Civile, Chimica, Ambientale e dei Materiali "DICAM", Università di Bologna, 40121, Bologna, Italy;

6Dipartimento Sostenibilità (SSPT), ENEA, 00123, Roma, Italy.

Tables

Table S1. Numerical values calculated during the screening of the sorption capacity of all the tested BP, GP and OP-based materials towards Nd3+ and Dy3+.

| ID | Adsorbent | qe a Nd3+ | qe a Dy3+ |
| --- | --- | --- | --- |
| A | RAW BP | 0.115 ± 0.006 | 0.076 ± 0.004 |
| B | BP LYO | 0.084 ± 0.004 | 0.038 ± 0.002 |
| C | BP LYO H2O | 0.183 ± 0.009 | 0.189 ± 0.009 |
| D | BP H2O | 0.274 ± 0.014 | 0.270 ± 0.014 |
| E | BP HNO3 | 0.211 ± 0.010 | 0.220 ± 0.011 |
| F | RAW OP | 0.155 ± 0.008 | 0.140 ± 0.007 |
| G | OP H2O | 0.092 ± 0.005 | 0.116 ± 0.006 |
| H | OP HNO3 | 0.071 ± 0.003 | 0.091 ± 0.005 |
| I | RAW GP | 0.098 ± 0.005 | 0.099 ± 0.005 |
| J | GP H2O | 0.130 ± 0.006 | 0.109 ± 0.005 |
| K | GP HNO3 | 0.071 ± 0.004 | 0.114 ± 0.006 |

a in mmol/g ± std. dev.;

Table S2. Parameters of PFO kinetic equation for the adsorption of Nd3+ and Dy3+ from aqueous solutions at pH = 5.0 and t = 25 °C.

| M3+ | Adsorbent | qe a | k1 b | R2 | RMSEc |
| --- | --- | --- | --- | --- | --- |
| Nd3+ | RAW OP | 0.11 ± 0.01 | 1.24 ± 0.25 | 0.9481 | 0.0076 |
|  | GP H2O | 0.07 ± 0.01 | 0.41 ± 0.06 | 0.9576 | 0.0050 |
|  | BP H2O | 0.25 ± 0.01 | 0.07 ± 0.01 | 0.9819 | 0.0118 |
| Dy3+ | RAW OP | 0.12 ± 0.01 | 1.23 ± 0.24 | 0.9567 | 0.0078 |
|  | GP H2O | 0.08 ± 0.01 | 0.28 ± 0.05 | 0.9553 | 0.0063 |
|  | BP H2O | 0.25 ± 0.01 | 0.12 ± 0.01 | 0.9407 | 0.0225 |

a mmol/g ± std. dev; b 1/min ± std. dev; c Root Mean Square Error, mmol/g.

Table S3. Parameters of PGO kinetic equation for the adsorption of Nd3+ and Dy3+ from aqueous solutions at pH = 5.0 and t = 25 °C.

| M3+ | Adsorbent | qe a | kn b | n c | R2 | RMSEd |
| --- | --- | --- | --- | --- | --- | --- |
| Nd3+ | RAW OP | 0.12 ± 0.01 | 1271 ± 3512 | 4 ± 1 | 0.9886 | 0.0036 |
|  | GP H2O | 0.08 ± 0.01 | 0.28 ± 0.05 | 1 ± 1 | 0.9741 | 0.0039 |
|  | BP H2O | 0.29 ± 0.03 | 0.12 ±0.02 | 2 ± 1 | 0.9915 | 0.0079 |
| Dy3+ | RAW OP | 0.23 ± 0.20 | 6·1010±1·1010 | 15 ± 22 | 0.9929 | 0.0032 |
|  | GP H2O | 0.11 ± 0.01 | 625 ± 968 | 4 ± 1 | 0.9987 | 0.0011 |
|  | BP H2O | 0.40 ± 0.11 | 6.00 ± 4.78 | 5 ± 1 | 0.9919 | 0.0083 |

a mmol/g ± std. dev; b [(1/min)(g·mmol)(n-1))]± std. dev; c general order of adsorption; d Root Mean Square Error, mmol/g.

Table S4. Parameters of DEM kinetic equation for the adsorption of Nd3+ and Dy3+ from aqueous solutions at pH = 5.0 and t = 25 °C.

| M3+ | Adsorbent | qe a | α b | kp1 c | kp2 c | R2 | RMSEd |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Nd3+ | RAW OP | 0.12 ± 0.01 | 0.22 ± 0.04 | 0.07 ± 0.01 | 1.94 ± 0.35 | 0.9912 | 0.0031 |
|  | GP H2O | 0.07 ± 0.01 | 0.20 ± 0.14 | 0.05 ± 0.07 | 0.60 ± 0.20 | 0.9658 | 0.0045 |
|  | BP H2O | 0.26 ± 0.08 | 0.82 ± 0.06 | 0.05 ± 0.01 | 430 ± 1 | 0.9807 | 0.0094 |
| Dy3+ | RAW OP | 0.13 ± 0.01 | 0.19 ± 0.02 | 0.03 ± 0.01 | 1.66 ± 0.20 | 0.9928 | 0.0032 |
|  | GP H2O | 0.09 ± 0.01 | 0.44 ± 0.02 | 0.02 ± 0.01 | 0.94 ± 0.13 | 0.9997 | 0.0011 |
|  | BP H2O | 0.27 ± 0.11 | 0.65 ± 0.03 | 0.05 ± 0.01 | 0.74 ± 0.13 | 0.9987 | 0.0083 |

a mmol/g ± std. dev; b (0 < α < 1); c 1/min ± std. dev; d Root Mean Square Error, mmol/g.

Table S5. Parameters of the Boyd’s model for the systems under analysis.

| Adsorbent | Metal | Slope (min⁻¹) | Intercept | R² |
| --- | --- | --- | --- | --- |
| OP RAW | Dy3+ | 0.012±0.002 | 0.885±0.08 | 0.8556 |
| OP RAW | Nd3+ | 0.002±0.001 | 0.389±0.04 | 0.3912 |
| GP H2O | Dy3+ | 0.003±0.001 | 0.176±0.03 | 0.7467 |
| GP H2O | Nd3+ | 0.009±0.003 | 0.108±0.02 | 0.3968 |
| BP H2O | Dy3+ | 0.005±0.001 | 0.153±0.051 | 0.6156 |
| BP H2O | Nd3+ | 0.007±0.001 | 0.132±0.06 | 0.7882 |
| BP H2O | La3+ | 0.010±0.001 | 0.187±0.09 | 0.7894 |

± std. dev

Table S6. Freundlich isotherm parameters for the Nd3+, Dy3+ and La3+ ions from aqueous solutions adsorption onto RAW OP, GP H2O and BP H2O at t = 25°C, pHi = 3.0 to 5.0, low ionic strength (absence of ionic medium) and in NaNO3 0.10 mol/dm3.

| M3+ | Adsorbent | pHia | pHeb | KFc | n | R2 | RMSEd |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Nd3+ | RAW OP | 5.0 | 4.1 | 0.22 ± 0.02 | 5.1 ± 0.9 | 0.9625 | 0.0107 |
|  | GP H2O | 5.0 | 4.0 | 0.22 ± 0.02 | 2.5 ± 0.3 | 0.9763 | 0.0062 |
|  | BP H2O | 5.0 | 3.4 | 0.53 ± 0.05 | 3.2 ± 0.5 | 0.9523 | 0.0249 |
|  | BP H2O | 5.0 e | 3.6 | 0.32 ± 0.02 | 2.2 ± 0.2 | 0.9749 | 0.0075 |
| La3+ | BP H2O | 5.0 | 3.6 | 0.49 ± 0.05 | 3.5 ± 0.5 | 0.9441 | 0.0279 |
|  | BP H2O | 5.0 e | 3.4 | 0.27 ± 0.03 | 3.4 ± 0.8 | 0.9384 | 0.0167 |
| Dy3+ | RAW OP | 5.0 | 4.1 | 0.21 ± 0.02 | 4.7 ± 0.8 | 0.9641 | 0.0084 |
|  | GP H2O | 5.0 | 4.0 | 0.26 ± 0.04 | 2.3 ± 0.4 | 0.9217 | 0.0108 |
|  | BP H2O | 5.0 | 3.2 | 0.59 ± 0.05 | 2.4 ± 0.3 | 0.9668 | 0.0216 |
|  | BP H2O | 5.0 e | 3.4 | 0.23 ± 0.03 | 3.1 ± 0.8 | 0.9215 | 0.0159 |
| Nd3+ | BP H2O | 4.0 | 3.3 | 0.41 ± 0.05 | 5 ± 1 | 0.9293 | 0.0223 |
| Dy3+ | BP H2O | 4.0 | 3.6 | 0.36 ± 0.05 | 6 ± 1 | 0.8766 | 0.0296 |
| Nd3+ | BP H2O | 3.0 | 2.9 | 0.27 ± 0.02 | 9 ± 3 | 0.9948 | 0.0065 |
| Dy3+ | BP H2O | 3.0 | 2.9 | 0.21 ± 0.01 | 13 ± 2 | 0.9884 | 0.0068 |

a initial pH value of REE ions solutions; b mean pH value at adsorption equilibrium; c mmol/g (dm3/mmol)1/n ± std. dev.; d Root Mean Square Error; e adsorption isotherm carried out in NaNO3 0.10 mol/dm3.

Table S7. TEA of producing 1 kg of Bergamot Pomace H2O

| Material and cost input | B1 | S1 | S2 | S3 | Unit |
| --- | --- | --- | --- | --- | --- |
| Bergamot pomace H2O | 4.16 | 4.16 | 1.04 | 1.04 | kg |
| Drying electricity consumptiona | 11.96 | 1.40 | 2.99 | 0.35 | kWh |
| Grinding electricity consumption a | 0.023 | 0.023 | 0.006 | 0.006 | kWh |
| Centrifuge electricity consumption a | 0.14 | 0.14 | 0.04 | 0.04 | kWh |
| Deionized water b | 166.66 | 166.66 | 41.67 | 41.67 | dm3 |
| Nitric acid (0.1 mol/dm3) (for regeneration) c | - | - | 0.75 | 0.75 | dm3 |
| Material and cost output |  |  |  |  |  |
| €/kg of BP H2O | 13.64 | 10.47 | 3.79 | 2.99 |  |
| €/kg Ln | 194.80 | 149.54 | 54.10 | 42.74 |  |

a Electricity cost was based on €0.30/kWh, the average supply costs to non-domestic customers, low voltage (Arera, relazione annuale 2023-2024); b deionized water cost: laboratory inventory, €60 for 1000 dm3 filter, 0.06 €/dm3; c nitric acid cost: Merck.com, €100 for 1 dm3 of 10 mol/dm3 nitric acid solution, €0.5/0.1 mol/dm3.

Figures

Figure S1. Flow diagram of the system boundaries and life cycle stages across the four scenarios considered.

| a) GP H2O | b) RAW OP |
| --- | --- |

Figure S2. ATR FT-IR spectra of: a) GP H2O (black line) [1], GP H2O + Nd3+ (red line), GP H2O + Dy3+ (blue line); b) RAW OP (black line) [1], RAW OP + Nd3+ (red line), RAW OP + Dy3+ (blue line).

| a) |  |  |
| --- | --- | --- |
| b) |  |  |
| c) |  |  |

Figure S3. SEM images of a) OP RAW before adsorption experiments and after adsorption of b) Nd, c) Dy. On the right the elemental analysis.

| a) |  |
| --- | --- |
| b) |  |
| c) |  |

Figure S4. SEM images of a) GP H2O before adsorption experiments and after adsorption of b) Nd, c) Dy. On the right is the elemental analysis.

| a) Nd3+ | b) Dy3+ |
| --- | --- |

Figure S5. PFO kinetics of adsorption of Nd3+ (a) and Dy3+ (b) ions on BP H2O (△), RAW OP (□), and GP H2O (○) adsorbents at low ionic strength and t = 25°C.

| a) | b) |
| --- | --- |

Figure S6. PGO kinetics of adsorption of Nd3+ (a) and Dy3+ (b) ions on BP H2O (△), RAW OP (□), and GP H2O (○) adsorbents at low ionic strength and t = 25°C.

| a) | b) |
| --- | --- |

Figure S7. DEM kinetics of adsorption of Nd3+ (a) and Dy3+ (b) ions on BP H2O (△), RAW OP (□), and GP H2O (○) adsorbents at low ionic strength and t = 25°C.

Figure S8. PSO kinetics of adsorption of La3+ on BP H2O (Δ) at low ionic strength and t = 25°C.

| Dy | Nd |
| --- | --- |
| La |  |

Figure S9. Bt vs. t scatter plots for Dy (upper left), Nd (upper right), and La (lower left) and fitting with the Boyd’s kinetics model (straight lines) at low ionic strength and t = 25°C.

Figure S10. Adsorption isotherms of Dy3+ onto BP H2O in aqueous solutions, at t = 25°C, pH = 5.0, 0.10 mol/dm³ in NaNO3 (○) and without ionic medium (△). The experimental data were processed using the Langmuir (solid line) and Freundlich (dotted line) models.

Figure S11. Adsorption isotherms of Nd3+ onto BP H2O in aqueous solutions, at t = 25°C, pH = 5.0, 0.10 mol/dm³ in NaNO3 (○) and without ionic medium (△). The experimental data were processed using the Langmuir (solid line) and Freundlich (dotted line) models.

Figure S12. Adsorption isotherms of La3+ onto BP H2O in aqueous solutions, at t = 25°C, pH = 5.0, 0.10 mol/dm³ in NaNO3 (○) and without ionic medium (△). The experimental data were processed using the Langmuir (solid line) and Freundlich (dotted line) models.

The results obtained, in terms of qe of adsorption and desorption for the four cycles, are depicted in the histograms reported in Figures S13 (a-f).

RAW OP (Figures S13a and S13b) exhibited qₑ values of 0.1509 mmol/g for Nd³⁺ and 0.1224 mmol/g for Dy³⁺ in the first cycle, but capacities dropped by more than half after the first regeneration. A similar trend was observed for qdes, which progressively decreased over the cycles, indicating a reduced desorption capacity. GP H₂O (Figures S12c and S12d) started at 0.1125 mmol/g (Nd³⁺) and 0.1029 mmol/g (Dy³⁺) and showed a gradual decline in both qₑ and qdes across the cycles. BP H₂O (Figures S13e and S13f) maintained significantly higher and more stable capacities, with qₑ decreasing only from 0.3194 to 0.2586 mmol/g for Nd³⁺ and from 0.3086 to 0.2697 mmol/g for Dy³⁺. In this case, qdes consistently matched qₑ in all cycles, showing no loss of desorption capacity over time.

| a) Nd3+, RAW OP | b) Dy3+, RAW OP |
| --- | --- |
| c) Nd3+, GP H2O | d) Dy3+, GP H2O |
| e) Nd3+, BP H2O | f) Dy3+, BP H2O |

Figure S13. qe values determined by using the different biomass samples for various REEs adsorption/desorption steps.

References

[1] S.G.M. Raccuia, E. Zanda, C. Bretti, M. Formica, E. Macedi, A. Melchior, M. Tolazzi, M. Sanadar, D. Lascari, G. De Luca, A. Irto, C. De Stefano, P. Cardiano, G. Lando, Molecules, 29 (2024) 5735.