Supplementary Information for

Enhanced Efficiency in Hollow Core Electrospun Nanofiber-Based Organic Solar Cells

Mohammad Ali Haghighat Bayan 1,2, Faramarz Afshar Taromi 2, Massimiliano Lanzi 3 and Filippo Pierini *1

- Department of Biosystems and Soft Matter, Institute of Fundamental Technological Research, Polish Academy of Sciences, Warsaw 02-106, Poland

2. Department of Polymer Engineering, Amirkabir University of Technology, Tehran 15875-4414, Iran

3. Department of Industrial Chemistry“Toso Montanari”, Alma Mater Studiorum – University of Bologna, Bologna 40136, Italy

Corresponding Author: *Email:fpierini@ippt.pan.pl

Supplementary Figures and Tables

Figure S1. FT-IR spectra of PANI and ANI to show the polymerization.

Table S1. Surface resistance and conductivity of Sulfonated PANI, PANI, and Hollow PANI

| Sample | Conductivity (S/cm) | Resistance (Ohm/sq) |
| --- | --- | --- |
| Sulfonated PANI | 19.70 3.45 | 2.05*104359 |
| PANI | 24.35 1.39 | 1.41*10480.48 |
| Hollow PANI | 47.95 0.79 | 5.84*10396.21 |

Figure S2. Change in conductivity of samples.

Figure S3. Tauc plot, derivated from UV-Vis data to estimate the optical Eg of PANI and Hollow PANI.

Table S2. Optical ban gaps for PANI and Hollow PANI.

| Sample | Band gap (eV) | Maximum absorption (nm) |
| --- | --- | --- |
| PANI | 3.45 | 260 |
| Hollow PANI | 2.60 | 219 |

Table S3. Photovoltaic characteristics of the examined solar cells (average values collected from five devices)

| Sample | Jsc (mA cm-2) | Voc (V) | FF | PCE (%) |
| --- | --- | --- | --- | --- |
| PEDOT:PSS | 11.97±1.2 | 0.70±0.01 | 0.52±0.05 | 4.35±0.08 |
| Sulfonated PANI | 14.82±1.4 | 0.49±0.01 | 0.50±0.07 | 3.63±0.07 |
| Hollow PANI | 14.18±1.3 | 0.71±0.01 | 0.68±0.06 | 6.85±0.11 |