Supplementary Material

Cobalt Recovery from Lithium Cobalt Oxide Cathode Scraps via Green Solvents: Process Development and Life Cycle Assessment

Shoayb Mojtahedia,b,‡, Leonardo Sparascioc,‡, Federico Mascettia, Salan Xierzatia, Andrea Vitalea, Simone D’Agostinoa, Chiara Samorìa, Alessandro Girolamo Rombolàa, Nicholas Greggioa, Daniele Cespic,d*, Fabrizio Passarinic,d, Chiara Zentilec, Antunes Staffolania,b, Ncholu Manyalae , Francesca Soavia,b

a Department of Chemistry “Giacomo Ciamician”, Alma Mater Studiorum University of Bologna, Via Gobetti 85, 40129 Bologna (BO), Italy.

b ENERCube lab, Centro Ricerche Energia, Ambiente e Mare, Centro Interdipartimentale per la Ricerca Industriale Fonti Rinnovabili, Ambiente, Mare ed Energia (CIRI-FRAME) – Alma Mater Studiorum University of Bologna, Viale Ciro Menotti, 48, 48122 Marina di Ravenna, Italy.

c Department of Industrial Chemistry “Toso Montanari, Via Gobetti 85, 40129 Bologna (BO), Italy.

d Interdepartmental Centre for Industrial Research – Renewable Resources, Environment, Sea and Energy, University of Bologna, Via D. Campana 71, 47923, Rimini, Italy.

e Department of Physics, University of Pretoria, Pretoria, South Africa

‡ Both authors contributed equally

Corresponding Author

Daniele Cespi, daniele.cespi2@unibo.it

Figure S1 illustrates the visual evolution observed during cobalt recovery from the DES leachate upon gradual addition of a 5 M KOH solution. Progressive pH increase induced distinct color changes in the solution and precipitate, culminating in the formation of a brown cobalt-containing solid at pH 12, which was subsequently collected and dried.

Figure S1. Cobalt recovery using 5M potassium hydroxide solution, showing transition from dark green to purple (pH=1), purple (pH=9), and finally brown as pH increases to 12 and cobalt precipitates. After the first drops of KOH the colour of the DES solution starts changing to pinkish. A pink precipitated is formed at a pH of approximately 1. As the pH raises to 9, the precipitate turns to purple and, when the pH reached 12, a brown powder was formed. T The brown precipitate was collected and dried at 80 °C overnight.

Figure S2 presents the process flow diagram for the separation of black mass from shredded lithium cobalt oxide (LCO) cathode scraps using triethyl phosphate (TEP), followed by a deep eutectic solvent (DES)–based hydrometallurgical route for cobalt recovery. The scheme outlines the main unit operations, including mechanical pre-treatment, TEP-assisted separation, DES leaching, solid–liquid separation, and downstream cobalt recovery steps, which define the system boundaries adopted in the life cycle assessment.

Figure S2. Flowchart of the cobalt recovery process from shredded LCO cathode.

Tables S2 to S16 report the LCI activities for the units involved in the recycling process, as well as for the chemicals for which it was not possible to find available datasets on software libraries.

Note that, to achieve the main functional unit selected for the study, all flows were linearly scaled to match 1 g of cobalt hydroxide powder as the system output.

Table S2: LCI related to black mass separation with TEP (Step 1)

| Process | Quantity | Unit | Notes |
| --- | --- | --- | --- |
| Input |  |  |  |
| Materials/fuels |  |  |  |
| LCO cathode | 1 | g | burden-free |
| Triethyl phosphate (made in China), Cut-off, U | 12.7 | g |  |
| Electricity/heat |  |  |  |
| Electricity, medium voltage {IT}¦ market for ¦ Cut-off, U | 0.025 | kWh | Electricity used for separating the black mass (heating plate) |
| Electricity, medium voltage {IT}¦ market for ¦ Cut-off, U | 0.0000103 | kWh | Electricity used for drying aluminium (oven) |
| Output |  |  |  |
| Product |  |  |  |
| Suspension (from black mass separation) | 12 | g |  |
| Waste to treatment |  |  |  |
| Hazardous waste, for incineration {Europe without Switzerland}¦ market for hazardous waste, for incineration ¦ Cut-off, U | 1.39 | g | Losses recorded during lab operations |
| Aluminium (waste treatment) {GLO}¦ recycling of aluminium ¦ Cut-off, U | 0.165 | g | Aluminium recovered from the black mass |
| Emissions to air |  |  |  |
| Triethyl phosphate | 0.146 | g | Sub compartment: low-population. Assumption that all material losses derive from TEP evaporation |

Table S3: LCI related to suspension centrifugation (Step 2)

| Process | Quantity | Unit | Notes |
| --- | --- | --- | --- |
| Input |  |  |  |
| Materials/fuels |  |  |  |
| Suspension (from black mass separation) | 12 | g | input from the previous step |
| Electricity/heat |  |  |  |
| Electricity, medium voltage {IT}¦ market for ¦ Cut-off, U | 0.00752 | kWh | Electricity used for centrifugation |
| Output |  |  |  |
| Product |  |  |  |
| Black powder and residual TEP (from centrifugation) | 1.28 | g | Value estimated by difference. No losses were assumed. |
| Waste to treatment |  |  |  |
| Hazardous waste, for incineration {Europe without Switzerland}¦ market for hazardous waste, for incineration ¦ Cut-off, U | 10.8 | g | Solution of TEP, carbon & binder |

Table S4: LCI related to washing of the black mass and centrifugation (Step 3)

| Process | Quantity | Unit | Notes |
| --- | --- | --- | --- |
| Input |  |  |  |
| Materials/fuels |  |  |  |
| Black powder and residual TEP (from centrifugation) | 1.28 | g | Input from previous step |
| Water, ultrapure {RER}¦ water production, ultrapure ¦ Cut-off, U | 35.6 | g |  |
| Electricity/heat |  |  |  |
| Electricity, medium voltage {IT}¦ market for ¦ Cut-off, U | 0.023 | kWh | Electricity used for centrifugation |
| Output |  |  |  |
| Product |  |  |  |
| Black powder and residual water (from washing and centrifugation) | 1.73 | g |  |
| Waste to treatment |  |  |  |
| Hazardous waste, for incineration {Europe without Switzerland}¦ market for hazardous waste, for incineration ¦ Cut-off, U | 35.2 | g | water and remaining TEP |

Table S5: LCI related to black powder drying (Step 4)

| Process | Quantity | Unit | Notes |
| --- | --- | --- | --- |
| Input |  |  |  |
| Materials/fuels |  |  |  |
| Black powder and residual water (from washing and centrifugation) | 1.73 | g | Input from previous step |
| Electricity/heat |  |  |  |
| Electricity, medium voltage {IT}¦ market for ¦ Cut-off, U | 5.45E-05 | kWh | Electricity used for centrifugation |
| Output |  |  |  |
| Product |  |  |  |
| Black powder (from drying) | 0.767 | g |  |
| Emission to air |  |  |  |
| Water | 0.961 | g | Sub compartment: low population |

Table S6: LCI related to Deep Eutectic Solvent preparation (Step 5)

| Process | Quantity | Unit | Notes |
| --- | --- | --- | --- |
| Input |  |  |  |
| Materials/fuels |  |  |  |
| Oxalic acid {GLO}¦ market for oxalic acid ¦ Cut-off, U | 12.1 | g | Input from previous step |
| _Choline chloride (from reaction yield 100%), Cut-off, U, CN | 18.6 | g | Dataset adapted from Zaib et al. |
| Electricity/heat |  |  |  |
| Electricity, medium voltage {IT}¦ market for ¦ Cut-off, U | 0.0219 | kWh |  |
| Output |  |  |  |
| Product |  |  |  |
| DES (from DES preparation) | 30.7 | g |  |

Table S7: LCI related to dissolution of the black mass in the Deep Eutectic Solvent (Step 6)

| Process | Quantity | Unit | Notes |
| --- | --- | --- | --- |
| Input |  |  |  |
| Materials/fuels |  |  |  |
| Black powder (from drying) | 0.767 | g | input from the previous step |
| DES (from DES preparation) | 30.7 | g | input from the previous step |
| Electricity/heat |  |  |  |
| Electricity, medium voltage {IT}¦ market for ¦ Cut-off, U | 0.587 | kWh |  |
| Output |  |  |  |
| Product |  |  |  |
| Dark green suspension (from dissolution in DES) | 29.8 | g |  |
| Waste to treatment |  |  |  |
| Hazardous waste, for incineration {Europe without Switzerland}¦ market for hazardous waste, for incineration ¦ Cut-off, U | 1.6 | g | Material losses during lab operations, calculated as difference |

Table S8: LCI related to centrifugation for separation of the viscous liquid (Step 7)

| Process | Quantity | Unit | Notes |
| --- | --- | --- | --- |
| Input |  |  |  |
| Materials/fuels |  |  |  |
| Dark green suspension (from dissolution in DES) | 29.8 | g | input from the previous step |
| Electricity/heat |  |  |  |
| Electricity, medium voltage {IT}¦ market for ¦ Cut-off, U | 0.0146 | kWh | Electricity used for centrifugation |
| Output |  |  |  |
| Product |  |  |  |
| Dark green viscous liquid (from centrifugation) | 27.2 | g |  |
| Waste to treatment |  |  |  |
| Hazardous waste, for incineration {Europe without Switzerland}¦ market for hazardous waste, for incineration ¦ Cut-off, U | 2.48 | g | Solid residue |
| Hazardous waste, for incineration {Europe without Switzerland}¦ market for hazardous waste, for incineration ¦ Cut-off, U | 6.91E-04 | g | Losses during lab procedure, calculated as difference |

Table S9: LCI related to preparation of the KOH solution (Step 8)

| Process | Quantity | Unit | Notes |
| --- | --- | --- | --- |
| Input |  |  |  |
| Materials/fuels |  |  |  |
| Potassium hydroxide {GLO}¦ market for potassium hydroxide ¦ Cut-off, U | 14.8 | g |  |
| Water, ultrapure {RER}¦ water production, ultrapure ¦ Cut-off, U | 52.8 | g |  |
| Electricity/heat |  |  |  |
| Electricity, medium voltage {IT}¦ market for ¦ Cut-off, U | 7.92E-03 | kWh | Electricity used for stirring and heating |
| Output |  |  |  |
| Product |  |  |  |
| KOH solution 5M (from KOH solution preparation) | 67.6 | g |  |

Table S10: LCI related to pH adjustment of viscous liquid with KOH (Step 9)

| Process | Quantity | Unit | Notes |
| --- | --- | --- | --- |
| Input |  |  |  |
| Materials/fuels |  |  |  |
| KOH solution 5M (from KOH solution preparation) | 67.6 | g | Input from previous step |
| Dark green viscous liquid (from centrifugation) | 27.2 | g | Input from previous step |
| Electricity/heat |  |  |  |
| Electricity, medium voltage {IT}¦ market for ¦ Cut-off, U | 0.211 | kWh | Electricity used for stirring and heating |
| Output |  |  |  |
| Product |  |  |  |
| Suspension (from pH adjustment) | 94.8 | g |  |

Table S11: LCI related to centrifugation for separation of the precipitate (Step 10)

| Process | Quantity | Unit | Notes |
| --- | --- | --- | --- |
| Input |  |  |  |
| Materials/fuels |  |  |  |
| Suspension (from pH adjustment) | 94.8 | g | Input from previous step |
| Water, ultrapure {RER}¦ water production, ultrapure ¦ Cut-off, U | 0.158 | g |  |
| Electricity/heat |  |  |  |
| Electricity, medium voltage {IT}¦ market for ¦ Cut-off, U | 0.1 | kWh | Electricity used for centrifugation |
| Output |  |  |  |
| Product |  |  |  |
| Precipitate and residual solution (from centrifugation) | 31.3 | g |  |
| Waste to treatment |  |  |  |
| Hazardous waste, for incineration {Europe without Switzerland}¦ market for hazardous waste, for incineration ¦ Cut-off, U | 63.6 | g | Solution containing lithium. Not yet recovered |

Table S12: LCI related to precipitate washing (Step 11)

| Process | Quantity | Unit | Notes |
| --- | --- | --- | --- |
| Input |  |  |  |
| Materials/fuels |  |  |  |
| Precipitate and residual solution (from centrifugation) | 31.3 | g | Input from previous step |
| Water, ultrapure {RER}¦ water production, ultrapure ¦ Cut-off, U | 422 | g |  |
| Electricity/heat |  |  |  |
| Electricity, medium voltage {IT}¦ market for ¦ Cut-off, U | 0.127 | kWh | Electricity used for heating |
| Output |  |  |  |
| Product |  |  |  |
| Precipitate and residual water (from washing) | 454 | g |  |

Table S13: LCI related to centrifugation to remove potassium oxalate (Step 12)

| Process | Quantity | Unit | Notes |
| --- | --- | --- | --- |
| Input |  |  |  |
| Materials/fuels |  |  |  |
| Precipitate and residual water (from washing) | 454 | g | Input from previous step |
| Electricity/heat |  |  |  |
| Electricity, medium voltage {IT}¦ market for ¦ Cut-off, U | 0.401 | kWh | Electricity used for centrifugation |
| Output |  |  |  |
| Product |  |  |  |
| Solid and residual water (from centrifugation) | 5.36 | g |  |
| Waste to treatment |  |  |  |
| Wastewater, average {Europe without Switzerland}¦ market for wastewater, average ¦ Cut-off, U | 448 | cm3 | Water containing potassium oxalate |

Table S14: LCI related to brown powder drying (Step 13)

| Process | Quantity | Unit | Notes |
| --- | --- | --- | --- |
| Input |  |  |  |
| Materials/fuels |  |  |  |
| Solid and residual water (from centrifugation) | 5.36 | g | Input from previous step |
| Water, ultrapure {RER}¦ water production, ultrapure ¦ Cut-off, U | 13.2 | g |  |
| Electricity/heat |  |  |  |
| Electricity, medium voltage {IT}¦ market for ¦ Cut-off, U | 8.45E-04 | kWh | Electricity used for heating (oven) |
| Output |  |  |  |
| Product |  |  |  |
| Cobalt hydroxide | 0.459 | g |  |
| Emissions to air |  |  |  |
| Water | 18.1 | g | Sub compartment: low-population. |

Table S15: LCI related to the production of choline chloride

| Process | Quantity | Unit | Notes |
| --- | --- | --- | --- |
| Input |  |  |  |
| Materials/fuels |  |  |  |
| Hydrochloric acid, without water, in 30% solution state {RoW}¦ market for hydrochloric acid, without water, in 30% solution state ¦ Cut-off, U | 0.6812 | kg |  |
| Trimethylamine {RoW}¦ market for trimethylamine ¦ Cut-off, U | 0.4233 | kg |  |
| Water, deionized {RoW}¦ water production, deionised ¦ Cut-off, U | 0.9878 | kg |  |
| Ethylene oxide {RoW}¦ market for ethylene oxide ¦ Cut-off, U | 0.3155 | kg |  |
| Transport, freight, lorry, >32 metric ton, diesel, EURO 4 {RER}¦ market for transport, freight, lorry, >32 metric ton, diesel, EURO 4 ¦ Cut-off, U | 1000 | kgkm |  |
| Transport, freight, sea, container ship, heavy fuel oil {GLO}¦ transport, freight, sea, container ship, heavy fuel oil ¦ Cut-off, U | 15800 | kgkm |  |
| Electricity/heat |  |  |  |
| Electricity, high voltage {CN}¦ market group for electricity, high voltage ¦ Cut-off, U | 129600 | J | Mixer |
| Electricity, high voltage {CN}¦ market group for electricity, high voltage ¦ Cut-off, U | 2.931 | MJ | Reactor |
| Heat, from steam, in chemical industry {RoW}¦ steam production, as energy carrier, in chemical industry ¦ Cut-off, U | 16.569 | MJ | Evaporator |
| Output |  |  |  |
| Product |  |  |  |
| Choline chloride (from reaction yield 100%), Cut-off, U, CN | 1 | kg |  |
| Emission to air |  |  |  |
| Water | 1.465 | kg |  |
| Heat, waste | 3.31 | kJ |  |

Table S16: LCI related to the production of triethyl phosphate

| Process | Quantity | Unit | Notes |
| --- | --- | --- | --- |
| Input |  |  |  |
| Resources |  |  |  |
| Water, cooling, unspecified natural origin, CN | 0.031 | m3 |  |
| Materials/fuels |  |  |  |
| Ammonia, anhydrous, liquid {CN}¦ market for ammonia, anhydrous, liquid ¦ Cut-off, U | 0.32 | kg |  |
| Chemical factory, organics {RoW}¦ chemical factory construction, organics ¦ Cut-off, U | 4E-10 | p |  |
| Ethanol, without water, in 99.7% solution state, from ethylene {RoW}¦ ethanol production, ethylene hydration ¦ Cut-off, U | 0.87 | kg |  |
| Oxygen, liquid {RoW}¦ market for oxygen, liquid ¦ Cut-off, U | 0.093 | kg |  |
| Phosphorous chloride {RoW}¦ phosphorous chloride production ¦ Cut-off, U | 0.8 | kg |  |
| Steam, in chemical industry {RoW}¦ market for steam, in chemical industry ¦ Cut-off, U | 1.8 | kg |  |
| Transport, freight, lorry, >32 metric ton, diesel, EURO 4 {RER}¦ market for transport, freight, lorry, >32 metric ton, diesel, EURO 4 ¦ Cut-off, U | 1000 | kgkm |  |
| Transport, freight, sea, container ship, heavy fuel oil {GLO}¦ transport, freight, sea, container ship, heavy fuel oil ¦ Cut-off, U | 15800 | kgkm |  |
| Electricity/heat |  |  |  |
| Electricity, medium voltage {CN}¦ market group for electricity, medium voltage ¦ Cut-off, U | 0.92 | kWh |  |
| Output |  |  |  |
| Product |  |  |  |
| Triethyl phosphate (made in China), Cut-off, U | 1 | kg |  |
| Ammonium chloride [co-product of Triethylphosphate production CN] | 0.93 | kg | Co-product |
| Waste to treatment |  |  |  |
| Spent solvent mixture {RoW}¦ market for spent solvent mixture ¦ Cut-off, U | 0.16 | kg |  |
| Wastewater, average {RoW}¦ market for wastewater, average ¦ Cut-off, U | 0.031 | m3 |  |

Table S 17: LCI related to production of oxalic acid via CO coupling method. This dataset was adapted from IDEA database and used for sensitivity analysis

| Process | Quantity | Unit | Notes |
| --- | --- | --- | --- |
| Input |  |  |  |
| Resources |  |  |  |
| Resources, building site, land use, land occupation | 0.0017648 | m2a |  |
| Resources, forest to building site, land use, land transformation | 3.53E-05 | m2 |  |
| Materials/fuels |  |  |  |
| Chemical factory, organics {RoW}¦ chemical factory construction, organics ¦ Cut-off, U | 1.059E-09 | p | This piece of data was obtained by calculating the sum (in m2) of three inputs of the IDEA dataset, referring to the construction of the factory, and by transforming m2 in p (10500 m2 : 1 p) |
| Nitric acid, without water, in 50% solution state {RoW}¦ market for nitric acid, without water, in 50% solution state ¦ Cut-off, U | 0.0042 | kg | Amount of pure nitric acid (100%) |
| Water, deionised {RoW}¦ market for water, deionised ¦ Cut-off, U | 0.0000857 | kg | Water contained in HNO3 solution |
| Oxygen, liquid {RoW}¦ market for oxygen, liquid ¦ Cut-off, U | 90.79 | g | Values reported in the original IDEA dataset are in Nm3, so they were converted in unit of mass |
| Hydrogen, gaseous, low pressure {RoW}¦ market for hydrogen, gaseous, low pressure ¦ Cut-off, U | 2.085 | g | Values reported in the original IDEA dataset are in Nm3, so they were converted in unit of mass |
| Carbon monoxide {RoW}¦ market for carbon monoxide ¦ Cut-off, U | 369.98 | g | Values reported in the original IDEA dataset are in Nm3, so they were converted in unit of mass |
| N-butanol {GLO}¦ market for n-butanol ¦ Cut-off, U | 0.842 | kg |  |
| Tap water {RoW}¦ tap water production, underground water with chemical treatment ¦ Cut-off, U | 0.00455 | ton | Both water supply and its treatment are included (in the original IDEA dataset inputs are separated) |
| Water, deionised {RoW}¦ market for water, deionised ¦ Cut-off, U | 0.178 | kg | Stoichiometric amount of water used to hydrolyze dibutyl oxalate |
| Electricity/heat |  |  |  |
| Steam, in chemical industry {RoW}¦ market for steam, in chemical industry ¦ Cut-off, U | 1.26 | kg |  |
| Electricity, high voltage {JP}¦ market for electricity, high voltage ¦ Cut-off, U | 0.227 | kWh |  |
| Output |  |  |  |
| Product |  |  |  |
| Oxalic acid | 0.445 | kg | dataset adapted from IDEA database |
| Avoided Products |  |  |  |
| N-butanol {GLO}¦ market for n-butanol ¦ Cut-off, U | 0.8 | kg | We assume that 95% of butanol is recovered after hydrolysis of dibutyl oxalate (percentage was chosen following methodology of Hischier et al.) |
| Emissions to air |  |  |  |
| Emissions, nitrous oxide, air, unspecified | 0.00307 | kg | Sub compartment: low-population. Calculated by assuming that all nitric acid is oxidized to nitrous oxide |
| Emissions, carbon dioxide (fossil), air, unspecified | 0.246 | kg | Sub compartment: low-population. Calculated by assuming that carbon contained in input material and not contained in the final product is emitted as carbon dioxide |

Figure S3 reports the contribution analysis of the main process phases and the sensitivity analysis performed on Phase 6 (dissolution of the black mass in the DES). The baseline scenario uses the Italian electricity mix from ecoinvent 3, while the alternative scenario is based on IEA 2023 data assuming a 20% increase in renewable energy sources. The modified electricity mix results in a 37.7% reduction in the total environmental impact of Phase 6, with reductions in global warming, fine particulate matter formation, and fossil resource scarcity, accompanied by increases in selected impact categories (e.g., terrestrial ecotoxicity).

Figure S3. Comparison between the baseline scenario (Italian energy mix from ecoinvent 3) and the renewable scenario (Italian energy mix based on IEA 2023 data with a 20% increase in renewable sources) for step 6.

Table S17: LCIA results presented at the Midpoint-level results (Recipe2016, H), for 1 g of recovered cobalt hydroxide

| Impact Category | Unit | Step 1 | Step 2 | Step 3 | Step 4 | Step 5 | Step 6 | Step 7 | Step 8 | Step 9 | Step 10 | Step 11 | Step 12 | Step 13 | Total |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| GW | kg CO2 eq | 2.66E-01 | 6.39E-02 | 2.07E-01 | 4.50E-05 | 7.62E-01 | 4.93E-01 | 2.53E-02 | 1.55E-01 | 1.74E-01 | 4.23E-01 | 1.07E-01 | 3.31E-01 | 7.70E-04 | 3.01E+00 |
| SOD | kg CFC11 eq | 6.61E-08 | 1.41E-08 | 4.57E-08 | 2.02E-11 | 3.66E-06 | 2.19E-07 | 8.02E-09 | 5.00E-08 | 7.83E-08 | 1.04E-07 | 4.98E-08 | 1.50E-07 | 3.97E-10 | 4.45E-06 |
| IR | kBq Co-60 eq | 1.57E-02 | 2.18E-03 | 7.04E-03 | 6.02E-06 | 1.65E-02 | 6.51E-02 | 1.92E-03 | 1.31E-02 | 2.33E-02 | 1.90E-02 | 1.52E-02 | 4.44E-02 | 1.30E-04 | 2.24E-01 |
| OFHH | kg NOx eq | 6.34E-04 | 5.05E-05 | 1.63E-04 | 6.93E-08 | 1.14E-02 | 7.53E-04 | 2.80E-05 | 3.97E-04 | 2.68E-04 | 3.69E-04 | 1.66E-04 | 5.11E-04 | 1.20E-06 | 1.47E-02 |
| FPMF | kg PM2.5 eq | 3.90E-04 | 2.22E-05 | 7.16E-05 | 3.79E-08 | 2.42E-03 | 4.11E-04 | 1.41E-05 | 2.98E-04 | 1.47E-04 | 1.69E-04 | 9.14E-05 | 2.79E-04 | 6.83E-07 | 4.32E-03 |
| OFTE | kg NOx eq | 6.67E-04 | 5.42E-05 | 1.75E-04 | 7.42E-08 | 1.15E-02 | 8.06E-04 | 3.00E-05 | 4.09E-04 | 2.87E-04 | 3.95E-04 | 1.77E-04 | 5.47E-04 | 1.28E-06 | 1.50E-02 |
| TA | kg SO2 eq | 8.11E-04 | 5.74E-05 | 1.85E-04 | 9.69E-08 | 7.29E-03 | 1.05E-03 | 3.61E-05 | 5.48E-04 | 3.75E-04 | 4.37E-04 | 2.33E-04 | 7.14E-04 | 1.73E-06 | 1.17E-02 |
| FE | kg P eq | 1.18E-04 | 1.99E-05 | 6.81E-05 | 1.07E-08 | 2.09E-04 | 1.18E-04 | 7.10E-06 | 9.14E-05 | 4.15E-05 | 1.28E-04 | 6.80E-05 | 8.12E-05 | 1.51E-06 | 9.52E-04 |
| ME | kg N eq | 9.23E-06 | 1.17E-06 | 4.27E-06 | 8.68E-10 | 4.18E-05 | 9.51E-06 | 4.73E-07 | 6.45E-06 | 3.36E-06 | 7.75E-06 | 7.90E-06 | 1.09E-05 | 1.97E-07 | 1.03E-04 |
| TE | kg 1,4-DCB | 4.71E-01 | 5.16E-02 | 1.68E-01 | 2.86E-05 | 1.31E+00 | 3.15E-01 | 1.86E-02 | 4.20E-01 | 1.11E-01 | 3.33E-01 | 6.99E-02 | 2.12E-01 | 5.45E-04 | 3.48E+00 |
| FET | kg 1,4-DCB | 9.16E-03 | 1.35E-03 | 4.39E-03 | 1.17E-06 | 2.45E-02 | 1.28E-02 | 5.87E-04 | 9.86E-03 | 4.53E-03 | 9.16E-03 | 2.85E-03 | 8.66E-03 | 2.21E-05 | 8.78E-02 |
| MET | kg 1,4-DCB | 1.22E-02 | 1.82E-03 | 5.92E-03 | 1.51E-06 | 3.25E-02 | 1.65E-02 | 7.76E-04 | 1.29E-02 | 5.86E-03 | 1.23E-02 | 3.69E-03 | 1.12E-02 | 2.88E-05 | 1.16E-01 |
| HCT | kg 1,4-DCB | 3.84E-02 | 1.09E-02 | 3.54E-02 | 3.97E-06 | 8.35E-02 | 4.42E-02 | 3.43E-03 | 3.41E-02 | 1.54E-02 | 6.81E-02 | 1.09E-02 | 2.94E-02 | 1.13E-04 | 3.74E-01 |
| HNCT | kg 1,4-DCB | 2.53E-01 | 3.30E-02 | 1.07E-01 | 2.27E-05 | 6.87E-01 | 2.49E-01 | 1.30E-02 | 2.46E-01 | 8.80E-02 | 2.18E-01 | 5.61E-02 | 1.71E-01 | 4.51E-04 | 2.12E+00 |
| LU | m2a crop eq | 9.14E-03 | 4.98E-04 | 1.60E-03 | 1.08E-06 | 1.17E-02 | 1.16E-02 | 3.69E-04 | 4.75E-03 | 4.17E-03 | 4.03E-03 | 2.58E-03 | 7.93E-03 | 1.89E-05 | 5.85E-02 |
| MRS | kg Cu eq | 3.93E-03 | 6.00E-05 | 1.95E-04 | 6.17E-08 | 1.45E-03 | 6.72E-04 | 2.83E-05 | 6.01E-04 | 2.39E-04 | 4.16E-04 | 1.53E-04 | 4.57E-04 | 1.26E-06 | 8.20E-03 |
| FRS | kg oil eq | 8.24E-02 | 8.04E-03 | 2.59E-02 | 1.51E-05 | 2.13E-01 | 1.63E-01 | 5.41E-03 | 4.16E-02 | 5.83E-02 | 6.28E-02 | 3.57E-02 | 1.11E-01 | 2.52E-04 | 8.07E-01 |
| WC | m3 | 2.04E-03 | 1.75E-04 | 6.38E-04 | 6.06E-07 | 4.18E-03 | 6.54E-03 | 1.83E-04 | 1.43E-03 | 2.35E-03 | 1.65E-03 | 2.43E-03 | 3.49E-03 | 4.12E-05 | 2.51E-02 |

GW=Global warming, SOD=Stratospheric ozone depletion, IR=Ionizing radiation, OFHH =Ozone formation, Human health, FPMF=Fine particulate matter formation, OFTE=Ozone formation, Terrestrial ecosystems, TA=Terrestrial acidification, FA=Freshwater eutrophication, ME=Marine eutrophication, HCT=Human carcinogenic toxicity, HNCT=Human non-carcinogenic toxicity, LU=Land use, MRS=Mineral resource scarcity, FRS=Fossil resource scarcity, WC=Water consumption.

Table S18: LCIA results presented at the Endpoint-level results (Recipe2016, H), for 1 g of recovered cobalt hydroxide

| Damage category | Human health | Ecosystems | Resources |
| --- | --- | --- | --- |
| Unit | DALY | species. yr | USD2013 |
| Step 1 | 6.80E-07 | 1.18E-09 | 2.37E-02 |
| Step 2 | 1.17E-07 | 2.19E-10 | 3.03E-03 |
| Step 3 | 3.81E-07 | 7.13E-10 | 9.74E-03 |
| Step 4 | 8.50E-11 | 1.77E-13 | 4.85E-06 |
| Step 5 | 2.68E-06 | 5.47E-09 | 6.04E-02 |
| Step 6 | 9.32E-07 | 1.93E-09 | 5.26E-02 |
| Step 7 | 4.70E-08 | 9.21E-11 | 1.84E-03 |
| Step 8 | 5.03E-07 | 7.32E-10 | 1.00E-02 |
| Step 9 | 3.29E-07 | 6.85E-10 | 1.88E-02 |
| Step 10 | 7.77E-07 | 1.47E-09 | 2.28E-02 |
| Step 11 | 2.12E-07 | 4.69E-10 | 1.14E-02 |
| Step 12 | 6.26E-07 | 1.29E-09 | 3.57E-02 |
| Step 13 | 1.74E-09 | 4.51E-12 | 7.92E-05 |
| Total | 7.29E-06 | 1.43E-08 | 2.50E-01 |

DALY=Disability Adjusted Life Years; USD=United States Dollars

Figure S4: Heat maps of the process: on the left the original (base scenario) and on the right the scenario without the allocations related to the energy consumed by the oven in steps 1, 4, and 13 (alternative scenario). The two maps should be interpreted separately.

Table S18: Results of the Monte Carlo uncertainty analysis for the entire process at the midpoint level

| Impact category | Unit | Mean | Median | SD | CV | 2.5% | 97.5% | SEM |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Fine particulate matter formation | kg PM2.5 eq | 0.00432 | 0.00431 | 0.00024 | 5.57 % | 0.0039 | 0.00479 | 0.000024 |
| Fossil resource scarcity | kg oil eq | 0.819 | 0.81 | 0.0803 | 9.8 % | 0.682 | 1.04 | 0.00803 |
| Freshwater ecotoxicity | kg 1,4-DCB | 0.0879 | 0.0837 | 0.0349 | 39.7 % | 0.0113 | 0.192 | 0.00349 |
| Freshwater eutrophication | kg P eq | 0.000983 | 0.000915 | 0.000343 | 34.9 % | 0.000493 | 0.00185 | 3.43E-05 |
| Global warming | kg CO2 eq | 3.01 | 2.99 | 0.172 | 5.71 % | 2.64 | 3.47 | 0.0172 |
| Human carcinogenic toxicity | kg 1,4-DCB | 0.359 | 0.343 | 0.124 | 34.5 % | 0.181 | 0.757 | 0.0124 |
| Human non-carcinogenic toxicity | kg 1,4-DCB | 5.29 | 3.54 | 17.4 | 329 % | -25.3 | 43.4 | 1.74 |
| Ionizing radiation | kBq Co-60 eq | 0.181 | 0.107 | 0.222 | 123 % | 0.0286 | 0.82 | 0.0222 |
| Land use | m2a crop eq | 0.057 | 0.0548 | 0.0151 | 26.4 % | 0.0241 | 0.0867 | 0.00151 |
| Marine ecotoxicity | kg 1,4-DCB | 0.116 | 0.111 | 0.0444 | 38.3 % | 0.0206 | 0.244 | 0.00444 |
| Marine eutrophication | kg N eq | 0.000104 | 0.000102 | 1.47E-05 | 14.2 % | 7.58E-05 | 0.000141 | 1.47E-06 |
| Mineral resource scarcity | kg Cu eq | 0.00834 | 0.00782 | 0.00227 | 27.2 % | 0.00499 | 0.0141 | 0.000227 |
| Ozone formation, Human health | kg NOx eq | 0.0147 | 0.0145 | 0.00167 | 11.4 % | 0.0118 | 0.0188 | 0.000167 |
| Ozone formation, Terrestrial ecosystems | kg NOx eq | 0.015 | 0.0148 | 0.00169 | 11.3 % | 0.012 | 0.0191 | 0.000169 |
| Stratospheric ozone depletion | kg CFC11 eq | 4.56E-06 | 4.46E-06 | 7.32E-07 | 16 % | 3.26E-06 | 6.14E-06 | 7.32E-08 |
| Terrestrial acidification | kg SO2 eq | 0.0117 | 0.0116 | 0.000679 | 5.8 % | 0.0106 | 0.0132 | 6.79E-05 |
| Terrestrial ecotoxicity | kg 1,4-DCB | 3.52 | 3.4 | 0.634 | 18 % | 2.5 | 5.26 | 0.0634 |
| Water consumption | m3 | -0.351 | -0.00917 | 4.87 | -1.39E3 % | -13.8 | 6.48 | 0.487 |

Table S19: Comparison of the results of three impact categories within the ReCiPe 2016 and Environmental Footprint 3.1 impact assessment methods.

| ReCiPe 2016 | EF 3.1 | Unit | Variation (%) |
| --- | --- | --- | --- |
| Global warming | Climate change | kg CO2 eq | 1.94 |
| 1.38 | 1.35 |  |  |
| Water consumption | Water use | m3 | 189 |
| 0.0115 | 0.424 |  |  |
| Fossil resource scarcity | Resource use, fossils | MJ | 11.8 |
| 15.5 | 17.5 |  |  |

Table S20: Variation of the impacts (expressed as a percentage) compared to the baseline scenario, by modifying efficiency recovery values for TEP and number of reuses for DES.

|  | GW | SOD | IR | OFHH | FPMF | OFTE | TA | FE | ME | TE | FET | MET | HCT | HNCT | LU | MR | FRS | WC |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | kg CO2 eq | kg CFC11 eq | kBq Co-60 eq | kg NOx eq | kg PM2.5 eq | kg NOx eq | kg SO2 eq | kg P eq | kg N eq | kg 1,4-DCB | kg 1,4-DCB | kg 1,4-DCB | kg 1,4-DCB | kg 1,4-DCB | m2a crop eq | kg Cu eq | kg oil eq | m3 |
| Scenario: 0% recycled TEP, DES reused 1 time | -7.1% | -15.8% | -1.9% | -14.7% | -10.6% | -14.6% | -11.6% | -6.1% | -9.5% | -9.2% | -7.0% | -7.1% | -9.2% | -7.7% | -4.5% | -4.3% | -5.9% | -4.1% |
| 0% recycled TEP, DES reused 2 times | -9.7% | -22.1% | -2.6% | -20.5% | -14.7% | -20.4% | -16.2% | -8.3% | -12.8% | -12.6% | -9.6% | -9.7% | -12.4% | -10.6% | -6.2% | -5.9% | -8.1% | -5.6% |
| 0% recycled TEP, DES reused 3 times | -11.0% | -25.3% | -2.9% | -23.5% | -16.8% | -23.2% | -18.5% | -9.5% | -14.4% | -14.3% | -10.9% | -11.0% | -14.0% | -12.0% | -7.0% | -6.7% | -9.2% | -6.4% |
| 0% recycled TEP, DES reused 4 times | -11.8% | -27.2% | -3.1% | -25.2% | -18.0% | -25.0% | -19.9% | -10.1% | -15.4% | -15.3% | -11.6% | -11.8% | -15.0% | -12.9% | -7.5% | -7.2% | -9.8% | -6.9% |
| Scenario: 30% recycled TEP, DES reused 1 time | -6.3% | -15.3% | 0.9% | -14.5% | -10.3% | -14.4% | -11.2% | -6.0% | -9.4% | -10.0% | -6.6% | -6.8% | -9.8% | -7.8% | -4.1% | -10.0% | -4.7% | -2.2% |
| 30% recycled TEP, DES reused 2 times | -8.9% | -21.7% | 0.2% | -20.4% | -14.5% | -20.2% | -15.7% | -8.2% | -12.6% | -13.3% | -9.2% | -9.4% | -13.0% | -10.7% | -5.8% | -11.6% | -6.8% | -3.8% |
| 30% recycled TEP, DES reused 3 times | -10.2% | -24.8% | -0.1% | -23.3% | -16.5% | -23.1% | -18.0% | -9.3% | -14.2% | -15.0% | -10.5% | -10.7% | -14.6% | -12.1% | -6.6% | -12.4% | -7.9% | -4.5% |
| 30% recycled TEP, DES reused 4 times | -11.0% | -26.7% | -0.3% | -25.1% | -17.8% | -24.8% | -19.4% | -10.0% | -15.2% | -16.0% | -11.3% | -11.5% | -15.6% | -13.0% | -7.1% | -12.9% | -8.6% | -5.0% |
| Scenario: 50% recycled TEP, DES reused 1 time | -7.1% | -15.4% | 0.4% | -14.9% | -11.0% | -14.8% | -11.6% | -7.0% | -10.1% | -11.0% | -7.5% | -7.6% | -10.8% | -8.8% | -5.3% | -13.8% | -5.4% | -2.9% |
| 50% recycled TEP, DES reused 2 times | -9.6% | -21.8% | -0.3% | -20.7% | -15.1% | -20.5% | -16.2% | -9.2% | -13.3% | -14.4% | -10.1% | -10.2% | -14.0% | -11.7% | -6.9% | -15.3% | -7.6% | -4.4% |
| 50% recycled TEP, DES reused 3 times | -10.9% | -24.9% | -0.6% | -23.7% | -17.2% | -23.4% | -18.5% | -10.3% | -14.9% | -16.0% | -11.4% | -11.5% | -15.6% | -13.1% | -7.8% | -16.1% | -8.7% | -5.2% |
| 50% recycled TEP, DES reused 4 times | -11.7% | -26.8% | -0.8% | -25.4% | -18.4% | -25.2% | -19.9% | -11.0% | -15.9% | -17.0% | -12.1% | -12.3% | -16.6% | -13.9% | -8.3% | -16.6% | -9.3% | -5.6% |
| Scenario: 70% recycled TEP, DES reused 1 time | -7.8% | -15.6% | -0.1% | -15.2% | -11.6% | -15.1% | -12.1% | -8.0% | -10.8% | -12.1% | -8.3% | -8.5% | -11.8% | -9.7% | -6.4% | -17.5% | -6.2% | -3.5% |
| 70% recycled TEP, DES reused 2 times | -10.4% | -21.9% | -0.8% | -21.1% | -15.8% | -20.9% | -16.7% | -10.2% | -14.0% | -15.4% | -10.9% | -11.1% | -15.0% | -12.6% | -8.1% | -19.1% | -8.3% | -5.1% |
| 70% recycled TEP, DES reused 3 times | -11.7% | -25.1% | -1.1% | -24.0% | -17.8% | -23.8% | -19.0% | -11.3% | -15.6% | -17.1% | -12.2% | -12.4% | -16.6% | -14.0% | -8.9% | -19.9% | -9.4% | -5.8% |
| 70% recycled TEP, DES reused 4 times | -12.5% | -26.9% | -1.3% | -25.7% | -19.1% | -25.5% | -20.4% | -12.0% | -16.6% | -18.1% | -13.0% | -13.2% | -17.6% | -14.9% | -9.4% | -20.3% | -10.1% | -6.3% |
| Scenario: 90% recycled TEP, DES reused 1 time | -8.6% | -15.7% | -0.6% | -15.5% | -12.3% | -15.4% | -12.6% | -9.0% | -11.5% | -13.2% | -9.2% | -9.3% | -12.8% | -10.7% | -7.6% | -21.2% | -6.9% | -4.2% |
| 90% recycled TEP, DES reused 2 times | -11.1% | -22.0% | -1.2% | -21.4% | -16.4% | -21.2% | -17.2% | -11.2% | -14.7% | -16.5% | -11.8% | -11.9% | -16.0% | -13.6% | -9.2% | -22.8% | -9.1% | -5.7% |
| 90% recycled TEP, DES reused 3 times | -12.4% | -25.2% | -1.6% | -24.3% | -18.5% | -24.1% | -19.5% | -12.3% | -16.3% | -18.2% | -13.0% | -13.2% | -17.6% | -15.0% | -10.1% | -23.6% | -10.2% | -6.5% |
| 90% recycled TEP, DES reused 4 times | -13.2% | -27.1% | -1.8% | -26.1% | -19.7% | -25.9% | -20.8% | -12.9% | -17.3% | -19.2% | -13.8% | -14.0% | -18.6% | -15.9% | -10.6% | -24.0% | -10.8% | -6.9% |
| Scenario: 30% recycled TEP, DES reused 0 times | 0.8% | 0.4% | 2.8% | 0.1% | 0.2% | 0.2% | 0.5% | 0.1% | 0.2% | -0.7% | 0.4% | 0.3% | -0.6% | -0.1% | 0.4% | -5.7% | 1.3% | 1.9% |
| 50% recycled TEP, DES reused 0 times | 0.1% | 0.3% | 2.3% | -0.2% | -0.4% | -0.2% | 0.0% | -0.9% | -0.5% | -1.8% | -0.5% | -0.5% | -1.6% | -1.0% | -0.7% | -9.5% | 0.5% | 1.2% |
| 70% recycled TEP, DES reused 0 times | -0.7% | 0.2% | 1.8% | -0.5% | -1.0% | -0.5% | -0.5% | -1.9% | -1.3% | -2.9% | -1.3% | -1.4% | -2.6% | -2.0% | -1.9% | -13.2% | -0.2% | 0.6% |
| 90% recycled TEP, DES reused 0 times | -1.4% | 0.1% | 1.3% | -0.8% | -1.7% | -0.9% | -1.0% | -2.8% | -2.0% | -3.9% | -2.2% | -2.2% | -3.6% | -2.9% | -3.0% | -16.9% | -1.0% | -0.1% |