SUPPLEMENTARY INFORMATION

NANOFILTRATION EFFICIENCY

IN THE PURIFICATION OF LACTOSE

FROM ULTRAFILTERED ACID WHEY

Riccardo Onesti(1,a) and Marco Roselli (1,a), Cristiana Boi(1,2), Serena Bandini(1,*)

(1)	Department of Civil, Chemical, Environmental and Materials Engineering - DICAM

Alma Mater Studiorum - University of Bologna-Via Terracini, 28, I-40131, Bologna, Italy

(2)	Department of Chemical and Biomolecular Engineering - North Carolina State University- Raleigh, USA

(*) corresponding author

e-mail: serena.bandini@unibo.it

tel: +39 051 2090231

(a) both authors contributed equally

S1. Transmembrane flux and pressure regulation mode

The entire experimental campaign was carried out with the aim of operating at average constant fluxes across the membrane.

Figure S1 shows the behavior of TMP and the corresponding permeate fluxes, as a function of VCF and VDF during the NF and DF steps, respectively.

Specifically, in the NF step, the increasing lactose concentration with VCF and the subsequent rise in osmotic pressure caused a rapid flux reduction (symbols and black continuous lines). To ensure operation at constant average fluxes, the pressure was increased stepwise (dashed red lines). A typical sawtooth pattern was obtained for each case. The arithmetic mean was assumed to be the “nominal average flux value”.

During the DF experiments, average fluxes were ensured simply by constant values of TMP because the lactose concentration was rather constant.

Figure S1.	Permeate flux (continuous lines) and evolution of the TMP (dashed lines). Details of the operating conditions of trials A, B, C are reported in Table 1 of the main text.

S2. Fouling tests

Fouling tests were conducted in total recirculation mode, where both permeate and retentate streams were continuously recirculated to the feed tank. This ensured that the system operated at constant volume and concentration. Operating conditions: temperature=50 °C, pH=4.0, feed flow rate = 600 L/h.

Figure S2 shows the evolution of the volume flux relative to the initial value (J/Jv,0) and the lactose and lactic acid rejection rates over time. Solutions labelled “A” and “B” correspond to trials A and B, respectively, as detailed in Table 1 of the main text. Solution “Cconcentrated”, corresponds to the feed solution used in trial C (Table 1), previously concentrated at VCF=2.3. The filtration tests were prolonged for 400 minutes while operating at a constant TMP, which was adjusted to yield an initial permeate flux of 11 L/(m2h).

Apparently, no appreciable fouling was observed at low concentrations (A and B) over 4-hour operating period, as demonstrated by the nearly constant flux measured. Similarly, solutes rejection remained stable throughout, with average values of 99.5±0.2% for lactose and 21.2±1.8% for lactic acid.

In contrast, the use of the concentrated solution (Cconcentrated) led to a slight gradual decline, indicating mild fouling: the flux steadily declined by 3.2% after 3 hours and 8.2% after 6 hours. Nevertheless, the separation performance remained unaffected; lactose and lactic acid rejection values remained nearly constant over time, with average values of 99.3±0.03% and 23.0±2.45%, respectively.

After the experiments, a simple rinsing step with warm water was sufficient to fully restore the initial hydraulic permeability of the modules.

Notably, during DF, despite the lactose concentration (99–105 g/L) remaining consistently much higher than in the “Concentrated” solution (67 g/L), a slight increase in transmembrane flux with VDF was instead observed, as a result of the reduction in total solute concentration. These results, together with the absence of performance loss of both the modules throughout the entire experimental campaign, suggest that fouling has a negligible effect during individual purification runs and that it can be prevented by properly planning appropriate cleaning cycles for long-term operations. For a limited number of runs, cleaning cycles may consist of recirculating hot demineralized water only, while in the longer-term washing cycles with suitable detergents should be scheduled to prevent biofouling.

Figure S2.	Fouling tests: permeate flux and rejections with time.

Solutions A and B at TMP=4.3 bar; solution Cconcentrated at TMP=7.3 bar.

S3. Instantaneous rejections

Throughout the experimental campaign, samples of the feed side stream (FS) and instantaneous permeate (PS) (see Figure 2) were collected and analyzed to determine lactose and lactic acid concentrations and to calculate their rejection. For each trial, sampling times correspond to the points indicated in Figure S1. Instantaneous rejections of lactose and lactic acid, calculated using Equation (12) (Table2), are shown in Figures S3 and S4, respectively.

For lactose (Figure S3), both the absolute values and the observed trend were consistent with literature data (Roselli et al., 2024; Chandrapala et al., 2017; Talebi et al., 2020; Nielsen et al., 2021) was observed. Rejection was consistently above 98% in both NF (Figure S3a) and DF (Figure 3) steps, increasing with flux showing negligible dependence on lactose concentration in the feed.

In contrast, lactic acid rejection (Figure S4) showed a significant dependence on both flux and solute concentration. During NF (Figure S4a), where the average flux was maintained constant but the instantaneous flux varied (Figure S1), a clear increase in rejection with flux was observed. In addition, at constant flux, a significant variation in rejection could be attributed to different lactic acid concentrations. These values are in excellent agreement with those previously observed in (Roselli et al., 2024), where all experiments were performed with artificial solutions. The influence of lactic acid concentration on rejection became even more evident during the DF step, where instantaneous flux varied only slightly and could be considered constant, thereby excluding its effect on solute rejection. Under these conditions, at each flux a clear increase in lactic acid rejection was observed as the feed concentration decreased. A detailed explanation of the rationale behind these phenomena is provided in the main text, Section 4.1.

Figure S3.  Instantaneous lactose rejection: a) NF step; b) DF step.

Figure S4.  Instantaneous lactic acid rejection: a) NF step; b) DF step.

S4. Photographic documentation

Figure S5 provides photographic documentation of the effectiveness of the NF+DF process for the trial A solution (see Table 1 of the main text). The NF step was performed at VCF=3.52, while the DF was prolonged up to VDF=1.91. The yellow color of the solution is attributed to riboflavin (376.4 g/mol), a vitamin that is naturally present in milk whey at very low concentrations (0.80-4.80 mg/L) and is completely retained by the DK membrane. The greater color intensity in streams RNF and RDF indicates the concentration of stream F. The permeate PTOT, obtained by mixing the permeates from each step, was clear and with a pungent smell, due to the presence of lactic acid.

Figure S5. Pictures of samples of the corresponding solutions

S5. Scale-up methodology

The experimental data obtained with the lab module (DK1812) were scaled-up to simulate the performance of industrial spiral wound modules.

The DK400 module (37.2 m2 nominal membrane area, 40 inches long, 4 inches diameter, 34 mil feed spacer, manufactured by Veolia Water Technologies & Solutions) was selected for this purpose. To maintain hydrodynamic conditions equivalent to those in the DK1812 module, the module was assumed to operate at a recirculation rate of 17.6 m3/h. Under these conditions, the pressure drops were assumed as =1 bar/module, to account for friction losses along the flow channels and entrance/exit effects. This value is broadly consistent with estimations from [1] and corroborated by practical experience [2].

The scale-up strategy is based on the criterion that a single housing, comprising DK400 modules in series, should operate under the same average flux () as maintained in the DK1812 module and achieve the same VCF values. This condition can be ensured by maintaining the same values of the effective driving force across the housing as those existing in the lab module, namely the same experimental values of TMP and osmotic pressure.

From the experimental data, the trend of the osmotic pressure difference, , as a function of the experimental VCF, was calculated according to Eq. (S1):

(S1)

where the values of flux and  , at the corresponding VCF, are taken from Figure S1, assuming the validity of the solution-diffusion model with an hydraulic permeability of  =9.65 L/(m2 h bar).

The results are displayed in Figure S6.

Figure S6.	Osmotic pressure differences calculated from the experimental results in the NF step. Operating conditions of trials A, B, C are reported in Table 1 of the main text.

As can be observed, the data are consistent with the operating conditions. Indeed,  increases with increasing flux (from trial A to C), due to enhanced concentration polarization. This effect increases the solute concentration at the feed/membrane interface resulting in a higher osmotic pressure difference.

The maximum number of modules per housing is then determined by setting the condition that the last module in series operates at an average TMP sufficient to sustain an acceptable permeate flux under the highest experimentally observed VCF condition.

Referring to the scheme of a housing shown in Figure S7, the following calculations were performed.

Figure S7. Scheme of spiral wound modules arrangement in a housing.

The permeate flux in the Nm-th module at the final VCF () can be estimated by reapplying the solution-diffusion model (Eq. S2), using the corresponding values of  as a function of VCF obtained from Figure S4:

(S2)

where  is the average TMP in the final module of the housing, calculated based on the interrelationships among ,  and , as reported in Eqs (S3).

(S3)

The number of modules  is deemed accepted only if the calculated value is not less than 40-50% of the nominal average flux of the housing.

References

[1]	Shock G., Miquel A., Mass transfer and pressure loss in spiral wound modules, Desalination 64 (1987) 339

[2]	Wagner J., Membrane Filtration Handbook-Practical Tips and Hints, Osmonics, 2001