Recycling Polyamide 6 Fishing Nets and Carbon Fibers for the Development

of Novel Sustainable Composites: Properties and LCA Process Analysis

Francesco Pasciucco 1, Damiano Rossi 2,*, Emanuele Maccaferri 3,

Isabella Pecorini 1, Loris Giorgini 3, Maurizia Seggiani 2

1 Department of Engineering for Energy, Systems, Territory and Constructions (DESTEC), University of Pisa, Via Carlo Francesco Gabba 22, 56122, Pisa, Italy

2 Department of Civil and Industrial Engineering (DICI), Università di Pisa, Largo Lucio Lazzarino 1, 56122 Pisa, Italy

3 Department of Industrial Chemistry "Toso Montanari", Viale del Risorgimento 4, Bologna, 40136, Italy

* Corresponding author: damiano.rossi@unipi.it

Supplementary material

Tab. S1 - Main technical specifications of electric forklift.

| Parameter | Unit | Value | Reference |
| --- | --- | --- | --- |
| Maximum speed | km/h | 15 | * |
| Maximum load | kg | 3,500 | * |
| Maximum lifting height | m | 4.8 | * |
| Battery charging time | h | 2.7 | * |
| Battery life | h | 4 | * |
| Capacity | Ah | 250 | * |
| Voltage | V | 80 | * |

*data provided by commercial producer.

Tab. S2 - Main technical specifications of diesel-powered crane.

| Parameter | Unit | Value | Reference |
| --- | --- | --- | --- |
| Maximum load | ton | 2.82 | * |
| Maximum lifting height | m | 8.7 | * |
| Maximum working radius | m | 8.205 | * |
| Power | kW | 6.57 | * |
| Fuel tank capacity | L | 12 | * |

*data provided by commercial producer.

Tab. S3 - Main technical specifications of conveyor belt.

| Parameter | Unit | Value | Reference |
| --- | --- | --- | --- |
| Belt length | mm | 6,500 | * |
| Belt width | mm | 560 | * |
| Maximum height | mm | 3,150 | * |
| Power | kW | 2 | * |
| Maximum capacity | ton/h | 1 | * |

*data provided by commercial producer.

Tab. S4 - Main technical specifications of industrial shredder for recycling applications.

| Parameter | Unit |  | Value |  | Reference |  |
| --- | --- | --- | --- | --- | --- | --- |
| Feeding hopper | m3 |  | 2 |  | * |  |
| Blades thickness | mm |  | 50 - 30 |  | * |  |
| Shedder chamber size | mm |  | 850 x 1,000 |  | * |  |
| Power | kW |  | 37 |  | * |  |

*data provided by commercial producer.

Tab. S5 - Main technical specifications of screw conveyor.

| Parameter | Unit | Value | Reference |
| --- | --- | --- | --- |
| Pipe diameter | mm | 160 | * |
| Length | mm | 2,100 | * |
| Height | mm | 450 | * |
| Power | kW | 3 | * |
| Maximum capacity | ton/h | 1 | * |

*data provided by commercial producer.

Tab. S6 - Average characterization of wastewater from fishing net washing.

| Parameter | Unit | Value | Reference |
| --- | --- | --- | --- |
| pH | - | 7.2 – 7.7 | (Ozgur et al. 2023) |
| Chemical oxygen demand (COD) | mg/L | 1,400 | (Ozgur et al. 2023) |
| Conductivity | µs/cm | 28,000 | (Ozgur et al. 2023) |
| Total organic carbon (TOC) | mg/L | 790 | (Ozgur et al. 2023) |
| Color | 465 nm Pt-Co | 6,160 | (Ozgur et al. 2023) |
| Salinity | mg/L | 10,000 | (Pasciucco et al. 2021) |

Tab. S7 - Inventory data of reverse osmosis treatment (per m³ treated water).

| Parameter | Unit | Value | Reference |
| --- | --- | --- | --- |
| Electricity consumption | kWh | 4 | (Tarnacki et al. 2012) |
| Chlorine consumption | kg | 7,06E-03 | (Tarnacki et al. 2012) |
| Ferric chloride consumption | kg | 7,06E-03 | (Tarnacki et al. 2012) |
| Sodium bisulfite consumption | kg | 1,41E-02 | (Tarnacki et al. 2012) |
| Sulphuric acid consumption | kg | 5,88E-02 | (Tarnacki et al. 2012) |
| Sodium hypochlorite consumption | kg | 5,88E-03 | (Tarnacki et al. 2012) |
| Reclaimed water | % | 67 | (Qasim et al. 2019) |
| COD removal | % | 85 | (Thirugnanasambandham et al. 2016) |
| Salinity removal | % | 91 | (Thirugnanasambandham et al. 2016) |
| Brine production | % | 33 | (Qasim et al. 2019) |

Tab. S8 - Inventory data for pyro-gasification process.

| Parameter | Unit | Value | Reference |
| --- | --- | --- | --- |
| Heating rate | °C/min | 8 | (Ciacci et al. 2022) |
| Pyrolysis temperature | °C | 510 | (Ciacci et al. 2022) |
| Pyrolysis time | min | 20 | (Ciacci et al. 2022) |
| Gasification temperature | °C | 510 | (Ciacci et al. 2022) |
| Gasification time | min | 120 | (Ciacci et al. 2022) |
| Electricity consumption | kWh/kgrCF | 8.33 | (Ciacci et al. 2022; Witik et al. 2013) |
| Nitrogen consumption | kg/kgrCF | 0.182 | (Ciacci et al. 2022; Xayachak et al. 2023) |
| Oxygen consumption | kg/kgrCF | 1.173 | (Ciacci et al. 2022; Xayachak et al. 2023) |
| Liquefied petroleum gas consumption | kg/kgrCF | 0.08 | (Ciacci et al. 2022; Xayachak et al. 2023) |
| Ash production | %CFRP | 8 | (Ciacci et al. 2022; Witik et al. 2013) |
| CO emission | gCO/gCFRP | 0.08 | (Ciacci et al. 2022; Dao et al. 2016) |
| CO2 emission | gCO2/gCFRP | 1.6 | (Ciacci et al. 2022; Dao et al. 2016) |

Tab. S9 - Inventory data for virgin carbon fiber production.

| From acrylonitrile to polyacrylonitrile |  |  |  |
| --- | --- | --- | --- |
| Parameter | Unit | Value | Reference |
| Acrylonitrile consumption | kg | 1.75 | (Meng et al. 2017) |
| Vinyl Acetate consumption | kg | 0.16 | (Meng et al. 2017) |
| Steam consumption | kg | 31.4 | (Meng et al. 2017) |
| Electricity consumption | MJ | 117 | (Meng et al. 2017) |
| From polyacrylonitrile to carbon fiber |  |  |  |
| Parameter | Unit | Value | Reference |
| Water consumption | kg | 2.77 | (Meng et al. 2017) |
| Sizing solids consumption | kg | 0.01 | (Meng et al. 2017) |
| Sulphuric acid consumption | kg | 0.02 | (Meng et al. 2017) |
| Electricity consumption | MJ | 32.4 | (Meng et al. 2017) |
| Natural gas consumption | MJ | 177.8 | (Meng et al. 2017) |

Tab. S10 - Life cycle impact assessment

| Impact category | Scenario 0 | Scenario 1 | Scenario 2 |
| --- | --- | --- | --- |
| Abiotic depletion [kg Sb eq.] | 7.07E-02 | -3.28E-02 | -6.04E-02 |
| Abiotic depletion (fossil fuels) [MJ] | 2.03E+05 | 1.10E+05 | -9.77E+04 |
| Global warming [kg CO2 eq.] | 1.37E+04 | 4.26E+03 | -5.74E+03 |
| Ozone layer depletion [kg CFC-11 eq.] | 1.57E-04 | 2.33E-04 | -4.04E-05 |
| Human toxicity [kg 1,4-DB eq.] | 1.78E+04 | 2.83E+04 | -3.18E+03 |
| Freshwater aquatic ecotoxicity [kg 1,4-DB eq.] | 3.68E+03 | 5.97E+03 | -3.55E+02 |
| Marine aquatic ecotoxicity [kg 1,4-DB eq.] | 1.05E+07 | 1.67E+07 | -9.43E+05 |
| Terrestrial ecotoxicity [kg 1,4-DB eq.] | 1.30E+02 | 1.86E+02 | -3.36E+01 |
| Photochemical oxidation [kg C2H4 eq.] | 2.26E+00 | 5.37E-01 | -8.86E-01 |
| Acidification [kg SO2 eq.] | 4.49E+01 | 1.50E+00 | -3.21E+01 |
| Eutrophication [kg PO4 eq.] | 1.75E+01 | 1.05E+01 | -1.36E+01 |

Tab. S11 - Percentage differences in the environmental impacts generated by the alternative scenarios in sensitivity analysis (WWTP 50 km away) compared to default LCA.

| Impact category | Scenario 1 | Scenario 2 |
| --- | --- | --- |
| Abiotic depletion [kg Sb eq.] | 7% | 4% |
| Abiotic depletion (fossil fuels) [MJ] | -51% | -58% |
| Global warming [kg CO2 eq.] | -83% | -62% |
| Ozone layer depletion [kg CFC-11 eq.] | -17% | -96% |
| Human toxicity [kg 1,4-DB eq.] | -4% | -38% |
| Freshwater aquatic ecotoxicity [kg 1,4-DB eq.] | -11% | -192% |
| Marine aquatic ecotoxicity [kg 1,4-DB eq.] | -15% | -271% |
| Terrestrial ecotoxicity [kg 1,4-DB eq.] | 46% | 253% |
| Photochemical oxidation [kg C2H4 eq.] | -43% | -26% |
| Acidification [kg SO2 eq.] | -126% | -6% |
| Eutrophication [kg PO4 eq.] | 43% | 33% |

Tab. S12 - Percentage differences in the environmental impacts generated by the alternative scenarios in sensitivity analysis (WWTP 150 km away) compared to default LCA.

| Impact category | Scenario 1 | Scenario 2 |
| --- | --- | --- |
| Abiotic depletion [kg Sb eq.] | 56% | 30% |
| Abiotic depletion (fossil fuels) [MJ] | -2% | -3% |
| Global warming [kg CO2 eq.] | 12% | 9% |
| Ozone layer depletion [kg CFC-11 eq.] | 11% | 62% |
| Human toxicity [kg 1,4-DB eq.] | 51% | 457% |
| Freshwater aquatic ecotoxicity [kg 1,4-DB eq.] | 22% | 377% |
| Marine aquatic ecotoxicity [kg 1,4-DB eq.] | 21% | 366% |
| Terrestrial ecotoxicity [kg 1,4-DB eq.] | 101% | 556% |
| Photochemical oxidation [kg C2H4 eq.] | 61% | 37% |
| Acidification [kg SO2 eq.] | 315% | 15% |
| Eutrophication [kg PO4 eq.] | 61% | 47% |

Tab. S13 - Percentage differences in the environmental impacts generated by the alternative scenarios in sensitivity analysis (WWTP 200 km away) compared to default LCA.

| Impact category | Scenario 1 | Scenario 2 |
| --- | --- | --- |
| Abiotic depletion [kg Sb eq.] | 81% | 44% |
| Abiotic depletion (fossil fuels) [MJ] | 22% | 25% |
| Global warming [kg CO2 eq.] | 59% | 44% |
| Ozone layer depletion [kg CFC-11 eq.] | 24% | 141% |
| Human toxicity [kg 1,4-DB eq.] | 79% | 705% |
| Freshwater aquatic ecotoxicity [kg 1,4-DB eq.] | 39% | 662% |
| Marine aquatic ecotoxicity [kg 1,4-DB eq.] | 39% | 684% |
| Terrestrial ecotoxicity [kg 1,4-DB eq.] | 128% | 708% |
| Photochemical oxidation [kg C2H4 eq.] | 114% | 69% |
| Acidification [kg SO2 eq.] | 536% | 25% |
| Eutrophication [kg PO4 eq.] | 71% | 54% |

Tab. S14 - Percentage differences in the environmental impacts generated by the alternative scenarios in sensitivity analysis (WWTP 250 km away) compared to default LCA.

| Impact category | Scenario 1 | Scenario 2 |
| --- | --- | --- |
| Abiotic depletion [kg Sb eq.] | 106% | 57% |
| Abiotic depletion (fossil fuels) [MJ] | 47% | 53% |
| Global warming [kg CO2 eq.] | 106% | 79% |
| Ozone layer depletion [kg CFC-11 eq.] | 38% | 220% |
| Human toxicity [kg 1,4-DB eq.] | 107% | 952% |
| Freshwater aquatic ecotoxicity [kg 1,4-DB eq.] | 56% | 946% |
| Marine aquatic ecotoxicity [kg 1,4-DB eq.] | 57% | 1003% |
| Terrestrial ecotoxicity [kg 1,4-DB eq.] | 155% | 860% |
| Photochemical oxidation [kg C2H4 eq.] | 166% | 100% |
| Acidification [kg SO2 eq.] | 756% | 35% |
| Eutrophication [kg PO4 eq.] | 80% | 62% |

Fig. S1 - TGA of vCF and rCF. Temperature profile: Troom to 900 °C (10 °C/min in N2); 900 °C to 1300 °C (10 °C/min in air).

| a | b |
| --- | --- |

Fig. S2 - TGA of rPA6, PvCFX (a), and rPA6, PrCFX (b). Temperature profile: Troom to 900 °C (10 °C/min in N2); 900 °C to 1300 °C (10 °C/min in air).

| a | b |
| --- | --- |

Fig. S3 - DSC thermograms of rPA6, PvCFX (a), and rPA6, PrCFX (b). Data referring to the 2nd heating scan at 10 °C/min from -50 °C to 330 °C.

Fig. S4 - contribution analysis for abiotic depletion potential.

Fig. S5 - Contribution analysis for abiotic depletion (fossil fuel) potential.

Fig. S6 - Contribution analysis for human toxicity potential.

Fig. S7 - Contribution analysis for freshwater aquatic ecotoxicity potential.

Fig. S8 - Contribution analysis for marine aquatic ecotoxicity potential.

Fig. S9 - Contribution analysis for terrestrial ecotoxicity potential.

Fig. S10 - Contribution analysis for photochemical oxidation potential.

Fig. S11 - Contribution analysis for acidification potential.

Fig. S12 - Percentage differences in the environmental impacts compared to the reference (Scenario 0) – sensitivity analysis (WWTP 100 km away).

Fig. S13 - Percentage differences in the environmental impacts compared to the reference (Scenario 0) – sensitivity analysis (WWTP 50 km away).

Fig. S14 - Percentage differences in the environmental impacts compared to the reference (Scenario 0) – sensitivity analysis (WWTP 150 km away).

Fig. S15 - Percentage differences in the environmental impacts compared to the reference (Scenario 0) – sensitivity analysis (WWTP 200 km away).

Fig. S16 - Percentage differences in the environmental impacts compared to the reference (Scenario 0) – sensitivity analysis (WWTP 250 km away).

|  |  |  | rCF after pyro-gasification |  |  | vCF T830H Torayca® |  |  | rPA6 fishing nets |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Materials |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  | Single-screw extruder |  |  | CF-rPA6 filaments |  |  | CF-rPA6 granules |  |  |
| Extrusion Compounding |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  | Dog-bones specimens |  |  | Tensile tests |  |  |  |  |  |
| Mechanical Characterization |  |  |  |  |  |  |  |  |  |  |  |

Fig. S17 - Images of raw materials, extrusion process, and characterization of the composites.

References

Ciacci, L., Zattini, G., Tosi, C., Berti, B., Passarini, F., & Giorgini, L. (2022). Carbon Fibers Waste Recovery via Pyro-Gasification: Semi-Industrial Pilot Plant Testing and LCA. Sustainability (Switzerland), 14(7). https://doi.org/10.3390/su14073744

Dao, D. Q., Rogaume, T., Luche, J., Richard, F., Bustamante Valencia, L., & Ruban, S. (2016). Thermal degradation of epoxy resin/carbon fiber composites: Influence of carbon fiber fraction on the fire reaction properties and on the gaseous species release. Fire and Materials, 40(1). https://doi.org/10.1002/fam.2265

Meng, F., McKechnie, J., Turner, T. A., & Pickering, S. J. (2017). Energy and environmental assessment and reuse of fluidised bed recycled carbon fibres. Composites Part A: Applied Science and Manufacturing, 100. https://doi.org/10.1016/j.compositesa.2017.05.008

Ozgur, C., Senel, K., Aykut-Senel, B., & Bekaroglu, S. S. K. (2023). Treatment of net washing wastewater by Fenton process. Global Nest Journal, 25(6). https://doi.org/10.30955/gnj.005088

Pasciucco, F., Pecorini, I., Di Gregorio, S., Pilato, F., & Iannelli, R. (2021). Recovery strategies of contaminated marine sediments: A life cycle assessment. Sustainability (Switzerland), 13(15). https://doi.org/10.3390/su13158520

Qasim, M., Badrelzaman, M., Darwish, N. N., Darwish, N. A., & Hilal, N. (2019). Reverse osmosis desalination: A state-of-the-art review. Desalination, 459, 59–104. https://doi.org/10.1016/j.desal.2019.02.008

Tarnacki, K., Meneses, M., Melin, T., van Medevoort, J., & Jansen, A. (2012). Environmental assessment of desalination processes: Reverse osmosis and Memstill®. Desalination, 296, 69–80. https://doi.org/10.1016/j.desal.2012.04.009

Thirugnanasambandham, K., Sivakumar, V., & Shine, K. (2016). Optimization of reverse osmosis treatment process to reuse the distillery wastewater using taguchi design. Desalination and Water Treatment, 57(51). https://doi.org/10.1080/19443994.2016.1141323

Witik, R. A., Teuscher, R., Michaud, V., Ludwig, C., & Månson, J. A. E. (2013). Carbon fibre reinforced composite waste: An environmental assessment of recycling, energy recovery and landfilling. Composites Part A: Applied Science and Manufacturing, 49. https://doi.org/10.1016/j.compositesa.2013.02.009

Xayachak, T., Haque, N., Lau, D., Parthasarathy, R., & Pramanik, B. K. (2023). Assessing the environmental footprint of plastic pyrolysis and gasification: A life cycle inventory study. Process Safety and Environmental Protection, 173. https://doi.org/10.1016/j.psep.2023.03.061