# A detailed characterization study of Ni/CeO2 catalysts identifies Ni availability as the primary factor affecting CO2 methanation performance

Sining Chen1,2, Luke Higgins2,3, Ilenia Giarnieri4,5, Patricia Benito4,5, Andrew M. Beale1,2,*

1Department of Chemistry, University College London, 20 Gordon Street, WC1H 0AJ, UK

2Research Complex at Harwell, Rutherford Appleton Laboratories, Harwell Science and Innovation Campus, Harwell, Didcot, OX11 0FA, UK

3Diamond Light Source, Rutherford Appleton Laboratories, Harwell Science and Innovation Campus, Harwell, Didcot, OX11 0FA, UK

4Department of Industrial Chemistry “Toso Montanari”, Alma Mater Studiorum – Università di Bologna, Viale Risorgimento, 4, 40136, Bologna, Italy

5Center for Chemical Catalysis – C3, Alma Mater Studiorum – Università di Bologna, Viale Risorgimento 4, 40136, Bologna, Italy

Supplementary information

Fig. S1. CO hydrogenation over (a) Ni/CeO2 (600, air) and Ni/CeO2 (700, air) at the GHSV = 15, 000 mL/(h·g), and (b) Ni/CeO2 (600, air), Ni/CeO2 (600, He) and Ni/CeO2 (600, NO) at the GHSV = 30, 000 mL/(h·g).

The CO hydrogenation experiments of different catalysts was also carried out to have a better understanding on the role of CO during the reaction, as displayed in Fig. S1. It can be seen that all samples exhibit much worse performance for CO hydrogenation with conversion being less than 20 % at 270 °C. The CO hydrogenation ability over these catalysts can be ranked according to the CH4 formation, with the order being Ni/CeO2 (600, He) ~ Ni/CeO2 (600, NO) ＞Ni/CeO2 (600, air) ＞Ni/CeO2 (700, air).

Fig. S2. XRD patterns of CeO2 (600) and CeO2 (700) recorded in lab-based Rigaku XRD instrument at the range of 2θ = 2080°, Phase compositions: CeO2 (JCPDS No. 43-1002).

The pure CeO2 supports calcined at 600 and 700 °C were also measured, as seen in Fig. S2. For the pure CeO2 supports calcined at different temperatures, cerianite-styled CeO2 (JCPDS No. 43-1002) were formed with the 2θ diffraction peaks at 28.55, 33.08, 47.48, 56.34, 59.09, 69.40o, 76.70 and 79.04 °. The intensity of these diffraction peaks indicates an obvious increase in the crystallinity of CeO2 calcined at higher temperatures.

Fig. S3. XRD patterns of Ni/CeO2 (600, air), Ni/CeO2 (700, air), Ni/CeO2 (600, He) and Ni/CeO2 (600, NO) recorded in Rigaku XRD instrument at the range of (a) 2θ = 2080° and (b) 2θ = 4346°, Phase compositions: CeO2 (JCPDS No. 43-1002), Ni0 (JCPDS No. 04-0850).

Fig. S4. Synchrotron XRD profiles of NiO/CeO2 (600, NO) at different Y-axis magnifications (×1 and ×27)

Table S1. Position and full width at half maximum (FWHM) of CeO2 (111) and Ni(O) (111) in synchrotron XRD profiles

| Samples | CeO2 (111) |  | NiO (111) |  | Ni (111) |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Position | FWHM | Position | FWHM | Position | FWHM |
| NiO/CeO2 (600, air) | 2.4979(1) | 0.056(1) | 3.231(2) | 0.052(8) | / | / |
| NiO/CeO2 (700, air) | 2.4978(9) | 0.043(3) | 3.231(1) | 0.044(5) | / | / |
| NiO/CeO2 (600, He) | 2.4988(2) | 0.056(1) | 3.232(3) | 0.047(9) | / | / |
| NiO/CeO2 (600, NO) | 2.4989(1) | 0.056(1) | 3.231(2) | 0.051(8) | / | / |
| Ni/CeO2 (600, air) | 2.4962(1) | 0.049(1) | / | / | 3.834(2) | 0.058(7) |
| Ni/CeO2 (700, air) | 2.4965(1) | 0.041(1) | / | / | 3.833(1) | 0.050(4) |
| Ni/CeO2 (600, He) | 2.4962(1) | 0.050 (1) | / | / | 3.834(1) | 0.056(5) |
| Ni/CeO2 (600, NO) | 2.4961(1) | 0.053(1) | / | / | 3.833(1) | 0.055(6) |

Fig. S5. HAADF images and EDX maps (Ni and Ce) of Ni/CeO2 (600, air)

Table S2. Atomic percentage of the surface Ni, Ce and O over different samples

| Sample | Ni (at %) | Ce (at %) | O (at %) | Ni/Ce (at/at %) |
| --- | --- | --- | --- | --- |
| NiO/CeO2 (600, air) | 7.6 | 14.41 | 78.0 | 0.52 |
| NiO/CeO2 (700, air) | 9.3 | 13.78 | 76.9 | 0.68 |
| NiO/CeO2 (600, He) | 5.7 | 11.50 | 82.8 | 0.49 |
| NiO/CeO2 (600, NO) | 9.2 | 19.58 | 71.3 | 0.47 |
| Ni/CeO2 (600, air) | 5.7 | 26.8 | 67.5 | 0.21 |
| Ni/CeO2 (700, air) | 6.9 | 23.2 | 69.9 | 0.30 |
| Ni/CeO2 (600, He) | 5.5 | 44.0 | 50.5 | 0.13 |
| Ni/CeO2 (600, NO) | 3.9 | 47.1 | 49.0 | 0.08 |

The survey spectra were scanned up to 1100 eV, with the relative percentage of each element is given in Table S2. The inelastic mean free paths (IMFP) of the photoelectrons from Ni 2p and Ce 3d are respectively 11.1 and 13.6 Å, suggesting that the mean escape depth of electrons and the probing depth in the Ni(O)/CeO2 are within 20 % of each other [1]. It is therefore reasonable to evaluate the surface element composition over the different samples from the results given in Table S2. For the NiO/CeO2, it can be observed that the Ni/Ce ratio is in the following order: NiO/CeO2 (600, NO) < NiO/CeO2 (600, He) < NiO/CeO2 (600, air) < NiO/CeO2 (700, air), respectively. The lower surface Ni/Ce ratio can be achieved on the catalyst with smaller Ni crystallite size, suggesting the presence of ultra-small nanoparticles which cannot be detected by XPS. A slightly decreased Ni/Ce ratio over the NO calcined sample could explain its highest Ni dispersion to some extent, as the presence of ultrasmall Ni species can go into the CeO2 structure more easily. The surface Ni/Ce ratio on the reduced catalysts are also given in Table S2, which are around 0.21, 0.30, 0.13 and 0.08 on the Ni/CeO2 (600, air), Ni/CeO2 (700, air), Ni/CeO2 (600, He) and Ni/CeO2 (600, NO), respectively. We propose that the decrease in surface Ni over all the Ni/CeO2 can be explained by the encapsulation of Ni by the coverage of CeOx layers after the reduction, due to the formation of a strong metal-support interaction (SMSI) over the Ni/CeO2 [2-4]. However, the extent of SMSI over these Ni/CeO2 catalysts are difficult to estimate and compare based on the Ni/Ce ratio as the Ni/Ce ratio can be significantly affected by the Ni NP size, SMSI and the NiO film formed during O2 passivation etc.

Table S3. Number of Ni sites (mmol/g) and Ni coverage (%) over different Ni/CeO2 catalysts

| Sample | NNi-sites, expected (mmol/g)a | H2-TPD |  | CO chemisorption |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | NNi-sites, H2 (mmol/g)b | Ni coverage (%)b |  | NNi-sites, CO (mmol/g)c | Ni coverage (%)c |
| Ni/CeO2 (600, air) | 0.250 | 0.095 | 61.8 |  | 0.049 | 80.3 |
| Ni/CeO2 (700, air) | 0.199 | 0.057 | 71.3 |  | 0.025 | 87.5 |
| Ni/CeO2 (600, He) | 0.265 | 0.080 | 69.7 |  | 0.039 | 85.3 |
| Ni/CeO2 (600, NO) | 0.330 | 0.115 | 65.0 |  | 0.058 | 82.4 |

a Estimated from Ni dispersion DNi b Estimated from H2-TPD c Estimated from CO chemisorption

Fig. S6. Results (background, observed data, calculated data and differences) of Rietveld refinement over various NiO/CeO2 and Ni/CeO2. (a) NiO/CeO2 (600, air), (b) Ni/CeO2 (600, air), (c) NiO/CeO2 (700, air), (d) Ni/CeO2 (700, air), (e) NiO/CeO2 (600, He), (f) Ni/CeO2 (600, He), (g) NiO/CeO2 (600, NO) and (h) Ni/CeO2 (600, NO)

Table S4. Crystalline (NiO, Ni and CeO2) weight percentages and Ni loadings over the NiO/CeO2 and Ni/CeO2 estimated by the Rietveld refinement.

| Samples | Crystalline percentage (wt%) |  |  | Ni loadings (wt. %) | Weighed profile R-factor (Rwp) | Goodness of fitting |
| --- | --- | --- | --- | --- | --- | --- |
|  | CeO2 | NiO | Ni0 |  |  |  |
| NiO/CeO2 (600, air) | 89.1 | 10.9 | / | 9.6 | 2.79 | 1.74 |
| NiO/CeO2 (700, air) | 88.7 | 11.3 | / | 10.0 | 2.41 | 1.38 |
| NiO/CeO2 (600, He) | 89.2 | 10.8 | / | 9.5 | 2.24 | 1.07 |
| NiO/CeO2 (600, NO) | 89.3 | 10.7 | / | 9.4 | 2.77 | 1.68 |
| Ni/CeO2 (600, air) | 91.7 | / | 8.3 | 9.1 | 2.48 | 1.29 |
| Ni/CeO2 (700, air) | 91.2 | / | 8.8 | 9.6 | 2.54 | 1.31 |
| Ni/CeO2 (600, He) | 93.3 | / | 6.7 | 7.2 | 2.43 | 1.35 |
| Ni/CeO2 (600, NO) | 93.7 | / | 6.3 | 6.7 | 2.16 | 1.03 |

Table S5. Liner composition fitting results of the Ni/CeO2 sample calcined at different atmospheres (air, He and NO)

| Sample | NiO (%) | Ni0 (%) | χ2 |
| --- | --- | --- | --- |
| Ni/CeO2 (600, air) | 20.5 | 79.5 | 0.026 |
| Ni/CeO2 (700, air) | 39.3 | 60.7 | 0.070 |
| Ni/CeO2 (600, He) | 30.0 | 70.0 | 0.084 |
| Ni/CeO2 (600, NO) | 32.4 | 67.6 | 0.059 |

Table S6. EXAFS fitting information of the first shell of the Ni/CeO2 samples

| Sample | 1st Shell | R (Å) | C.N. | σ2 (Å2) | ΔE0 (eV) |
| --- | --- | --- | --- | --- | --- |
| Ni/CeO2 (600, air) | NiNi (Ni0) | 2.485 ± 0.003 | 8.7 ± 0.9 | 0.006 ± 0.003 | 1.15 |
| Ni/CeO2 (700, air) | NiNi (Ni0) | 2.493 ± 0.007 | 7.7 ± 1.7 | 0.006 ± 0.002 | 2.58 |
| Ni/CeO2 (600, He) | NiNi (Ni0) | 2.486 ± 0.004 | 8.1 ± 1.1 | 0.006 ± 0.001 | 1.35 |
| Ni/CeO2 (600, NO) | NiNi (Ni0) | 2.489 ± 0.005 | 7.7 ± 1.3 | 0.006 ± 0.001 | 1.83 |

Fig. S7. TPR profiles of the NiO/CeO2 (600, air), NiO/CeO2 (700, air) and their supports CeO2

In order to clearly investigate the reduction performance of surface CeO2 species, the H2-TPR analysis were also carried out over the pure CeO2 (600) and CeO2 (700), the results of which are displayed in Fig. S7. For the pure CeO2, apart from the reduction process of bulk CeO2 (3) at around 800 °C, two reduction peaks (1 and 2) attributed to be the reduction of surface oxygen on CeO2 are also detected at low temperatures (300600 °C). The intensities of peaks 1 and 2 decrease at a higher calcination temperature of CeO2, most likely as a consequence of decreased surface area with increased calcination temperature.

Fig. S8. Ni K-edge EXAFS fitting results of the (c) R and (d) k space based on the NiNi (Ni0) path over the Ni/CeO2. Short dots: raw data. Solid line: fitting data.

Fig. S9. 1st H2-TPR profile of the NiO/CeO2 (600, air) and 2nd H2-TPR profile after the in situ oxidisation (O2 pulse) of the reduced sample

Fig. S10. In situ DRIFTS profiles of CO2 adsorption at different temperatures over (a) Ni/CeO2 (600, air), (b) Ni/CeO2 (700, air), (c) Ni/CeO2 (600, He) and (d) Ni/CeO2 (600, NO). Each spetrum was collected from 100 to 400 °C with the interval of 50 °C. The wavelength region is 40001000 cm1.

The CO2 adsorption performance over different reduced samples is displayed in Fig. S10. For all the samples, the typical CO2 association species (carbonates and bicarbonates) are observed on all the samples in the region of 22501000 cm1 after the introduction of 20% CO2 flowing gas. Carbonate species can be divided as two main types, including bidentate carbonates (~1590 cm1) and monodentate carbonates (~1336 cm1) [5, 6]. Bicarbonates, generated from monodentate carbonate and surface OH groups on Ce sites, can also be seen at around 1480 cm1, 1428 cm1, and 1212 cm1 [6, 7]. The adsorbed CO2 on the Ni0 active sites also benefit the CO formation with the linear CO (21001950 cm1) and bridge CO (19501750 cm1) seen in the spectra [8]. The reaction process is regarded as the CO2 dissociation (CO2(ads) → CO(ads) + O(ads)).  In addition, the bands at 1550 and 1290 cm1 assigned as the formate are observed, indicating the reaction between chemisorbed CO2 and dissociated H on the Ni0 sites after reduction [9, 10]. It can be seen that the reaction between surface OH groups and CO2 occur more easily at high temperatures over all the samples, accompanied by a slightly increase in bicarbonate species (14901420 cm1). However, the formate species at around 1550 cm1 and 1290 cm1 decrease significantly with the increasing temperature over the different Ni/CeO2 samples, which implicit the thermal unstable properties of the formate species. The thermal instability of carbonates and formate over the Ni/CeO2 (600, NO) could indicate its highest reactivity of these species, thereby leading to its highest catalytic performance in CO2 methanation. The CO2 dissociation is similar to the reverse water gas shift (RWGS) reaction which produces CO from CO2 and H2 (CO2 + H2 → CO + H2O). One possible mechanism of RWGS is regarded as the oxidation of oxygen vacancies over the support by CO2, followed by the formation of Ni-carboxyl species [11]. Therefore, the CO formation route by CO2 dissociation over the Ni/CeO2 catalysts can be proposed. One of the O atoms of CO2 can go into the oxygen vacancies on Ce3+ sites, and then dissociated CO* moves to active Ni0 sites. The role of oxygen vacancies in CO2 dissociation was also studied over the CeO2 [12]. It should be noted in Fig. S10 that the intensities of CO bands over Ni/CeO2 (600, air) gradually increase with the adsorption temperature getting higher, indicating its higher dissociation ability of CO2 at the higher temperature [13].

Fig. S11. In situ DRIFTS spectra of transient CO2 methanation at 250 °C over CO2 adsorbed (a) Ni/CeO2 (600, air), (b) Ni/CeO2 (700, air), (c) Ni/CeO2 (600, He) and (d) Ni/CeO2 (600, NO).

The transient reaction over the CO2 adsorbed catalysts were also performed for the investigation of active intermediates during CO2 hydrogenation with the gas switch in the process of H2 (reduction) → He (purge and background collection) → CO2 (adsorption) → He (removal of physically adsorbed species) → H2 (reaction between H2 and chemisorbed CO2(ads)). Firstly, the lower reaction temperature of 250 °C was applied, the results of which can be seen in Fig. S11. All Ni/CeO2 samples see a similar CO2 adsorption and transient performance at this temperature. After CO2 adsorption for 30 min followed by He purge, the presence of monodentate carbonates, bidentate carbonates and bicarbonates are observed in all Ni/CeO2 samples, denoted as the spectra named “CO2 30 min” [5]. As seen in Fig. S11, when H2 is introduced into the system, the gas phase CO2 shows up immediately at the spectra collected at 1 min on all Ni/CeO2 samples, suggesting the competitive adsorption sites of CO2 and H2 species. Expect for Ni/CeO2 (600, NO), the intensities of formate species (~1550 and 1370 cm1) significantly increase at 1 min over the Ni/CeO2. This could be due to the highest reaction rate on Ni/CeO2 (600, NO). Furthermore, the adsorbed CO species from CO2 dissociation disappears rapidly after the H2 introduction, exhibiting the role of CO as the intermediate in CO2 methanation reaction. For the spectra collected at 1 minute, the intensities of gas phase CH4 (~3016 cm1) over different samples reach to the maximal, resulting from the largest concentration of adsorbed carbonates after CO2 adsorption. Afterwards, the CH4 formation amount significantly decreases with the reaction time and eventually disappears at around 5 min, accompanied by the continuous consumption of surface adsorbed carbonate and formate species. Therefore, the reactivity of formate species as the intermediate can be proposed. Interestingly, the consumption of surface carbonates and formate species still takes place continuously with no CH4 peak observed. It could be due to the low formation rate of CH4 or the generation of adsorbed CO on Ce3+ sites observed at ~2100 cm1. Unlike the CO(ads) on Ni0 sites, the CO(ads) on Ce3+ sites cannot be hydrogenated for CH4 formation [7].

Fig. S12. In situ DRIFTS spectra of transient CO2 methanation at 350 °C over CO2 adsorbed (a) Ni/CeO2 (600, air), (b) Ni/CeO2 (700, air), (c) Ni/CeO2 (600, He) and (d) Ni/CeO2 (600, NO).

A similar transient reaction was also conducted over the Ni/CeO2 at 350 °C, as exhibited in Fig. S12. Similarly, after CO2 adsorption, all carbonate (bidentate carbonate, monodentate carbonate and bicarbonate) and formate species are formed. Moreover, the bands at the region of 21001800 cm1 belonging to the adsorbed CO species are also clearly observed. Upon the introduction of H2, the hydrogenation of active species also take place rapidly on all Ni/CeO2 samples, and the highest CH4 formation rate can be obtained at 1 min. Besides, the band of CH methane (1305 cm1) is also observed as the formation of CH4 [9]. At this reaction temperature, the increases of formate species observed at 1 min in the previous experiment (Fig. S8) are not seen at 350 °C, demonstrating the higher reaction rate at a higher temperature. Moreover, unlike other samples, Fig. S12 shows that the CO species over the Ni/CeO2 (700, air) are much more stable than others at 1 min, although they can be totally consumed in the next 1 min. The poor reactivity of surface formate and CO species over the Ni/CeO2 (700, air) then demonstrate its low reaction rate of intermediates, indicating the poor activity of Ni/CeO2 (700, air) during the CO2 methanation. The consumption amount of the adsorbed CO2 species at 350 °C in all the catalysts are then roughly calculated by the integration of curves collected before H2 and after H2 for 20 min in the range of 22001000 cm1. It can be seen that the Ni/CeO2 (600, NO) displays the highest utilization efficiency of adsorbed CO2 species (ca. 95 %), followed by the Ni/CeO2 (600, air) (ca. 80 %), Ni/CeO2 (600, He) (ca. 74 %) and Ni/CeO2 (700, air) (ca. 56%), demonstrating the outstanding catalytic ability of the Ni/CeO2 (600, NO) under CO2 methanation condition.

Based on the discussion of the transient reaction above, both of the CO(ads) and formate species can be regarded as the active intermediates in CO2 methanation over these Ni/CeO2 catalysts. The ‘CO route’ takes place with the roughly process of CO2 → CO → CH4, while the ‘formate route’ occur in the process of CO2 → (bi)carbonates → formate → CH4 [14]. By comparing the consumption performance of formate species after H2 introduction at different temperatures (Figs. S11 and S12), we see that the bands of formate species (2840 and 1580 cm1) on all samples are much more stable during the hydrogenation reaction at 250 °C than those at 350 °C. Combining the higher intensity of methane (3014 and 1304 cm1) in Fig. S12 and the enhanced catalytic activity of all Ni/CeO2 at higher temperatures displayed in Fig. 1, we note that the increase in methane formation comes at the expense of the formate species, suggesting that the formate species are key intermediates and the formate hydrogenation is the rate-determined step during the CO2 methanation. This is consistent with the activity assessment of all catalysts during the CO hydrogenation reaction shown in Fig. S1, which points out that the CO is not the main active species for CH4 formation.

Reference

[1] W.T. Figueiredo, R. Prakash, C.G. Vieira, D.S. Lima, V.E. Carvalho, E.A. Soares, S. Buchner, H. Raschke, O.W. Perez-Lopez, D.L. Baptista, R. Hergenröder, M. Segala, F. Bernardi, New insights on the electronic factor of the SMSI effect in Pd/TiO2 nanoparticles, Appl. Surf. Sci., 574 (2022) 151647, https://doi.org/10.1016/j.apsusc.2021.151647.

[2] Y. Guo, S. Mei, K. Yuan, D. Wang, H. Liu, C. Yan, Y. Zhang, Low-temperature CO2 methanation over CeO2-supported Ru single atoms, nanoclusters, and nanoparticles competitively tuned by strong metal–support interactions and H-spillover effect, ACS Catal., 8 (2018) 6203-6215, https://doi.org/10.1021/acscatal.7b04469.

[3] J. Li, Y. Lin, X. Pan, D. Miao, D. Ding, Y. Cui, J. Dong, X. Bao, Enhanced CO2 methanation activity of Ni/Anatase catalyst by tuning strong metal–support Interactions, ACS Catal., 9 (2019) 6342-6348, https://doi.org/10.1021/acscatal.9b00401.

[4] L.P. Matte, A.S. Kilian, L. Luza, M.C.M. Alves, J. Morais, D.L. Baptista, J. Dupont, F. Bernardi, Influence of the CeO2 support on the reduction properties of Cu/CeO2 and Ni/CeO2 nanoparticles, J. Phys. Chem. C, 119 (2015) 26459-26470, https://doi.org/10.1021/acs.jpcc.5b07654.

[5] A. Cárdenas-Arenas, A. Quindimil, A. Davó-Quiñonero, E. Bailón-García, D. Lozano-Castelló, U. De-La-Torre, B. Pereda-Ayo, J.A. González-Marcos, J.R. González-Velasco, A. Bueno-López, Isotopic and in situ DRIFTS study of the CO2 methanation mechanism using Ni/CeO2 and Ni/Al2O3 catalysts, Appl. Catal. B: Environ., 265 (2020) 118538, https://doi.org/10.1016/j.apcatb.2019.118538.

[6] S. Collins, M. Baltanas, A. Bonivardi, An infrared study of the intermediates of methanol synthesis from carbon dioxide over Pd/β-Ga2O3, J. Catal., 226 (2004) 410-421, https://doi.org/10.1016/j.jcat.2004.06.012.

[7] Y. Yu, Y.M. Chan, Z. Bian, F. Song, J. Wang, Q. Zhong, S. Kawi, Enhanced performance and selectivity of CO2 methanation over g-C3N4 assisted synthesis of Ni-CeO2 catalyst: kinetics and DRIFTS studies, Int. J. Hydrog. Energy, 43 (2018) 15191-15204, https://doi.org/10.1016/j.ijhydene.2018.06.090.

[8] S. Ewald, M. Kolbeck, T. Kratky, M. Wolf, O. Hinrichsen, On the deactivation of Ni-Al catalysts in CO2 methanation, Appl. Catal. A: Gen., 570 (2019) 376-386, https://doi.org/10.1016/j.apcata.2018.10.033.

[9] P.H. Ho, G.S. de Luna, S. Angelucci, A. Canciani, W. Jones, D. Decarolis, F. Ospitali, E.R. Aguado, E. Rodríguez-Castellón, G. Fornasari, A. Vaccari, A.M. Beale, P. Benito, Understanding structure-activity relationships in highly active La promoted Ni catalysts for CO2 methanation, Appl. Catal. B: Environ., 278 (2020) 119256, https://doi.org/10.1016/j.apcatb.2020.119256.

[10] R. Ye, Q. Li, W. Gong, T. Wang, J.J. Razink, L. Lin, Y.-Y. Qin, Z. Zhou, H. Adidharma, J. Tang, A.G. Russell, M. Fan, Y.-G. Yao, High-performance of nanostructured Ni/CeO2 catalyst on CO2 methanation, Appl. Catal. B: Environ., 268 (2020) 118474, https://doi.org/10.1016/j.apcatb.2019.118474.

[11] A. Goguet, S. Shekhtman, R. Burch, C. Hardacre, F. Meunier, G. Yablonsky, Pulse-response TAP studies of the reverse water–gas shift reaction over a Pt/CeO2 catalyst, J. Catal., 237 (2006) 102-110, https://doi.org/10.1016/j.jcat.2005.10.020.

[12] B. Dai, S. Cao, H. Xie, G. Zhou, S. Chen, Reduction of CO2 to CO via reverse water-gas shift reaction over CeO2 catalyst, Korean J. Chem. Eng., 35 (2017) 421-427, https://doi.org/10.1007/s11814-017-0267-y.

[13] C. Heine, B.A. Lechner, H. Bluhm, M. Salmeron, Recycling of CO2: probing the chemical state of the Ni(111) surface during the methanation reaction with ambient-pressure X-Ray photoelectron spectroscopy, J. Am. Chem. Soc., 138 (2016) 13246-13252, https://doi.org/10.1021/jacs.6b06939.

[14] P. Hongmanorom, J. Ashok, P. Chirawatkul, S. Kawi, Interfacial synergistic catalysis over Ni nanoparticles encapsulated in mesoporous ceria for CO2 methanation, Appl. Catal. B: Environ., 297 (2021) 120454, https://doi.org/10.1016/j.apcatb.2021.120454.