SUPPLEMENTARY INFORMATION

Capping agent, solvent and nanoparticle interactions: driving selectivity for biomass transformations.

George F. Tierney,*[a,b] Daniel Banks,[a] Marina Carravetta,[a] Alice E. Oakley,[a] Shahram Alijani,[c] Ilaria Barlocco, [c] Nikolaos Dimitratos,[d] Alberto Villa,*[c] and Peter P. Wells*[a,b,e]

AUTHOR ADDRESS:
[a]	Dr. G. F. Tierney, D. Banks, Dr. A. E. Oakley, Prof. M. Carravetta and Prof. P. P.Wells
	School of Chemistry
	University of Southampton, Southampton, SO17 1BJ, United Kingdom.

[b]	Dr. G. F. Tierney and Prof. P. P. Wells 	
UK Catalysis Hub	
Research Complex at Harwell, Rutherford Appleton Laboratory, Harwell, Didcot,	
OX11 0FA, United Kingdom.

[c]	Dr. S. Alijani, Dr. I. Barlocco and Prof. A. Villa	
Dipartimento di Chimica	
Universitá degli Studi di Milano, via Golgi 19, 20133, Milano, Italy.

[d]	Prof. N. Dimitratos	
Dipartimento di Chimica Industriale	
“Toso Montanari” Alma Mater Studiorum Universitá di Bologna, Viale Risorgimento 4, 40136 Bologna, Italy.

[e]	Prof. P. P. Wells	
Diamond Light Source	
Harwell Science and Innovation Campus, Chilton, Didcot, OX11 0DE, United Kingdom.

Figure S1. Schematic detailing the possible routes to furfural hydrogenation (above) and acetalization (below) over Pd/TiO2 catalysts prepared using altered synthesis solvents, PVA and acidification procedures. Wherein, the complexation of PVA and MeOH during synthesis covers not only the NP surface, but also the support surface. This suppresses the potential for hydrogen spillover from the Pd NPs to the support, resulting in fewer Bronsted acid sites on Titania, and in turn selectivity only to the primary hydrogenation products. Schematic devised by incorporating results taken from our previous work on this, Tierney et al., ChemCatChem., 2021, 13, 5121-5133.1

Supplementary Figures 2 and Tables for 13C NMR.

Fittings of the 13C Cross Polarization NMR signals for the prepared catalysts are listed below. Bruker data were processed in Mestrenova, then imported in Matlab for fitting, using a Gauss-Lorentz lineshape for each NMR peak.

1 wt.% PdWPA

| Amplitude (A.U) | Peak Position (ppm) | Linewidth (ppm) | Gauss – Lorentz Ratio |
| --- | --- | --- | --- |
| 19.099 ± 22.973 | 73.234 ± 0.222 | 2.433 ± 0.545 | 0.007 ± 1.630 |
| 128.022 ± 36.565 | 67.965 ± 1.872 | 7.645 ± 0.970 | 1.000 ± 0.314 |
| 20.404 ± 23.633 | 64.514 ± 0.201 | 2.057 ± 0.706 | 0.816 ± 0.869 |
| 136.110 ± 17.053 | 41.160 ± 0.252 | 5.712 ± 0.255 | 0.348 ± 0.225 |
| 49.678 ± 24.529 | 30.211 ± 0.261 | 4.432 ± 0.467 | 0.001 ± 0.971 |
| 67.108 ± 13.256 | 17.672 ± 0.631 | 6.200 ± 0.783 | 0.880 ± 0.155 |

Number of scans = 56000

D1 = 3.5s

P15 = 500μs

Mestrenova settings:

Apodization = Exp 80 Hz. Phase 0th order = -21.53 Hz. Phase 1st order = 30 Hz. Baseline correction fit = Polynomial order 3

5 wt.% PdWPA

| Amplitude (A.U) | Peak Position (ppm) | Linewidth (ppm) | Gauss – Lorentz Ratio |
| --- | --- | --- | --- |
| 9.007 ± 3.391 | 75.716 ± 0.219 | 1.293 ± 0.251 | 3.401e-09 ± NaN |
| 40.033 ± 9.250 | 71.881 ± 0.189 | 2.515 ± 0.281 | 3.393e-07 ± 0.427 |
| 102.316 ± 8.060 | 64.506 ± 0.151 | 3.499 ± 0.242 | 1.000 ± NaN |
| 92.875 ± 34.717 | 42.399 ± 0.496 | 5.008 ± 0.500 | 0.305 ± 0.276 |
| 87.182 ± 42.751 | 32.113 ± 2.238 | 8.000 ± 1.767 | 6.178e-08 ± 0.409 |
| 23.658 ± 7.682 | 17.896 ± 0.453 | 3.749 ± 0.57 | 3.960e-09 ± NaN |

Number of scans = 24000

D1 = 3.5s

P15 = 200μs

Mest re nova settings:

Apodization = Exp 80 Hz. Phase 0th order = -20.49 Hz. Phase 1st order = 30 Hz.

Baseline correction fit = Polynomial order 3

10 wt.% PdWPA

| Amplitude (A.U) | Peak Position (ppm) | Linewidth (ppm) | Gauss – Lorentz Ratio |
| --- | --- | --- | --- |
| 6.737 ± 6.369 | 82.067 ± 0.390 | 1.687 ± 0.607 | 0.652 ± 0.940 |
| 2.780 ± 44.321 | 75.557 ± 2.881 | 2.540 ± 11.133 | 0.967 ± 11.012 |
| 52.465 ± 74.396 | 70.940 ± 0.213 | 2.984 ± 1.399 | 0.942 ± 1.113 |
| 47.586 ± 29.291 | 65.640 ± 0.341 | 3.483 ± 0.408 | 0.664 ± 0.387 |
| 120.601 ± 23.414 | 41.949 ± 0.805 | 5.721 ± 0.585 | 0.038 ± 0.240 |
| 12.737 ± 93.743 | 33.469 ± 1.131 | 2.754 7.462 | 1.000 ± 4.886 |
| 18.787 ± 75.803 | 29.371 ± 2.810 | 4.168 ± 3.704 | 0.760 ± 2.953 |
| 14.986 ± 12.097 | 19.668 ± 0.641 | 3.461 ± 0.685 | 0.098 ± 0.972 |

Number of scans = 7000

D1 = 3.5s

P15 = 200μs

Mest re nova settings:

Apodization = Exp 80 Hz. Phase 0th order = -23.46 Hz. Phase 1st order = 30 Hz. Baseline correction fit = Polynomial order 3

5 wt.% PdMeP

| Amplitude (A.U) | Peak Position (ppm) | Linewidth (ppm) | Gauss – Lorentz Ratio |
| --- | --- | --- | --- |
| 14.472 ± 16.987 | 75.177 ± 0.270 | 2.180 ± 0.829 | 0.751 ± 0.504 |
| 73.863 ± 31.333 | 70.449 ± 0.405 | 4.549 ± 1.463 | 0.695 ± 0.241 |
| 44.500± 13.024 | 64.933 ± 0.282 | 3.153 ± 0.268 | 0.679 ± 0.224 |
| 59.836 ± 160.342 | 44.266 ± 0.883 | 4.164 ± 1.729 | 0.379 ± 0.459 |
| 74.803 ± 176.799 | 39.197 ± 7.501 | 5.632 ± 5.675 | 0.021 ± 1.021 |
| 13.071 ± 25.234 | 29.791 ± 1.138 | 3.324 ± 1.456 | 0.005 ± 1.782 |
| 33.190 ± 6.711 | 20.250 ± 0.412 | 4.940 ± 0.365 | 0.042 ± 0.334 |

Number of scans = 22000

D1 = 3.5s

P15 = 200μs

Mest re nova settings:

Apodization = Exp 80 Hz. Phase 0th order = -8 Hz. Phase 1st order = 30 Hz. Baseline correction fit = Polynomial order 3

10 wt.% PdMeP

| Amplitude (A.U) | Peak Position (ppm) | Linewidth (ppm) | Gauss – Lorentz Ratio |
| --- | --- | --- | --- |
| 11.826 ± 14.677 | 76.242 ± 3.131 | 4.422 ± 2.265 | 5.652e-06 ± 1.513 |
| 52.464 ± 68.600 | 68.693 ± 1.600 | 3.494 ± 1.013 | 4.984e-11 ± NaN |
| 39.521 ± 46.097 | 63.254 ± 6.034 | 4.493 ± 3.150 | 7.877e-05 ± 1.743 |
| 78.931 ± 25.835 | 44.642 ± 0.473 | 4.433 ± 0.350 | 1.984e-04 ± 0.477 |
| 49.288 ± 20.724 | 36.402 ± 2.131 | 6.159 ± 1.466 | 8.052e-05 ± 0.923 |
| 6.123 ± 5.923 | 21.372 ± 0.372 | 1.795 ± 0.446 | 9.6972e-07 ± 2.243 |
| 5.589 ± 3.209 | 17.522 ± 0.284 | 1.431 ± 0.296 | 4.290e-07 ± 1.299 |

Number of scans = 6700

D1 = 3.5s

P15 = 200μs

Mest re nova settings:

Apodization = Exp 80 Hz. Phase 0th order = -11.36 Hz. Phase 1st order = 30 Hz. Baseline correction fit = Polynomial order 3

Figure S3. Pd K-edge ex situ XAS data acquired for Pd(0) foil and Pd(II)O reference materials. A) XANES region, b) 1st Derivative XANES, c) FT EXAFS data. Spectroscopic data was acquired during ex situ XAS measurements within the paper on the B18 beamline at the Diamond Light Source, U.K.

Figure S4. Pd K-edge Chi (Χ) EXAFS data acquired to k = 14 for the WPA and MeP series of Pd/TiO2 catalysts. A) displays the chi EXAFS data for the Pd0 and Pd(II)O measured references, b) chi EXAFS data for the WPA series of catalysts, c) chi EXAFS data for the MeP series of catalysts. All references and samples were measured as ex-situ pellets on the B18 beamline at the Diamond Light Source, Harwell, U.K.

Figure S5. Fitting of the FT EXAFS data acquired for the WPA and MeP Pd/TiO2 series of catalysts. 1st shell EXAFS fitting parameters were derived from the k2 weighted Fourier transform data for the Pd K-edge EXAFS for fresh catalysts. The amplitude reduction factor (S02) = 0.81, was determined through fitting of an acquired Pd metal reference foil using a crystallographic file. EXAFS fitting range: 3 < k < 13.5, 1< R < 3.5, number of independent points = 16.5.

Figure S6. Fitting of the k-space EXAFS data acquired for the WPA and MeP Pd/TiO2 series of catalysts. 1st shell EXAFS fitting parameters were derived from the k2 weighted Fourier transform data for the Pd K-edge EXAFS for fresh catalysts. The amplitude reduction factor (S02) = 0.81, was determined through fitting of an acquired Pd metal reference foil using a crystallographic file. EXAFS fitting range: 3 < k < 13.5, 1< R < 3.5, number of independent points = 16.5.

Figure S7. CO probe FTIR spectra of 10PdWPA.

Figure S8. Schematic of reaction pathways in furfural hydrogenation to value added products.

Figure S9. Selectivity plots as a function of reaction time acquired during the hydrogenation of furfural over the prepared fresh catalysts. A) Selectivity to furfuryl alcohol, b) selectivity to hydrofurfuryl alcohol, c) selectivity to 2-methyltetrahydrofurfuryl (2-MTHF).

1.	Tierney, G. F. et al. Controlling the Production of Acid Catalyzed Products of Furfural Hydrogenation by Pd/TiO2. ChemCatChem 13, 5121–5133 (2021).