# Sustainable Vegetable Tanning: Ultrasound-Assisted Tannin Extraction of Oak Bark and Analytical Approaches to Collagen–Tannin Interactions

Ilaria Quaratesi1,2, Vittoria Ferrara3, Ioan Călinescu4, Petre Chipurici4, Ioana Popa4, Cristina Carşote5*, Pellegrino La Manna6, Elena Badea2,7,8*

1Industrial Chemistry Department “Toso Montanari”, Alma Mater Studiorum-University of Bologna, Ue4 via Gobetti 85, 80129, Bologna, Italy.

2National Research and Development Institute for Textile and Leather, Research Institute for Leather and Footwear (INCDTP-ICPI), Strada Ion Minulescu 93, Sector 3, 031215, Bucharest, Romania.

3Department of Chemistry and Biology “A. Zambelli”, University of Salerno, Via Giovanni Paolo II 132, I-84084, Fisciano (SA), Italy.

4Faculty of Chemical Engineering and Biotechnologies, National University of Science and Technology Politehnica Bucharest, Strada Gheorghe Polizu 1-7, Sector 1, 011061, Bucharest, Romania.

5Center for Research and Physical-Chemical and Biological Investigations, National Museum of Romanian History, Calea Unirii 12, Bucharest, Romania.

6Water Science and technology group (WaSTe), Department of Civil Engineering, University of Salerno, Via Giovanni Paolo II 132, 84084, Fisciano (SA), Italy.

7Department of Chemistry, Faculty of Sciences, University of Craiova, Calea Bucuresti 107, Craiova, Romania.

8The Research Institute of the University of Bucharest, Șoseaua Panduri 90, Sector 5, 050663, Bucharest, Romania.

Table S1. Phenols extraction yield obtained using the UAE method and DFR equipment (plant material to solvent ratio of 1/10, T = 50 °C, particle size < 400 μm), according to our previous work [1]. DM: mean dry matter; GAE: gallic acid equivalents; DE: Dry Extract.

| Extract symbol | N0.1 | N0.2 | N0.5 | W | S |
| --- | --- | --- | --- | --- | --- |
| Solvent | NaOH 0.1% | NaOH 0.2% | NaOH 0.5% | Water | 0.25% Na2SO3/0.25% NaHSO3 |
| Dry extract (mg/g DM) | 111.8±0.8 | 146.7±1.6 | 196.5±3.2 | 100.5±1.1 | 159.5±3.5 |
| TPC (mg GAE/g DE) | 0.57 | 0.45 | 0.37 | 0.58 | 0.46 |

## Table S2. ATR-FTIR characteristic bands of aqueous tanning extracts.

| Main vibrational bands of tanning extracts (wave numbers, cm−1, intensity) |  | W | S | N01 | N02 | N05 |
| --- | --- | --- | --- | --- | --- | --- |
| Hydrolysable tannins' bands |  |  |  |  |  |  |
| I | 1724 cm-1, C=O stretching of phenolic esters of hydrolysable tannins, especially derivatives of gallic acid | w | - | - | - | - |
| VII | (1313 – 1317) cm-1, C-O stretching of lactones / O-H deformation | m | vs | vs | m | m |
| Condensed tannins' bands |  |  |  |  |  |  |
| VIII | (1260 – 1281) cm-1, C–O stretching of pyran, typical of flavonoid C-rings | m | vs | vs | s | s |
|  |  | m | m | w | sh | sh |
| IX | (1102 – 1110) cm-1 | vs | m | m | m | w |
| XII | (994 – 1004) cm-1 | m | m | w | sh | sh |
| XIV | (819 – 826) cm-1 | m | m | m | s | s |
| Vegetable tannins common bands |  |  |  |  |  |  |
| II | (1606 – 1611) cm-1, aromatic ring stretch vibrations/adsorbed water | vs | vs | s | m | w |
| IV | (1445 – 1453) cm-1, C=O stretching of aromatic rings | vs | vs | s | m | w |
| III | (1509 – 1512) cm-1, C=C skeletal vibration of the aromatic rings | vs | s | s | m | sh |
| XI | (1026 – 1031) cm-1, b=C-H deformation | s | s | w | w | sh |
| Gallotannins bands |  |  |  |  |  |  |
| X | (1067 – 1071) cm-1, C-O-C aryl phenolic esters | vs | w | w | w | w |
| XIII | (867 – 872) cm-1 | w | m | m | m | sh |
| Lignin bands |  |  |  |  |  |  |
| V | 1413 cm-1, aromatic skeleton vibrations, common to tannins and lignin | - | - | - | w | s |
| VI | (1365 – 1369) cm-1, phenolic stretch vibration of OH and aliphatic CH deformation in methyl groups, common to lignin | - | - | m | m | s |

vs - very strong; s - strong; m - medium; w - weak; sh – shoulder

In the micro-pilot test, the tanning process was performed in 120 mm wide and 300 mm diameter drums. About 50 g of pickled sheepskin, 350 g of extract, and 0.5g of NaCl were used for each batch. Adding NaCl in leather processing generally has a favourable impact on leather quality due to its ability to improve tannin penetration and fixation through the opening up of the collagen fiber network and the porosity of the leather [2].

The hides were soaked for 6 days at about 30 °C. They were tumbled three times a day for 30 minutes. The initial pH of the raw hides was adjusted to 4.5, and it was monitored during tanning by adding a 10% w/v solution of NaHCO3 to prevent it from falling below 3.8. To ensure that the hide was absorbing sufficient tanning substances, the hides were removed on the 3rd day and wrung out to allow fresh tannins to be absorbed after a portion of 50 g of fresh extract had been added. After the 5th day, the pH was raised to 4.2 to fix the tannins in the hide structure. After the 6th day, the tanned hides were washed and left on a stand overnight. The next day, the hides were again soaked in water and drummed for another 12 hours. The pH was adjusted to a final value of 5.5 with sodium formate solution. The hides were then left to stand overnight before oiling them. 13g of polyol AK and 13g of Sulphirol EG60 were used for oiling without the addition of any retanning agent. After these steps, the tanned hides can be considered as leather. Small pieces of about 50 g were kept unoiled for micro-DSC and 1H unilateral NMR analysis, which are affected by the oil presence, while physical-mechanical tests were carried out on oiled leather.

## Table S3. Tanning formulation and process on micro pilot scale.

| Tanning formulation - sheep hide a,b |  |  |  |
| --- | --- | --- | --- |
| Products | % w/w | g | Note |
| Extracts | 700 | 350 | T=30 °C, pH 4.5 ± 0.5 |
| NaCl | 10 | 0.5 |  |
| Hide | 100 | 50 |  |
|  |  |  | pH final = 4.2 ± 0.1 |
| 6 days in the tanning float, wash and drain |  |  |  |
| Hide | 100 | 50 | T=30 °C, pH = 4.5 ± 0.5 |
| HCOONa | 0.5 | 0.25 |  |
| H2O | 250 | 125 |  |
| Polyol AKc | 5 | 0.25 | pH = 5.5 ± 0.5 |
| Sulphirol EG60 c | 5 | 0.25 |  |
| Wash, drain and dry |  |  |  |
| a The percentage of added products in each process is related to weight of hides. That is, if we are working with 100 g of hides, we must add 700 g of extract per each process. b The actual weight of the leather is calculated on half of the real weight since the leather is weighed wet. c Applied only on the portion of leather for the physical mechanical tests. |  |  |  |

References:

1. 	Quaratesi, I.; Calinescu, I.; Lavric, V.; Ferrara, V.; Badea, E.; Chipurici, P.; Dumbravă, E.-G.; Constantinescu, R.-R.; Ignat, N.D.; Popa, I. Loop-Ultrasound-Assisted Extraction: An Efficient Approach for the Recovery of Bioactive Compounds from Oak Bark. Agronomy 2024, 14, 1452, doi:10.3390/agronomy14071452.

2. 	Li, X.; Wang, Y.N.; Li, J.; Shi, B. Effect of Sodium Chloride on Structure of Collagen Fiber Network in Pickling and Tanning. JALCA 2016, 111, 230–237.