Supplemental Materials for “Rheological control of cementitious composites incorporating ceramic wastes for 3D printing applications”

Lucia Ferrari1,*, Giacomo Rizzieri2, Liberato Ferrara2, and Elisa Franzoni1

1 Department of Civil, Chemical, Environmental, and Materials Engineering (DICAM)

University of Bologna - Via Terracini 28, 40131, Bologna, Italy

2 Department of Civil and Environmental Engineering, Polytechnic of Milan - Piazza Leonardo da Vinci 32, 20133 Milano, Italy

*corresponding author: lucia.ferrari9@unibo.it, ORCID ID 0000-0001-6785-9977

Supplementary Tables

Supplementary Table 1 – Mineralogical composition of CEM I, LS and CC by X-ray diffraction according to DIN EN 13925‑2 procedure and Rietveld refinement.

| Cement notation/mineralogical name | Chemical Formula | CEM I (%) | LS (%) | CC (%) |
| --- | --- | --- | --- | --- |
| C3S | Ca3SiO5 | 61.80 | - | - |
| C2S | Ca2SiO4 | 8.19 | - | - |
| C3A | Ca3Al2O6 | 6.00 | - | - |
| C4AF | Ca2(Al. Fe)2O5 | 11.10 | - | - |
| Portlandite | Ca(OH)2 | 1.19 | - | - |
| Periclase | MgO | 0.72 | - | - |
| Arcanite | K2SO4 | 1.40 | - | - |
| Syngenite | K2Ca(SO4)2 · H2O | 0.96 | - | - |
| Anhydrite | CaSO4 | 1.71 | - | - |
| Dihydrate calcium sulfate | CaSO4 · 2H2O | 0.45 | - | - |
| Hemihydrate calcium sulfate | CaSO4 · 1/2H2O | 2.45 | - | - |
| Quartz | SiO2 | 0.25 | - | 22.8 |
| Calcite | CaCO3 | 3.21 | 99.39 | - |
| Dolomite | CaMg(CO3)2 | 0.64 | 0.61 | - |
| Hematite | Fe2O3 | - | - | 3.9 |
| Anatase + Rutile | TiO2 | - | - | 1.3 |
| Amorphous | - | - | - | 72.1 |

Supplementary Table 2 – Reactivity index of calcined clay and ceramic wastes measured according to the standard ASTM C1897-20 [1] and by thermogravimetric analysis (TGA) after 7 days. Mechanical strength of LC3 mortars prepared and cured at for 28 days according to the standard EN 197-1:2011 [2].

|  | CC | CW1 | CW2 | CW3 | CW4 | CW5 | CW6 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Bound water at 7 days (%) | 10.5 | 4.2 | 2.6 | 3.5 | 1.4 | 3.5 | 3.5 |
|  | LC3-CC | LC3-CW1 | LC3-CW2 | LC3-CW3 | LC3-CW4 | LC3-CW5 | LC3-CW6 |
| Compressive strength at 28 days (MPa) | 48.1 ± 1.76 | 35.7 ± 0.63 | 35.1 ± 1.12 | 30.0 ± 0.34 | 29.5 ± 0.68 | 34.1 ± 3.09 | 34.0 ± 1.14 |

References

[1]	ASTM International, “ASTM C1897-20 Standard Test Methods for Measuring the Reactivity of Supplementary Cementitious Materials by Isothermal Calorimetry and Bound Water Measurements 1.” doi: 10.1520/C1897-20.

[2]	EN 197-1:2011 Cement. Part 1, Composition, specifications and conformity criteria for common cements. British Standards Institution, 2019, p. 56.