Supporting Information

Novel biobased poly(trimethylene 2,5-furanoate-co-trimethylene dodecanedioate) PTFcoDod copolymers for sustainable packaging

Giulia Guidotti a, Agata Zubkiewicz b, Anna Szymczyk c, Rafael Sablong d, Michelina Soccio a, Valentina Siracusa e, Nadia Lotti a

aDepartment of Civil, Chemical, Environmental, and Materials Engineering, University of Bologna, Via Terracini 28, 40131 Bologna, Italy

b Institute of Mathematics, Physics and Chemistry, Maritime University of Szczecin, Wały Chrobrego 1, 2,70-500 Szczecin, Poland

c Faculty of Mechanical Engineering and Mechatronics, West Pomeranian University of Technology, Al. Piastów 19, PL 70-310 Szczecin, Poland

d Polymer Technology Group/Eindhoven (PTG/e) B.V., De Lismortel 31, 5612 AR Eindhoven, The Netherlands

e Department of Chemical Science, University of Catania, Catania, Italy

*Corresponding authors: aszymczyk@zut.edu.pl (Anna Szymczyk); nadia.lotti@unibo.it (Nadia Lotti)

*Corresponding authors: aszymczyk@zut.edu.pl (Anna Szymczyk); nadia.lotti@unibo.it (Nadia Lotti)

Molecular characterization

Based on the signals obtained from 1H NMR (Fig. 1S), the actual compositions of TDod units (TDodB) (eq. 1S), number average sequence length of TF and TDod repeating units (Ln,TF, Ln,TDod) (eq. 2S-3S) and the degree of randomness (R) (eq. 4S) of the copolymers were calculated as follows:

φTDodB mol %= Ib3+Ib4Ib1+Ib2+Ib3+Ib4∙100%		(1S)

Ln,TF=1+Ic1Ic2						(2S)

Ln,TDod=1+Ic3Ic2						(3S)

R=1Ln,TF+1Ln,TSub						(4S)

where Ib1, Ib2, Ib3, Ib4, Ic1, Ic2, Ic3 represent the integrals of the corresponding peaks (Fig. 1S).

a)

b)

Fig. 1S. 1H-NMR spectra of PTF and PTFcoDod copolymers.

ATR-FTIR measurements were performed using a Bruker Tensor-27 spectrometer with an ATR attachment in the wavenumber range from 400 to 4000 cm-1, with a resolution of 2 cm-1 and results are presented in Fig. 2S and and corresponding data in Table 1S.

Fig. 2S. FTIR spectra of PTF and PTFcoDod copolymers.

Table 1S.  FTIR data for PTF and PTFcoDod copolymers.

| Typ of vibration |  | Wavenumber (cm-1) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | PTT | PTF5PTDod | PTF15PTDod | PTF25PTDod | PTF35PTDod | PTF45PTDod | PTF55PTDod |
| C-H stretching vibrations in the furan ring | 3121 | 3124 | 3120 | 3120 | 3120 | 3120 | 3120 |
| C–H stretching vibration (CH2) | 2923 2850 | 2923 2850 | 2924 2853 | 2924 2850 | 2924 2851 | 2924 2852 | 2918 2851 |
| C=O stretching vibration | 1720 | 1720 | 1720 | 1724 | 1721 | 1723 | 1723 |
| C=C ring stretching vibrations of the furan rings | 1580 | 1580 | 1576 | 1578 | 1578 | 1578 | 1578 |
| -CH- deformation and wagging vibrations | 1506 1464 | 1506 1468 | 1506 1468 | 1506 1467 | 1506 1469 | 1506 1469 | 1506 1470 |
| asymmetric and symmetric stretching vibrations of the ester C-O-C groups | 1268 1140 | 1265 140 | 1267 140 | 1270 1140 | 1270 1140 | 1270 1140 | 1270 1140 |
| =C-O-C= ring vibrations of the furan ring | 1023 | 1023 | 1023 | 1023 | 1023 | 1021 | 1021 |
| C-H out-of-plane deformation vibrations of the furan ring) | 964 826 766 | 964 826 766 | 964 826 766 | 964 825 766 | 964 825 766 | 964 825 766 | 964 825 766 |

Fig. 3S. DSC heating and cooling  scans for PTF and PTFcoDod copolymers at a rate of 1, 3, 5 and 10ºC/min (the dashed lines represent the first heating scans at 10°C/min).

X-ray diffraction and thermal properties of PTF and PTFcoDod copolymers

Fig. 4S. X-ray diffraction (XRD) curves of PTF and PTFcoDod copolymers before (dashed lines) and after annealing.  PTF, PTF5Dod, PTF15Dod annealed at 100 °C, 1 h; PTF25Dod, PTF35Dod, PTF45Dod annealed at 70 °C, 1 h; PTF55Dod annealed at 50 °C, 1 h.

Fig. 5S. TGA and DTG traces for PTF and PTFcoDod copolymers in inert (a, b) and oxidizing (c, d) atmosphere.

Table 2S. TGA data of PTF and PTFcoDod copolymers.

| Sample | Argon |  |  |  |  | Air |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Td5% (°C) | Td15% (°C) | Td50% (°C) | TDTG (°C) | R600 (%) | Td5% (°C) | Td15% (°C) | Td50% (°C) | TDTG1 (°C) | TDTG2 (°C) | R600 (%) |
| PTF | 364 | 377 | 393 | 391 | 4.4 | 360 | 376 | 396 | 393 | 491 | 2.5 |
| PTF5Dod | 367 | 379 | 397 | 394 | 8.0 | 361 | 376 | 396 | 393 | 492 | 2.8 |
| PTF15Dod | 363 | 378 | 397 | 396 | 4.9 | 363 | 378 | 397 | 395 | 519 | 1.1 |
| PTF25Dod | 370 | 382 | 401 | 397 | 9.2 | 360 | 380 | 401 | 397 | 527 | 1.4 |
| PTF35Dod | 370 | 384 | 405 | 400 | 9.2 | 369 | 383 | 403 | 400 | 525 | 1.2 |
| PTF45Dod | 368 | 384 | 406 | 402 | 6.2 | 364 | 380 | 403 | 399 | 515 | 1.1 |
| PTF55Dod | 370 | 386 | 411 | 406 | 7.8 | 367 | 382 | 404 | 398 | 512 | 2.4 |

Td5%, Td15%, Td55% - temperature corresponding to 5, 15 and 50 % weight loss respectively; TDTG1, TDTG2 - temperatures at maximum of weight loss rate; R600 – residue at 600˚C.

Tensile properties

Fig. 6S. Representative stress-strain curves for non-annealed and annealed PTF and copolymeric samples.

Gas barrier properties

Table 3S. GTR data of PTF and PTFcoDod copolymers.

| Sample | PTF | PTF5Dod | PTF15Dod | PTF25Dod | PTF35Dod | PTF45Dod | PTF55Dod |
| --- | --- | --- | --- | --- | --- | --- | --- |
| O2-TR [cm3cm m-2d-1atm-1] | 0.08 ±0.01 | 0.17 ±0.02 | 0.51 ±0.04 | 1.93 ±0.10 | 5.21 ±0.30 | 13.4 ±0.90 | 23.4 ±1.10 |
| CO2-TR [cm3cm m-2d-1atm-1] | 0.05 ±0.001 | 0.22 ±0.001 | 0.50 ±0.03 | 2.49 ±0.20 | 13.60 ±0.50 | 40.50 ±1.20 | 71.60 1.60 |

Changes of  thermal properties of PTF and copolymers during composting

Fig. 7S. I scan DSC curves of samples after 1, 3 and 6 months in compost  and their blanks (58 °C, no compost).

Table 4S. Thermal characterization data of partially degraded PTF and PTFcoDod copolymers together with the relative blanks (58 °C, no compost).

| Sample | Incubation time | Tg | DCp | Tm1 | Tm2 | Tm3 | DHm |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | (month) | (ºC) | (Jg-1 ºC-1) | (ºC) | (ºC) | (ºC) | (Jg-1) |
| PTF | 0 | 62 | 0.39 | - | - | - | - |
|  | 1 (blank) | 62 | 0.19 | 97 | - | 165 | 8; 31 |
|  | 1 | 69 | 0.33 | 103 | - | 165 | 9; 32 |
|  | 2 (blank) | 65 | 0.28 | 98 | - | 165 | 9; 33 |
|  | 2 | 69 | 0.30 | 105 | - | 166 | 9; 32 |
|  | 3 (blank) | 66 | 0.23 | 99 | - | 165 | 9; 33 |
|  | 3 | 69 | 0.27 | 106 | - | 166 | 10; 33 |
|  | 4 (blank) | 63 | 0.21 | 97 | - | 166 | 8; 32 |
|  | 4 | 66 | 0.17 | 106 | - | 166 | 10; 33 |
|  | 5 (blank) | 60 | 0.17 | 96 | - | 165 | 8; 34 |
|  | 5 | 65 | 0.17 | 106 | - | 166 | 10; 34 |
|  | 6 (blank) | 61 | 0.11 | 102 | - | 165 | 10; 31 |
|  | 6 | 63 | 0.17 | 106 | - | 166 | 10; 35 |
| PTF5PTDod | 0 | 48 | 0.41 | - | - | - | - |
|  | 1 (blank) | - | - | 64 | 95 | 158 | 4; 7; 28 |
|  | 1 | - | - | 63 | 98 | 158 | 4; 8; 29 |
|  | 3 (blank) | - | - | 63 | 97 | 159 | 4; 8; 30 |
|  | 3 | - | - | 62 | 99 | 159 | 3; 8; 31 |
|  | 6 (blank) | - | - | 63 | 98 | 160 | 3; 8; 32 |
|  | 6 | - | - | 62 | 101 | 160 | 3; 9; 41 |
| PTF15PTDod | 0 | 31 | 0.21 | 64 | - | 138 | 7; 34 |
|  | 1 (blank) | 26 | 0.18 | 92 | 125 | 141 | 10; 5; 20 |
|  | 1 | 26 | 0.21 | 95 | 124 | 142 | 8; 22 |
|  | 3 (blank) | 25 | 0.23 | 96 | 122 | 144 | 7; 2; 26 |
|  | 3 | 23 | 0.19 | 98 | 122 | 146 | 6; 25 |
|  | 6 (blank) | 23 | 0.16 | 97 | - | 147 | 8;31 |
|  | 6 | 23 | 0.23 | 102 | - | 147 | 7; 33 |
| PTF25PTDod | 0 | 0 | 0.23 | 63 | - | 122 | 7; 25 |
|  | 1 (blank) | -5 | 0.22 | 89 | - | 126 | 12; 22 |
|  | 1 | -3 | 0.20 | 92 | - | 128 | 14; 25 |
|  | 3 (blank) | -12 | 0.17 | 97 | - | 135 | 11; 31 |
|  | 3 | -7 | 0.15 | 103 | - | 136 | 15; 34 |
| PTF35PTDod | 0 | -15 | 0.32 | 62 | - | 104 | 6; 28 |
|  | 1 (blank) | -19 | 0.27 | 56 | - | 89; 107 | 1; 30 |
|  | 1 | -18 | 0.27 | 57 | - | 96; 110 | 2; 33 |
| PTF45PTDod | 0 | -27 | 0.42 | - | 60 | 90 | 16; 21 |
|  | 1 (blank) | -29 | 0.30 | -9 | 51 | 89 | 1; 6; 22 |
|  | 1 | -29 | 0.30 | -9 | 49 | 90 | 4; 22 |
| PTF55PTDod | 0 | -28 | 0.39 | -6 | - | 54; 78 | 6; 27 |
|  | 1 (blank) | -30 | 0.41 | -6 | 42; 48 | 80 | 7; 16; 13 |
|  | 1 | -29 | 0.39 | -5 | 42; 49 | 82 | 6; 14; 13 |

Fig. 8S. 1H-NMR spectra (4.10-4.70 ppm) of PTF5Dod, PTF15Dod and PTF25Dod copolymers before (top) and  after (bottom) 4 months in compost.

Fig. 9S. 1H-NMR spectra (3.55-4.15 ppm) of PTF5Dod, PTF15Dod and PTF25Dod copolymers before (top) and after (bottom) 4 months in compost.