Frontal Polymerization of Acrylamide/GelMA/Gelatin Hydrogels with Controlled Mechanical Properties and Inherent Self-Recovery

Luana Di Lisaa,‡, Mariangela Reaa,‡,Daniele Nuvolib*, Maria Letizia Focaretea,c* Cristiano Albonettid, Alberto Marianib

aDepartment of Chemistry ‘Giacomo Ciamician’ and INSTM UdR of Bologna, University of Bologna, via Selmi 2, 40126 Bologna, Italy

bDepartment of Chemical, Physical, Mathematical and Natural Sciences, University of Sassari, and local INSTM Unit, via Vienna 2, 07100 Sassari, Italy

cInterdepartmental Center for Industrial Research in Health Sciences and Technologies, University of Bologna, Via Tolara di Sopra, 41/E, 40064 Ozzano Emilia, Bologna, Italy

dConsiglio Nazionale delle Ricerche – Institute for the study of nanostructured materials (CNR-ISMN), Via P. Gobetti 101, 40129 Bologna, Italy

‡These authors contributed equally.

*Corresponding authors. E-mail addresses: dnuvoli@uniss.it (Daniele Nuvoli), marialetizia.focarete@unibo.it (Maria Letizia Focarete)

Table S1. Tmax and Vf for reference samples, AAm-GELMA copolymer networks, Semi-IPN AAm-GELMA and gelatin.

| Sample code | GelMA methacrylic groups (mol%) | AAm/gelatin weight ratio | Tmax (°C) | Vf (cm/min) |
| --- | --- | --- | --- | --- |
| PAAm | - | - | 103 | 0.45 |
| cag30-004 | 0.004 |  | 101 | 0.45 |
| CAG30-02 | 0.02 |  | 100 | 0.35 |
| CAG30-04 | 0.04 | - | 97 | 0.30 |
| CAG30-06 | 0.06 | - | 94 | 0.25 |
| CAG75-01 | 0.10 |  | 103 | 0.45 |
| CAG75-05 | 0.05 | - | 104 | 0.45 |
| CAG75-10 | 0.10 | - | 105 | 0.45 |
| CAG75-14 | 0.14 | - | 97 | 0.35 |
| SAG30-20 | 0.04 | 20:1 | 101 | 0.30 |
| SAG30-10 | 0.04 | 10:1 | 97 | 0.30 |
| sag30-07 | 0.04 | 7:1 | 96 | 0.30 |
| SAG30-03 | 0.04 | 3:1 | 99 | 0.30 |
| SAG75-20 | 0.04 | 20:1 | 105 | 0.45 |
| SAG75-10 | 0.04 | 10:1 | 105 | 0.45 |
| sag75-07 | 0.10 | 7:1 | 102 | 0.45 |
| SAG75-03 | 0.10 | 3:1 | 102 | 0.40 |

Table S2. Thermogravimetric analysis (TGA) data obtained for reference samples, AAm-GELMA copolymers, Semi-IPN AAm-GELMA and gelatin.

| Sample | Degradation stages (Tdegr (°C) and WeightLoss (%)) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 1° |  | 2° |  | 3° |  | 4° |  |
| Reference sample |  |  |  |  |  |  |  |  |
| Gelatin | - | - | 319 | 68 | - | - | - | - |
| GelMA30 |  |  | 330 | 63 |  |  |  |  |
| GelMA75 | - | - | 321 | 68 | - | - | - | - |
| PAAm | 296 | 14 | - | - | - | - | 394 | 45 |
| AAm-GelMA copolymer networks |  |  |  |  |  |  |  |  |
| CAG30-04 | 297 | 23 | - | - | nd | nd | 390 | 42 |
| CAG75-10 | 293 | 13 | - | - | nd | nd | 405 | 50 |
| Semi-IPN AAm-GelMA and gelatin |  |  |  |  |  |  |  |  |
| SAG30-20 | 294 | 15 | - | - | nd | nd | 400 | 37 |
| SAG30-10 | 297 | 15 | - | - | nd | nd | 397 | 38 |
| SAG30-03 | 289 | 12 | - | - | nd | nd | 391 | 41 |
| SAG75-20 | 288 | 12 | - | - | 351 | 15 | 408 | 40 |
| SAG75-10 | 287 | 12 | - | - | 350 | 14 | 406 | 39 |
| SAG75-03 | 287 | 14 | - | - | 350 | 18 | 408 | 36 |

and = not detectable

Table S3. Summary of the elastic (Gʹ) and loss (Gʺ) moduli, crossover point for hydrogel samples (Amplitude Sweep Test).

| Sample | Gʹ (Pa) | Gʺ (Pa) | Crossover Point (%) |
| --- | --- | --- | --- |
| Reference sample |  |  |  |
| PAAm | 635 | 80 | - |
| AAm-GelMA copolymer networks |  |  |  |
| CAG30-04 | 446 | 58 | 1000 |
| CAG75-10 | 6820 | 222 | 2 |
| Semi-IPN AAm-GelMA and gelatin |  |  |  |
| SAG30-20 | 43 | 4 | 100 |
| SAG30-10 | 34 | 5 | 318 |
| SAG30-03 | 86 | 4 | 10 |
| SAG75-20 | 1603 | 80 | 3 |
| SAG75-10 | 1232 | 36 | 5 |
| SAG75-03 | 3412 | 144 | 4 |

Table S4. Summary of Gʹ and Gʺ moduli (at 5°C and 60°C), and softening point temperature data for hydrogel samples (Temperature Sweep).

| Sample | Gʹ (Pa) | Gʺ (Pa) | Gʹ (Pa) | Gʺ (Pa) | Soft. Point Temp. (°C) |
| --- | --- | --- | --- | --- | --- |
|  | at 5°C |  | at 60°C |  |  |
| Reference sample |  |  |  |  |  |
| PAAm | 324 | 25 | 312 | 21 | - |
| AAm-GelMA copolymer networks |  |  |  |  |  |
| CAG30-04 | 925 | 175 | 123 | 34 | 34 |
| CAG75-10 | 1215 | 135 | 1084 | 254 | - |
| Semi-IPN AAm-GelMA and gelatin |  |  |  |  |  |
| SAG30-20 | 91 | 6 | 4 | 2 | 36 |
| SAG30-10 | 108 | 5 | 7 | 2 | 39 |
| SAG30-03 | 152 | 21 | 8 | 2 | 41 |
| SAG75-20 | 909 | 91 | 601 | 117 | - |
| SAG75-10 | 2957 | 504 | 1456 | 210 | - |
| SAG75-03 | 2551 | 25 | 822 | 99 | - |

Figure S1. Frequency Sweep experiments. Gʹ and Gʺ as a function of the applied angular frequency (rad/s) for A) for reference samples and AAm-GelMA copolymer networks and B,C,D,E) for Semi-IPN AAm-GelMA and gelatin.

Figure S2. Experimental data referring to SAG30-10 and SAG75-10 samples. (A) Temperature Sweep experiments. Gʹ and Gʺ as a function of temperature (°C) (B) Dynamic strain sweep experiments. Gʹ and Gʺ as a function of the time applying a cyclic low-high strain sweep at a low strain of 1% and high strain of 300%. (C) Compression stress-strain tests and (D) Recovery cyclic compression stress-strain tests, without intervals. (E) Energy of dissipation.

Table S5. Et30, fracture stress and strain obtained by INSTRON compression tests.

| Sample code | Et30a (KPa) | Fracture stress (KPa) | Fracture strain % |
| --- | --- | --- | --- |
| Reference sample |  |  |  |
| PAAm | 0.013 ± 0.004 | 6.24 ± 2.45 | 99.00 ± 11.65 |
| AAm GelMA copolymer networks |  |  |  |
| CAG30-04 | 0.006 ± 0.002 | 18.20 ± 10.98 | 155.00 ± 0.87 |
| CAG75-10 | 0.02 ± 0.01 | 1.90 ± 0.93 | 117.00 ± 13.00 |
| Semi-IPN AAm-GelMA and gelatin |  |  |  |
| SAG30-20 | 0.008 ± 0.002 | 6.60 ± 2.49 | 125.00 ± 17.31 |
| SAG30-10 | 0.005 ± 0.001 | 0.52 ± 0.29 | 109.40 ± 0.07 |
| SAG30-03 | 0.009 ± 0.001 | 2.92 ± 1.58 | 90.16 ± 18.38 |
| SAG75-20 | 0.017 ± 0.001 | 11.41 ± 2.30 | 155.45 ± 12.45 |
| SAG75-10 | 0.030 ± 0.002 | 13.69 ± 3.69 | 105.31 ± 19.09 |
| SAG75-03 | 0.017 ± 0.002 | 23.52 ± 1.67 | 125.00 ± 12.34 |

a Tangent modulus calculated at strain = 30%.